Section Cover Page

Section 02 82 15 2018-01-22 Asbestos Encapsulation

Use this Section in conjunction with Section 02 82 01 - Asbestos Control General Requirements and Section 02 82 05 - Asbestos Containment Procedures.

Edit this Section only in consultation with Infrastructure specialists in asbestos control procedures.

This Technical Specification Section contains:

.1	This Cover Sheet

.2	Data Sheet - General

.3	Specification Section Text:

1.	General

1.1	Intent

1.2	Related Sections

2.	Products

  - Asbestos Encapsulant

3.	Execution

3.1	Asbestos Encapsulation Procedure

3.2	Asbestos Encapsulation Schedule

Encapsulation is an interim method of controlling asbestos.  Prior to specifying encapsulation, ensure that this is the most appropriate asbestos control method.

Limit use of encapsulation to the following applications:

.1	Areas which will not be subject to physical damage or contact.

.2	Asbestos substrates which are capable of supporting themselves and the additional weight of the encapsulation sealant.

.3	Areas where fire rating will not be compromised by application of encapsulation sealant.

Other considerations:

.1	Asbestos will eventually have to be removed.

.2	Routine inspections are required of encapsulated areas to check for deterioration and damage. Damage may be considered high-risk abatement in accordance with Section 4.2 of the Alberta Asbestos Abatement Manual (current edition).

1.	General

1.1	INTENT

.1	Read this Section in conjunction with Section 02 82 01 - Asbestos Control General Requirements.

1.2	RELATED SECTIONS

.1	Asbestos Containment Procedures:	Section 02 82 05.

.2	Asbestos Removal:	Section 02 82 33.

- Products

  - Asbestos Encapsulant

.1	Asbestos Encapsulant:  to CAN/CGSB-1.205-03, Sealer for Application to Asbestos-Fibre-Releasing Materials, Class A - water-based, for spray application, and as follows:

.1	Type 1 – Penetrating Sealant.  Acceptable products are absorbed into the material and bond fibres together.

.2	Type 2 – Surface Coating (Bridging Sealant).  Acceptable products are bonded to the surface of the materials to provide a protective seal.

3.	Execution

3.1	CONTAINMENT

.1	Use full containment procedures in accordance with Section 02 82 05.

3.2	ASBESTOS ENCAPSULATION PROCEDURES

.1	Apply encapsulant at low pressure using airless spray equipment.

.2	Apply [Type 1 – Penetrating Sealant] [Type 2 - Surface Coating (Bridging Sealant)] encapsulant in accordance with manufacturer's instructions and in a manner which minimizes damage to surface of contaminated materials.

.3	Clean up debris which may be dislodged during encapsulation and dispose of as asbestos waste.

3.2	ASBESTOS ENCAPSULATION SCHEDULE

| Location | Substrate | Type of Application | Asbestos Type and Percentage |
| --- | --- | --- | --- |
| [ ] | [ ] | [ ] | [ ] |

SPEC NOTE:  Specify locations in terms which are easily identifiable, such as room number, major building areas or other identification methods which are used on drawings to delineate asbestos control area.

SPEC NOTE:  Identify substrate where asbestos is to be encapsulated, for example:  walls, ceilings, mechanical piping, columns, beams, joists, and underside of decking.

SPEC NOTE:  Identify type of asbestos and percentage of material by weight, for example, 30% Chryostile, 10% Amosite, 5% Crocidolite.

END OF SECTION