Section Cover Page

Section 06 15 00 2011-08-08 Wood Decking

Refer to “LEED Notes and Credits” page for additional guidance for LEED projects. Delete LEED items if project: .1 is excluded by the Department’s policy on LEED, or .2 the Department has determined that the work of this Contract is not to attain a LEED rating.

This Master Specification Section contains:

.1	This Cover Sheet

.2	LEED Notes and Credits

.3	Specification Section Text:

1.	General

1.1	Related Work specified In other Sections

1.2	Product Options and Substitutions

1.3	Reference Documents

1.4	Submittals

1.5	Quality Assurance

1.6	Delivery Storage and Handling

2.	Products

2.1	Description

2.2	Materials

2.3	Accessories

2.4	Wood Treatment

3.	Execution

3.1	Grade

3.2	Pattern

3.3	Pre-Drilled Holes

3.4	Nailing

3.5	Treatment Application

3.7	Cleaning

3.7	Protection

LEED Notes:

Refer to Section 01 35 18 – LEED Requirements for:

- Requirements necessary to obtain points for certification.

- Confirmation of LEED perquisites and credits affecting this Section.  Not all are mandatory for certification.

Maintain built-in sustainability regardless of LEED requirements for:

- Recycling, reuse of materials, components and assemblies.

- Diversion of construction waste from landfills.

- Use of recycled materials, local materials, rapidly renewable and durable materials.

- Maintain healthy indoor environment during constructing.

- Provide for thermal comfort, access to views and daylight for indoor spaces.

- Foster innovation into facility design and planning.

LEED Credits:

1.	Materials & Resources

-	Prereq 1 - Storage & Collection of Recyclables

-	Credit 2 - Construction Waste Management

-	Credit 5 - Regional Materials

-	Credit 6 - Rapidly Renewable Materials

-	Credit 7 - Certified Wood

2.	Indoor Environmental Quality

-	Prereq 1 - Minimum IAQ Performance

-	Credit 3.1 - Construction IAQ Management Plan During Construction

-	Credit 3.2 - Construction IAQ Management Plan Before Occupancy

-	Credit 4.1 - Low-Emitting Materials: Adhesives & Sealants

-	Credit 4.2 - Low-Emitting Materials: Paints and Coating

-	Credit 4.4 - Low-Emitting Materials: Composite Wood and Agrifibre Products

-	Credit 5 - Indoor Chemical & Pollutant Source Control

3.	Regional Priority

-	Credit 1 – Durable Building

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	[LEED Submittal Forms	Section 01 32 16.]

.2	[LEED Requirements	Section 01 35 18.]

.3	[Environmental Procedures	Section 01 35 20.]

.4	[Waste Management and Disposal	Section 01 74 19.]

.5	Rough Carpentry	Section 06 10 00.

.6	Wood Trusses:	Section 06 17 53.

1.2	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 01 for requirements pertaining to product options and substitutions.

1.3	REFERENCE Documents

SPEC NOTE: Edit this article to include only standards referenced within the edited version of this Section, including LEED requirements and sustainable practices.

.1	American Society for Testing and Materials (ASTM):

| .1 | ASTM A653/A653M-09 | Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process |
| --- | --- | --- |

.2	Canada Green Building Council (CaGBC):

| .1 | LEED Canada 2009 Rating System | LEED Canada for New Construction and Major Renovations. LEED Canada for Core and Shell Development. Website: www.cagbc.org |
| --- | --- | --- |

.3	Canadian Standards Association (CSA):

| .1 | CSA B111-1974 (R2003) | Wire Nails, Spikes and Staples |
| --- | --- | --- |
| .2 | CSA O80 Series-08/O80 S2-05 | Wood Preservation |
| .3 | CSA O80.20-97 (R2002) | Fire-Retardant Treatment of Lumber by Pressure Processes |
| .4 | CAN/CSA O86-01 | Consolidation(R2006), Engineering Design in Wood |

.4	FSC Forest Stewardship Council:

| .1 | FSC-STD-01-001-2004 | FSC Principle and Criteria for Forest Stewardship |
| --- | --- | --- |
| .2 | FSC-STD-20-002-2004 | Structure and Content of Forest Stewardship Standards V2-1 |
| .3 | FSC Certified Bodies |  |

.5	Green Seal: Standards:

| .1 | GS-11 | Green Seal Environmental Criteria for Anti-Corrosive Paints, Second Edition, May, 1993 |
| --- | --- | --- |

.6	National Lumber Grading Authority (NLGA):

| .1 | NLGA-07 | Standard Grading Rules for Canadian Lumber |
| --- | --- | --- |

.7	SCAQMD South Coast Air Quality Management District, California State (SCAQMD:

| .1 | SCAQMD Rule 1113-04 | Architectural Coatings |
| --- | --- | --- |
| .2 | SCAQMD Rule 1168-05 | Adhesives and Sealants Applications |

1.4	SUBMITTALS

.1	Product Data:

.1	Submit manufacturer's printed product literature, specifications and data sheet in accordance with Section 01 33 00   Submittal Procedures.

.2	Submit [two] [        ] copies of WHMIS MSDS   Material Safety Data Sheets in accordance with Section 01 33 00  Submittal Procedures. Indicate VOC's for:

.1	Wood Preservative.

.2	Adhesives.

SPEC NOTE:  For LEED projects include LEED Submittals.

.2	Sustainable Design Submittals:

.1	LEED Submittals: Co-ordinate submittals requirements in accordance with Section 01 35 18 - LEED Requirements.

2	Submit MSDS sheets or official manufacturer literature stating adhesives contain no urea-formaldehyde.

SPEC NOTE: Include below sentence for LEED projects seeking credit MRc7.

.3	Submit certificates by Forestry Stewardship Council Chain of Custody for wood materials in compliance with LEED Credit MR 7.

1.5	QUALITY ASSURANCE

.1	Regulatory Agency Approvals:

.1	Lumber identification: by grade stamp of an agency certified by Canadian Lumber Standards Accreditation Board.

1.6	DELIVERY, storage, AND handling

.1	Delivery and Acceptance Requirements:

.1	Protect materials from weather upon delivery to job site.

.2	Storage and Handling Requirements:

.1	Store materials on raised supports.  Cover materials with waterproof covering.  Provide adequate air circulation and ventilation.

.3	Do not store seasoned materials in wet or damp areas.

.4	Waste Management and Disposal:

.1	Separate waste materials for [reuse] [and] [recycling] in accordance with Section 01 74 19 - Management and Disposal.

2.	Products

2.1	Description

SPEC NOTE:  Consider including a list of manufacturers that are within the required distances of the project site and obtain materials and products which are extracted, harvested, recovered and processed within 800 km or 2400 km of final manufacturing site, depending on the method of transportation.  Refer to Materials and Resources Credit 5 Regional Materials.

.1	Sustainability Characteristics:

.1	Provide materials that have been extracted, harvested, recovered and processed within minimum distances required to the final point of manufacture.  Provide materials from a manufacturing facility within minimum distance required from Project site and delivered to Project site by acceptable transportation method.

.2	Refer to Section 01 35 18 LEED Requirements, Materials and Resources Credits:

.1	Credit 5 - Regional Materials

2.2	MATERIALS

SPEC NOTE:  Douglas Fir is typically from B.C..  Spruce and lodgepole pine are from Alberta , typically.

.1	Lumber:  Seasoned, [select] [and] [commercial] grade [Douglas Fir,] [Pacific Coast Hemlock,] [Spruce] [or] [Western Red Cedar].  Kiln dry to 15 percent maximum moisture content for 38 mm deck to 19 percent maximum content for 64 mm and 89 mm deck.  “Veed” one side.  Pre-drill at 750 mm on centre for lateral spiking.

SPEC NOTE:  Consider also recycled plastic as an alternative to wood decking material.  Consider also blue beetle stained lodgepole pine.

SPEC NOTE:  For LEED projects seeking MR credit 7 use wood materials that are certified by the Forestry Stewardship Council (FSC).

.1	Material and Resources Credit MR - 7 Certified Wood.

.2	Co-ordinate with Section 01 35 18 - LEED Requirements.

.3	Forest Stewardship Council (FSC) certified.

.2	Deck Sizes:  To NLGA:

.1	[38 mm Deck] - [38 mm x 137-181 mm] – Single tongue and groove.

.2	[64 mm Deck] - [64 mm x 141 mm] – Double tongue and groove.

.3	[89 mm Deck] - [89 mm x 141 mm] – Double tongue and groove.

.3	Piece Lengths:  10% of quantity supplied shall be 1.8 m to 3 m in length.  45% of quantity supplied shall be 5 m and longer.

2.3	Accessories

.1	Nails: To CSA B111:

.1	Finish: [galvanized] [hot dipped galvanized] [electro-galvanized] [stainless steel] finish.

.2	Sizes:  as recommended in [CAN/CSA O86] [ASTM 653/653M].

.3	Supply 200 mm spiral spikes for lateral nailing.

.2	Splines: galvanized metal, as recommended by decking manufacturer.

2.4	wood treatment

SPEC NOTE:  Use the paragraph below for LEED projects. Preservatives used in interior spaces of the building must have a VOC limit in compliance with the State of California South Coast Air Management Rule #1113, when applied on site.  Check SCAQMD rules at time of building permit as they become more stringent over time.

.1	Pressure Preservative Treated Wood:  in accordance with CSA O80 Series. [and as follows:]

.2	CSA O80.15 using ACA or CCA water borne preservative treatment for [         ].

SPEC NOTE:  Specify appropriate standard where CAN/CSA 080.15, Preservative Treatment for Building Foundation Systems, Basements and Crawl Spaces by Pressure Processes, is not appropriate.

.1	SCAQMD Rule #1113 - Architectural Coatings.

.2	Maximum allowable VOC limit [350] [___] g/L.

.2	CSA O80[     ] using [     ] [water borne] [oil borne] preservative treatment for [     ].

.1	SCAQMD Rule #1113 - Architectural Coatings.

.2	Maximum allowable VOC limit [350] [___] g/L.

.3	Water-borne preservative treated wood shall have maximum moisture content of 19% after treatment.

.1	SCAQMD Rule #1113 - Architectural Coatings.

.2	Maximum allowable VOC limit [350] [___] g/L.

.4	Fire-Retardant: to [CSA O80.20] [CSA O80.27], to provide:

.1	Flame Spread Classification: FSC [___].

.2	Smoke developed of not more than: [___].

.5	Provide coatings that do not contain chemical listed in GS-II.

3.	Execution

3.1	GRADE

.1	Install select grade where decking is exposed in finished structure and where specifically indicated.  Install commercial grade elsewhere.

3.2	PATTERN

.1	Multiple Span:  Install decking in accordance with CAN3-O86, [controlled random] [continuous over two spans] pattern.

.2	Single and double spans:  End joints shall be over support.

.3	Provide minimum of one bearing support for each plank [except for cantilevers which shall extend over two supports].  Install sloping deck with tongues up.  Join butt ends with splines to ensure a tight square fit,

.4	Touch up end cuts with preservative.

3.3	PRE-DRILLED HOLES

.1	For 64 mm and 89 mm deck drill 6 mm diameter holes horizontally through centre of section at 750 mm on centre unless otherwise indicated drawings.

3.4	NAILING

.1	Nail each piece at each support with one toe nail and one face nail.

.2	Nails shall penetrate 38 mm into supporting members.

.3	Side nail 64 mm and 89 mm Deck with 200 mm spiral spikes to adjoining piece through pre-drilled horizontal holes.

3.5	treatment application

.1	Application Preservative:

SPEC NOTE:  Schedule each wood product, type of preservative, and method of treatment, from CSA O80 Series, Commodity Standards retention.  Standards are minimum and may be increased where warranted by severe conditions, extended service life, or other factors.

.1	Treat [indicate material] [         ] to CSA O80 Series [indicate commodity standard number] [        ]using [         ] preservative to obtain minimum net retention of [         ] kg/m3of wood.

SPEC NOTE:  Use the following paragraph for treatment with water-borne preservatives.

.2	Following water-borne preservative treatment, dry material to maximum moisture content of [        ]%.

.2	Application – Fire Retardant

SPEC NOTE:  Use CSA O80.20 for lumber; CSA O80.27 for plywood.

.1	Treat [indicate material] [         ] by pressure impregnation with fire-retardant chemicals in accordance with [CSA O80.20] [CSA O80.27].

.2	Following treatment, kiln-dry material to maximum moisture content of [         ]%.

SPEC NOTE:  For field treatment of end cuts.

.3	Application – Field Treatment

SPEC NOTE:  Supplement requirements of AWPA M4 as required.

.1	Comply with AWPA M4 and revisions specified in CSA O80 Series, Supplementary Requirements to AWPA M2.

.2	Remove chemical deposits on treated wood to receive applied finish.  Refer to Section 09 91 05 – Painting and Finishing General Requirements.

.3	Site applied tough-ups to meet requirements of SCAQMD Rule #1113 - Architectural Coatings at time of building permit for [fire retardant coating]  [wood preservative].

.4	Maximum allowable VOC limit  g/L.

.1	[650] g/L if clear fire retardant.

.2	[350] if [fire retardant is pigmented] or if [wood preservative].

.5	Provide coatings that do not have chemicals listed in GS-II.

3.6	Cleaning

.1	Remove tool marks, bruises and scratches after completing erection.  Replace damaged decking if repairs are not approved by the consultant.

3.7	Protection

.1	Provide temporary waterproof covering to protect exposed decking before applying roofing.

END OF SECTION