Section Cover Page

Section 08 14 23 2014-11-01 Plastic Laminate Faced Wood Doors

Refer to “LEED Notes and Credits” page for additional guidance for LEED projects. Delete LEED items if project: .1 is excluded by the Department’s policy on LEED, or .2 the Department has determined that the work of this Contract is not to attain a LEED rating.

This Master Specification Section contains:

.1	This Cover Sheet

.2	LEED Notes and Credits

.3	Specification Section Text:

1.	General

1.1	Related Sections.

1.2	Reference Documents

1.3	Product Options and Substitutions.

1.4	Submittals

1.5	Delivery, Storage and Handling

2.	Products

2.1	Regulatory Requirements

2.2	Materials.

2.3	Mineral Core Doors

2.4	Solid Core Doors

2.5	Accessories

2.6	Fabrication.

3.	Execution

3.1	Installation.

LEED Notes:

Refer to Section 01 35 18 – LEED Requirements for:

- Requirements necessary to obtain points for certification.

- Confirmation of LEED perquisites and credits affecting this Section.  Not all are mandatory for certification.

Maintain built-in sustainability regardless of LEED requirements for:

- Recycling, reuse of materials, components and assemblies.

- Diversion of construction waste from landfills.

- Use of recycled materials, local materials, rapidly renewable and durable materials.

- Maintain healthy indoor environment during constructing.

- Provide for thermal comfort, access to views and daylight for indoor spaces.

- Foster innovation into facility design and planning.

LEED Credits:

1.	Materials & Resources

-	Prereq 1 - Storage & Collection of Recyclables

-	Credit 2 - Construction Waste Management

-	Credit 4 - Recycled Content

-	Credit 5 - Regional Materials

-	Credit 6 - Rapidly Renewable Materials

-	Credit 7 - Certified Wood

2.	Indoor Environmental Quality

-	Prereq 1 - Minimum IAQ Performance

-	Credit 4.1 - Low-Emitting Materials: Adhesives & Sealants

-	Credit 4.2 - Low-Emitting Materials: Paints and Coating

-	Credit 4.4 - Low-Emitting Materials: Composite Wood and Agrifibre Products

3.	Regional Priority

-	Credit 1 – Durable Building

1.	General

1.1	RELATED SECTIONS

.1	Submittal Procedures	Section 01 33 00.

.2	[LEED Requirements	Section 01 35 18.]

.3	[Waste Management and Disposal	Section 01 74 19.]

.4	Operation and Maintenance Data and Manuals	Section 01 78 23.

.5	Wood door frames:	Section 06 20 00.

.6	Hollow metal frames:	Section 08 12 13.

.7	Door hardware & weatherstripping:	Section 08 70 00.

.8	Glass and glazing:	Section 08 81 00.

.9	Finishing edges of [glazing stops] [louvres]:	Section 09 91 05.

.10	Supply of louvres:	Section [           .]

1.2	REFERENCE DOCUMENTS

SPEC NOTE: Edit this article to include only standards referenced within the edited version of this Section, including LEED requirements and sustainable practices.

.1	Architectural Woodwork Manufacturers Association of Canada (AWMAC)
and Architectural Woodwork Institute (AWI):

| .1 | Architectural Woodwork Standards, 1st Edition, 2009 |
| --- | --- |

.2	American National Standards Institute (ANSI):

| .1 | ANSI/NPA A208.1-2009 | Particleboard |
| --- | --- | --- |
| .2 | ANSI A208.2-2009 | Medium Density Fiberboard (MDF) for Interior Applications |

.3	Canada Green Building Council (CaGBC):

| .1 | LEED Canada 2009 Rating System | LEED Canada for New Construction and Major Renovations. LEED Canada for Core and Shell Development. Website: www.cagbc.org |
| --- | --- | --- |

.4	Canadian Standards Association (CSA):

| .1 | CAN3-A172- M79 (R1996) | High Pressure Paper Base, Decorative Laminates |
| --- | --- | --- |
| .2 | CSA O112 Series-M1977 (R2006) | Wood Adhesives |
| .3 | CAN/CSA O132.2 Series 90(R1998) | Wood Flush Doors |

.5	FSC Forest Stewardship Council:

| .1 | FSC-STD-01-001-2004 | FSC Principle and Criteria for Forest Stewardship |
| --- | --- | --- |
| .2 | FSC-STD-20-002-2004 | Structure and Content of Forest Stewardship Standards V2-1 |
| .3 | FSC Certified Bodies |  |

.6	Green Seal: Standards:

| .1 | GS-11 | Green Seal Environmental Criteria for Paint, First Edition, May 1993 |
| --- | --- | --- |

.7	National Fire Protection Association (NFPA):

| .1 | NFPA 80-99 | Fire Doors and Windows |
| --- | --- | --- |
| .2 | NFPA 252-08 | Fire Tests of Door Assemblies |

.8	NLGA National Lumber Grading Authority:

| .1 | NLGA-07 | Standard Grading Rules for Canadian Lumber |
| --- | --- | --- |

.9	South Coast Air Quality Management District (SCAQMD), California State:

| .1 | SCAQMD Rule 1113 | January 2004, Architectural Coatings |
| --- | --- | --- |
| .2 | SCAQMD Rule 1168 | June 2006, Adhesives and Sealants Applications |

.10	Underwriters' Laboratories of Canada (ULC):

| .1 | CAN4 S104M-M83 | Fire Tests of Door Assemblies |
| --- | --- | --- |
| .2 | CAN4 S105M-M85 | Fire Door Frames |

1.3	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 01 for requirements pertaining to product options and substitutions.

1.4	SUBMITTALS

.1	Product Data:

.1	Submit manufacturer's printed product literature, specifications and data sheet in accordance with Section 01 33 00 - Submittal Procedures.

.2	Submit [two] [        ] copies of WHMIS MSDS   Material Safety Data Sheets in accordance with Section 01 33 00 - Submittal Procedures. Indicate VOC's for:

.1	Finishes

.2	Adhesives

.3	Sealants

.2	Shop Drawings:

.1	Submit shop drawings in accordance with Section 01 33 00.

.2	Clearly indicate door construction and cut-outs for lights and louvres.

.3	Clearly indicate reinforcement for door hardware in mineral core fire rated doors.

.4	Reference door types to Door Schedule; indicate door and frame numbers as applicable.

.3	Samples:

SPEC NOTE:  Include the following paragraph for projects specifying at least 20 doors.

.1	Provide one 300 mm x 300 mm sample [for each door type [and finish]].  Sample to represent the upper hinge side corner of the door, showing hardware reinforcement, if applicable.

SPEC NOTE: Include the following paragraphs for project specifying at least 100 doors.

.2	Deliver one additional interior door of most common size shown on Door Schedule.

.3	A door from this range will be taken at random and cut as required to check for compliance with specification.

SPEC NOTE:  Use the following paragraph for LEED projects when LEED Submittals are required.

.4	Sustainable Design Submittals:

.1	LEED Submittals: Co-ordinate submittals requirements in accordance with Section 01 35 18 - LEED Requirements.

SPEC NOTE: Delete LEED submittal item below if project is not to attain LEED certification or if Credit EQ 4.4 Low Emitting Materials: Comp Wood and Agrifibre Products is not being sought. If project is to follow sustainable building practices but not attaining LEED certification, delete references to LEED and retain requirement for no added urea-formaldehyde permitted.

.2	[LEED] Submittals: [submit LEED submittal forms for Credit EQ 4.4 in accordance with Section 01 32 16 LEED Submittal Forms and Section 01 35 18 LEED Requirements and the following][submit sustainable submittals as follows]:

.1	Composite Wood products including core materials, must contain no added urea-formaldehyde resins.

.2	Adhesives used to fabricate laminated assemblies must contain no urea-formaldehyde.

SPEC NOTE: Include below sentence for LEED projects seeking credit MRc7.

.3	Provide certificates by Forestry Stewardship Council Chain of Custody for wood materials in compliance with LEED Credit MR 7.

1.5	DELIVERY, Storage, and handling

.1	Delivery and Acceptance Requirements:

.1	Deliver doors and panels to minimize storage on site and when site conditions conform to requirements for storage.

.2	Storage and Handling Requirements:

.1	Store and handle doors and panels in accordance with AWMAC requirements, and as follows:

.1	Arrange delivery after work causing abnormal humidity has been completed.

.2	Protect doors from dampness.

.3	Store doors in well ventilated area, off floor.

.4	Protect doors from scratches, handling marks and other damage.

.3	Waste Management and Disposal:

.1	Separate waste materials for [reuse] [and] [recycling] in accordance with Section 01 74 19 - Management and Disposal.

2.	Products

2.1	REGULATORY REQUIREMENTS

SPEC NOTE:  Include this article only if project has labeled doors.

.1	Wood fire rated doors shall be labeled and listed by an organization accredited by Standards Council of Canada.

2.2	MATERIALS

.1	Door materials:  to CAN/CSA-O132.2 Series.

.2	Adhesive for Plastic Laminate:  in accordance with CSA O112 Series or as recommended by plastic laminate manufacturer, not containing urea formaldehyde.

.3	Glazing stops:  [hardwood] [solid plastic] [metal] with mitred corners.

SPEC NOTES:  Utilize the following paragraphs to comply with LEED credits required for this project.  Edit paragraphs s requires to suit project conditions.

.4	Co-ordinate with Section 01 35 18 - LEED Requirements.

SPEC NOTE:  Utilize below paragraph for LEED projects seeking MR credit 4.1 or 4.2, for materials with recycle content, post-consumer and post industrial.   Recycle content materials are as defined in accordance with  the Federal Trade Commission document, Guides for the Use of Environmental Marketing Claims 16 CFR.7(e).

.5	Recycle Content:

.1	Material and Resources Credit MR – 4 Recycle Content:

.1	[10] [20]% (Post-Consumer + ½ Pre Consumer)

Consider including a list of manufacturers that are within the required distances of the project site and obtain materials and products which are extracted, harvested, recovered and processed within 800 km or 2400 km of final manufacturing site, depending on the method of transportation.  Refer to Materials and Resources Credit 5 Regional Materials.

.6	Materials and Resources, Regional Materials Credit 5 – Regional Materials: [20% & 30%]  Extracted and Manufactured Regionally.

SPEC NOTE:  Use the paragraph below for LEED projects pursuing MR credit 7, only wood materials that are certified by the Forestry Stewardship Council (FSC) will be recognized in the calculations.

.7	Material and Resources Credit MR - 7 Certified Wood.  Co-ordinate with Section 01 35 18 - LEED Requirements.

.1	Forestry Stewardship Council (FSC) certified.

SPEC NOTE:  Use the paragraph below for LEED projects pursuing EQ credit 4.1, Low-Emitting Materials:  Adhesives and Sealants

.8	Environmental Quality Credit EQ - 4.1 Low - Emitting Materials: Adhesives and Sealants.

.1	SCAQMD Rule 1168, Adhesives and Sealants Applications.

.2	Maximum allowable VOC limit [250] [___] g/L.

SPEC NOTE:  Use the paragraph below for LEED projects pursuing EQ credit 4.2, Paints and Coatings

.9	Environmental Quality Credit EQ - 4.1 Low - Emitting Materials: Paints and Cotings

.1	SCAQMD Rule #1113 - Architectural Coatings.

.2	Maximum allowable VOC limit [250] [___] g/L.

SPEC NOTE:  Use the paragraph below for LEED projects pursuing EQ credit 4.4, engineered or composite wood materials for interior building spaces containing no urea-formaldehyde in resins.

.10	Environmental Quality Credit EQ – 4.4 Low – Emitting Materials: Composite Wood and Agrifibre Products.

.1	Composite wood and agrifibre products shall contain no added urea-formaldehyde resins.

.2	Laminating adhesives used to fabricate on-site and shop-applied composite wood and agrifibre products shall contain no added urea-formaldehyde resins.

2.3	mineral core doors

SPEC NOTE: Specify a mineral core for plastic faced wood doors that require a fire resistance rating greater than 20 minutes.

.1 	Fire rated doors: tested in accordance with CAN4 S104 or NFPA 252 to achieve rating specified.

.1	Construction: mineral core with 3-ply 3 mm thick cross laminated plywood face in accordance with CAN/CSA-O132.2 Series-90 and 12 mm hardwood strips on vertical edges. Fir plywood is not acceptable under plastic laminate.

.2 	Plastic laminate:  1.6 mm laminate to CAN3-A172, Type HD, [solid] [pattern] colours, [texture] [furniture] finish, [to match non-rated doors].

.3	Edges: solid hardwood, finger jointing is not acceptable.

.4	Reinforcement: SLM, as required for hardware installation, [option no. 5 for doors requiring exit devices] [and] [option no. 6 for doors requiring passage or lock sets] as indicated in AWMAC Quality Standards for Architectural Woodwork.

.5	Overall Door Thickness: 45 mm.

.6	Fire Rating: [¾ hr,] [1 hr,] and [1½ hr] [as indicated [on drawings][in Door Schedule]].

.7	Metal Rating Label: identifying the fire resistance rating of door, secured to hinge edge.

.8	Paired doors shall have matching pattern for uniform appearance.

2.4	solid core doors

.1	Flush doors: solid core to CAN/CSA-O132.2.1.

.1 	Construction:

SPEC NOTE: Do not specify particleboard core doors in areas subject to free moisture or high humidity, e.g. steam rooms, sauna bath.

SPEC NOTE: Describe special wood blocking requirements.  Normally specify 7 ply construction. Specify 5 ply construction only when high profile architectural edges are required, since cost of these doors is considerably higher than 7 ply doors.

.1 	Solid Particleboard Core: with minimum 57 mm stile and rail frame bonded to particleboard core and as follows:

.1	Reinforcement: [with wood lock blocks] [and special [describe] wood blocking].

.2	Construction: [5-ply] [7-ply]

.3	Use: [interior] [and] [exterior] use.

.2	Solid Wood Core: glued block core [with wood edge band] and as follows:

.1	Construction: [5-ply] [7-ply].

.2	Use: [interior] [and] [exterior].

.3	Solid, Wood Block, Lined Core, With Two Core Liners: Glued block [with wood edge band] and as follows:

.1	Construction: [5-ply] [7-ply].

.2	Use: [interior] [and] [exterior].

.4	Door Thickness: 45 mm.

.2 	Plastic laminate:  1.6 mm laminate to CAN3-A172, Type HD, [solid] [pattern] colours, [texture] [furniture] finish.

.1	Paired doors shall have matching face pattern for uniform appearance.

.3 	Adhesive: Type I (water proof).

.4	Fire Rating:  20 minute fire rating [as indicated on drawings] [as scheduled]. 	Metal

rating label, identifying the fire resistance rating, secured to hinge edge of door.

2.5	Accessories

.1	Transom and Side Panels:  to match materials and construction of adjacent doors and as follows:

.1	Meeting edges of doors and transom panels to be [square] [rabbeted].

.2	Veneer of doors and transom panels to be [end] [and] [colour] matched.

.2	Wood louvers: [Flat-edge slat] [Round-edge slat] [Inverted-vee slat (sight proof)] type. Refer to [drawings for sizes] [mechanical drawings and free air required schedules].

2.6	FABRICATION

.1	Coordinate door fabrication with door frames and door hardware.

.2	Fabricate doors in accordance with CAN/CSA-O132.2, and as follows:

.1	Apply plastic laminate to both faces of door cores in accordance with adhesive and plastic laminate manufacturer's instructions.

.2	Finish plastic laminate smooth and flush with stile edges of doors and bevel 20 degrees.

.3	Fabricate fire rated doors to provide clearances that do not exceed the following maximum NFPA 80 clearances between:

.1	Door and Jamb or Head:  	3.2 mm.

.2	Meeting Edges of Paired Doors:  	3.2 mm.

.3	Door and Noncombustible Finished Floor:  	19.05 mm.

.4	Door and Floor Coverings:  	12.7 mm.

.5	Door and Raised Noncombustible Sill or Threshold:  	9.5 mm.

SPEC NOTE:  Specify AWMAC Edge Detail No.D, with 5 ply doors, Detail No.E in all other cases.

.4	Door Edges:  provide 13 mm thick vertical hardwood, [[name of] species,] edge strips, to AWMAC Edge Detail No.[D] [E], and edge profiles at strike side as follows:

.1	Single Acting Swing Doors:  bevel 3 mm in 50 mm.

.2	Double Acting Swing Doors:  radius of 55 mm.

.5	Factory seal top and bottom of doors and edges of glazed [and louvre] openings.

.6	Prepare doors for louvres and glazing. Provide [hardwood, [name of] species] [   ] to match face veneer,] glazing stops with mitered cornres.  [No cut-outs permitted within 125 mm of sides and top of door or 200 mm from bottom of door.

.7	Install wood louvres.

.8	Ensure door bottom  rail of exterior doors will accept weatherstripping.

.9	[Provide astragals for pairs of doors.]

SPEC NOTE:  Ensure door reinforcement and edge profiles  are coordinated with hardware.

.10	Prepare doors to receive hardware using templates provided by hardware supplier.

3.	Execution

3.1	INSTALLATION

.1	Install doors and hardware in accordance with manufacturer's instructions [and CAN/CSA-O132.2 Series, Appendix A].

.2	Install labeled fire rated doors to NFPA 80.

.3	Adjust hardware for correct function.

.4	Install glazing, louvres and stops.

.5	Seal top and bottom edges of doors after fitting. Seal edges of glass and louvre openings prior to installing stops.

.6	Maximum Permissible Warp Measured Diagonally Across Door: 6 mm.

END OF SECTION