Section Cover Page

Section 09 30 13 2014-11-01 Ceramic Tile

Refer to “LEED Notes and Credits” page for additional guidance for LEED projects. Delete LEED items if project: .1 is excluded by the Department’s policy on LEED, or .2 the Department has determined that the work of this Contract is not to attain a LEED rating.

This Master Specification Section contains:

.1	This Cover Sheet

.2	LEED Notes and Credits

.3	Specification Section Text:

1.	General

1.1	Related Work Specified in Other Sections

1.2	Reference Documents

1.3	Product Options and Substitutions

1.4	Submittals

1.5	Quality Assurance

1.6	Delivery, Storage, and Handling

1.7	Site Conditions

2.	Products

2.1	Materials

3.	Execution

3.1	Workmanship

3.2	Installation - Flooring

3.3	Installation - Walls

LEED Notes:

If the project is not a designated LEED project, but is following sustainable building practices, specify that adhesives meet SCAQMD Rule #1168 and architectural coating products meet SCAQMD Rule #1113.

LEED Credits:

Contribution towards LEED credits in this section may apply as follows:

1.	LEED Credit EQ 4.1 Low-Emitting Materials: Sealants and Adhesives.

In order to obtain EQ 4.1, VOC content in sealants and adhesives used on the inside of the building must be less than the VOC content limits of the State of California’s South Coast Air Quality Management District (SCAQMD) Rule #1168, June 2006.  Product data and/or LEED letters from manufacturers are required for verification.

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	[LEED Submittal Forms	Section 01 32 16]

.2	[LEED Requirements	Section 01 35 18]

.3	[Environmental Procedures	Section 01 35 20]

.4	Waste Management and Disposal	Section 01 74 19.

.5	Finishing of concrete floor:	Section 03 35 10.

.6	Plywood sub-floor:	Section 06 10 00.

.7	Caulking and sealing:	Section 07 92 00.

.8	Plaster scratch and brown coats:	Section 09 23 00.

.9	Gypsum wallboard:	Section 09 29 00.

.11	Quarry tile flooring:	Section 09 30 16.

.12	Resilient flooring:	Section 09 65 00.

.13	Non-ceramic washroom accessories:	Section 10 28 13.

1.2	refernce documents

SPEC NOTE: Edit this article to include only standards referenced within the edited version of this Section, including LEED documentation and sustainable practices.

.1	American National Standards Institute (ANSI/CTI):

| .1 | ANSI/CTI (Ceramic) A108/A118/A136.1-2005 | Specification for the Installation of Ceramic Tile - A Collection of 20 ANSI/CTI A108 Series Standards on Ceramic Tile Installation: A108.1A-C, 108.4 -.13, A118.1-.10, ANSI A136.1 |
| --- | --- | --- |

.2	American Society for Testing and Materials (ASTM):

| .1 | ASTM C207 06 | Standard Specification for Hydrated Lime for Masonry Purposes |
| --- | --- | --- |
| .2 | ASTM C847-06 | Standard Specification for Metal Lath |

.2	Canada Green Building Council (CaGBC):

| .1 | LEED Canada 2009 Rating System | LEED Canada for New Construction and Major Renovations. LEED Canada for Core and Shell Development. Website: www.cagbc.org |
| --- | --- | --- |

.4	Canadian General Standards Board (CGSB):

| .1 | CAN/CGSB-51.33-M89 | Vapour Barrier Sheet, Excluding Polyethylene, for Use in Building Construction |
| --- | --- | --- |
| .2 | CGSB 71 GP 22M | Adhesive, Organic, for Installation of Ceramic Wall Tile |
| .3 | CAN/CGSB-75.1-M88 | Tile, Ceramic |

.5	Canadian Standards Association (CSA):

| .1 | CAN/CSA-A8/A5/A362-93 | Portland Cement / Masonry Cement / Blended Hydraulic Cement |
| --- | --- | --- |
| .2 | CSA A82.5-M1978 (R1998) | Structural Clay Non-Load-Bearing Tile |
| .3 | CSA A123.3-05 | Asphalt Saturated Organic Roofing Felt |

.6	South Coast Air Quality Management District (SCAQMD), California State:

| .1 | SCAQMD Rule 1168, June 2006, Adhesives and Sealants Applications |
| --- | --- |

.7	Terrazzo, Tile & Marble Association of Canada (TTMAC):

| .1 | TTMAC, Specification Guide 09 30 00, Tile Installation Manual 2009-2010 |
| --- | --- |

1.3	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 01 for requirements pertaining to product options and substitutions.

1.4	Submittals

.1	Product Data:

.1	Submit manufacturer’s printed product literature, specifications and data sheets in accordance with Section 01 33 00 Submittal Procedures.

.2	Submit [two] [        ] copies of Workplace Hazardous Materials Information System (WHMIS) Material Safety Data Sheets (MSDS) in accordance with Section [01 33 00 - Submittal Procedures] [         ]. Indicate VOCs.

.2	Shop Drawings:

.1	Submit shop drawings of ceramic tile work in accordance with Division 01.

.2	Clearly show layout, [pattern] and relationship of tile joints to washroom and other fixed accessories and project-formed details.

SPEC NOTE:  Normally this clause above is only required for projects involving pools or special features.

.3	Samples:

.1	Submit duplicate 300 x 300 mm sample panels of each colour, texture, size and pattern of tile required for this project.

.2	Adhere tile samples to 12 mm thick plywood and grout joints to represent project installation.

.3	Obtain approval of each tile and grout sample prior to supplying material to project.

.4	Sustainable Design Submittals:

SPEC NOTE: Use the following paragraph when LEED Submittals are required.

.1	LEED Submittals: Submit documentation in accordance with Section 01 35 18 – LEED Requirements.  Submit documentation for the following:

.1	Indoor Environmental Quality:

SPEC NOTE: Delete LEED submittal item below if project is not to attain LEED certification or if Credit EQ 4.1 Low Emitting Materials: Adhesives and Sealants is not being sought. If project is to follow sustainable building practices but not attaining LEED certification, delete references to LEED and retain SCAQMD Rule #1168 as a sustainable submittal.

.1	EQ Credit 4.1 - Low-Emitting Materials: Adhesives & Sealants

1.5	QUALITY assurance

.1	Installation:

.1	Tile work in accordance with 2009-2010 Specification Guide 09 30 00 Tile Installation Manual, produced by Terrazzo Tile and Marble Association of Canada [TTMAC], except where specified otherwise.

1.6	delivery, storage, and handling

.1	Delivery and Acceptance Requirements:

.1	Deliver packaged materials in original unopened containers.

.2	Storage and Handling Requirements:

.1	Keep delivered material dry and free from stains.  Store cementitious material off damp surfaces.

.3	Waste Management and Disposal:

.1	Separate waste materials for [reuse] [and] [recycling] in accordance with Section 01 74 19 – Management and Disposal.

1.7	site conditions

.1	Ambient Conditions:

.1	Maintain minimum 13°C air temperature at tile installation area for 24 hours prior to, during and after installation.

2.	Products

2.1	MATERIALS

.1	Ceramic Mosaic Tile:  to CAN/CGSB-75.1, Type [1] [2], Class [     ], faces [     ], edges [     ], size [     ], colour will be selected by Province.

.2	Glazed Ceramic Mosaic Floor Tile:  to CAN/CGSB-75.1, Type 1, Class [     ], faces glazed incorporating non-slip silica granules within the glaze, cushioned edges on all 4 sides, size [       ], colour will be selected by Province.

.3	Ceramic Facing Veneer:  to CAN/CGSB-75.1, Type 3, Class [     ], faces glazed,  edges [     ], size [     ], colour will be selected by Province.

.4	Ceramic Wall Tile:  to CAN/CGSB-75.1, Type 5, Class MR4, faces glazed, cushioned edges on all 4 sides, size [     ], colour will be selected by Province.

.5	Cement:  [grey] [white] to CAN/CSA-A5.

.6	Sand:  to CSA A82.5.

.7	Water:  potable.

.8	Dry-Set Mortar:  to ANSI A118.1.

SPEC NOTE: Delete the following VOC content limit restriction if project is not to attain LEED certification or if Credit EQ 4.1 is not being sought, or if sustainable building practices are not being followed.

.9	Organic Adhesive:  to CGSB 71-GP-22M Type [1] [2],[having VOC content less than the VOC limits of State of California’s South Coast Air Quality Management District Rule #1168, June 2006.]

.10	Hydrated Lime:  to ASTM C207 Type S.

.11	Cleavage Plane:  [polyethylene film to CAN/CGSB-51.33-M89, Type 2] [No. 15 asphalt saturated felt to CSA A123.3]

.12	Metal Lath:  to ASTM C847, galvanized finish.

.13	Ceramic Washroom Accessories:  [         ].

3.	Execution

3.1	WORKMANSHIP

.1	Apply tile or backing coats to non-frozen frost free surfaces.

.2	Fit tile units around corners, fitments, fixtures, drains and other built-in objects to maintain uniform joint appearance.  Make cut edges smooth, even and free from chipping.  Edges resulting from splitting not acceptable.

.3	Make joints between tiles uniform and approximately 1.5 mm, plumb, straight, true, even and with adjacent tile flush.  Ensure sheet layout not visible after installation.

.4	Align patterns.

.5	Lay out tiles so that perimeter tiles are minimum 1/2 size.

.6	Sound tiles after setting and replace hollow sounding units to obtain full bond.

.7	Clean installed tile surfaces after installation cured.

.8	Maintain building expansion joints.  Keep free of mortar or grout.

.9	Locate ceramic accessories evenly spaced and centered on joint layout.  Rigidly install accessories.

.10	Make internal angles square, external angles [bullnosed] [square].  Use bullnose edged tiles to achieve bullnose effect.  [Use finished edge tiles for square external angles.]

.11	Use bullnose edged or trim tiles at termination of tile panels except where panel butts a projecting surface or differing plane.

3.2	INSTALLATION - FLOORING

.1	Install tile on floor substrates to TTMAC details No.  [200-13] [or 200-13A] [or 200-14] [or 200-14A] [or 200-15].

SPEC NOTE:  Only include the following when using conductive tile.

.2	Install electrically conductive tile in conductive portland cement mortar to TTMAC detail No. 200-20.  Set mesh reinforcing at midpoint of underbed.  Lap joints 150 mm.  Terminate reinforcing at expansion joints.

3.3	INSTALLATION - WALLS

.1	Apply scratch coat and mortar coat.  [Install cleavage plane and metal lath under all scratch and mortar coats].

SPEC NOTE:  Scratch and mortar coats are normally part of the plastering work and specified in the Plastering Section.  However, when there is no other plastering work on project, scratch and mortar coats can be specified in this Section as above.

.2	Install tile on [concrete] [concrete and masonry] walls to TTMAC details No. [200-1] [or 200-1A] [or 200-1B] [or 200-2] [or 200-2A] [or 200-2B] [or 200-3] [or 200-3A] [or 200-4] [or 200-4A] [or       ].

.3	Install tile on drywall to TTMAC details No. [200-5] [or 200-5a] [or 200-6] [or 200-6A] [or 200-7] [or 200-7A] [200-7B] [or 200-8] [or 200-8A] [or 200-9] [or 200-9A] [or 200-9B] [or     ].

.4	Install tile on plastered wall or ceiling substrates to TTMAC details No. [200-21].

END OF SECTION