Section Cover Page

Section 09 30 16 2014-11-01 Quarry Tile Flooring

Refer to “LEED Notes and Credits” page for additional guidance for LEED projects. Delete LEED items if project: .1 is excluded by the Department’s policy on LEED, or .2 the Department has determined that the work of this Contract is not to attain a LEED rating.

This Master Specification Section contains:

.1	This Cover Sheet

.2	LEED Notes and Credits

.3	Specification Section Text:

1.	General

1.1	Related Work in Other sections

1.2	Reference Documents

1.3	Submittals

1.4	Quality Assurance

1.5	Delivery, Storage, and Handling

1.6	Site Conditions

2.	Products

2.1	Materials

2.2	Mortar Mixes

3.	Execution

3.1	Workmanship

3.2	Setting Systems

LEED Notes:

If the project is not a designated LEED project, but is following sustainable building practices, specify that adhesives meet SCAQMD Rule #1168 and architectural coating products meet SCAQMD Rule #1113.

LEED Credits:

Contribution towards LEED credits in this section may apply as follows:

1.	LEED Credit EQ 4.1 Low-Emitting Materials: Sealants and Adhesives.

In order to obtain EQ 4.1, VOC content in sealants and adhesives used on the inside of the building must be less than the VOC content limits of the State of California’s South Coast Air Quality Management District (SCAQMD) Rule #1168, June 2006.  Product data and/or LEED letters from manufacturers are required for verification.

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	[LEED Submittal Forms	Section 01 32 16]

.2	[LEED Requirements	Section 01 35 18]

.3	[Environmental Procedures	Section 01 35 20]

.4	Waste Management and Disposal	Section 01 74 19.

.5	Application of sealants:	Section 07 92 00.

.6	Ceramic Tile: 	Section 09 30 13.

1.2	refernce documents

SPEC NOTE: Edit this article to include only standards referenced within the edited version of this Section, including LEED documentation and sustainable practices.

.1	American National Standards Institute (ANSI/CTI):

| .1 | ANSI/CTI (Ceramic) A108/A118/A136.1-2005 | Specification for the Installation of Ceramic Tile - A Collection of 20 ANSI/CTI A108 Series Standards on Ceramic Tile Installation: A108.1A-C, 108.4 -.13, A118.1-.10, ANSI A136.1 |
| --- | --- | --- |

.2	American Society for Testing and Materials (ASTM):

| .1 | ASTM C207 06 | Standard Specification for Hydrated Lime for Masonry Purposes |
| --- | --- | --- |
| .2 | ASTM C847-06 | Standard Specification for Metal Lath |

.2	Canada Green Building Council (CaGBC):

| .1 | LEED Canada 2009 Rating System | LEED Canada for New Construction and Major Renovations. LEED Canada for Core and Shell Development. Website: www.cagbc.org |
| --- | --- | --- |

.4	Canadian General Standards Board (CGSB):

| .1 | CAN/CGSB-51.33-M89 | Vapour Barrier Sheet, Excluding Polyethylene, for Use in Building Construction |
| --- | --- | --- |
| .2 | CGSB 71 GP 22M | Adhesive, Organic, for Installation of Ceramic Wall Tile |
| .3 | CAN/CGSB-75.1-M88 | Tile, Ceramic |

.5	Canadian Standards Association (CSA):

| .1 | CAN/CSA-A8/A5/A362-93 | Portland Cement / Masonry Cement / Blended Hydraulic Cement |
| --- | --- | --- |
| .2 | CSA A82.5-M1978 (R1998) | Structural Clay Non-Load-Bearing Tile |
| .3 | CSA A123.3-05 | Asphalt Saturated Organic Roofing Felt |

.6	South Coast Air Quality Management District (SCAQMD), California State:

| .1 | SCAQMD Rule 1168, June 2006, Adhesives and Sealants Applications |
| --- | --- |

.7	Terrazzo, Tile & Marble Association of Canada (TTMAC):

| .1 | TTMAC, Specification Guide 09 30 00, Tile Installation Manual 2009-2010 |
| --- | --- |

1.3	Submittals

.1	Product Data:

.1	Submit manufacturer’s printed product literature, specifications and data sheets in accordance with Section 01 33 00 - Submittal Procedures.

.2	Submit [two] [          ] copies of Workplace Hazardous Materials Information System (WHMIS) Material Safety Data Sheets (MSDS) in accordance with Section [01 33 00 - Submittal Procedures] [         ]. Indicate VOCs.

.2	Shop Drawings:

.1	Submit shop drawings of ceramic tile work in accordance with Division 01.

.2	Clearly show layout, [pattern] and relationship of tile joints to washroom and other fixed accessories and project-formed details.

SPEC NOTE:  Normally this clause is only required for projects involving pools or special features.

.3	Samples:

.1	Submit duplicate 600 x 600 mm sample panels of each colour, texture, size and pattern of tile required for this project.

.2	Adhere tile samples to 12 mm thick plywood and grout joints to represent project installation.

.3	Obtain approval of each tile sample prior to supplying material to project.

.4	Sustainable Design Submittals:

SPEC NOTE: Use the following paragraph when LEED Submittals are required.

.1	LEED Submittals: Submit documentation in accordance with Section 01 35 18 – LEED Requirements.  Submit documentation for the following:

.1	Indoor Environmental Quality:

SPEC NOTE: Delete LEED submittal item below if project is not to attain LEED certification or if Credit EQ 4.1 Low Emitting Materials: Adhesives and Sealants is not being sought. If project is to follow sustainable building practices but not attaining LEED certification, delete references to LEED and retain SCAQMD Rule #1168 as a sustainable submittal.

.1	EQ Credit 4.1 - Low-Emitting Materials: Adhesives & Sealants

1.4	QUALITY assurance

.1	Installation:

.1	Tile work in accordance with 2009-2010 Specification Guide 09 30 00 Tile Installation Manual, produced by Terrazzo Tile and Marble Association of Canada (TTMAC), except where specified otherwise

1.5	delivery, storage, and handling

.1	Delivery and Acceptance Requirements:

.1	Deliver packaged materials in original unopened containers.

.2	Storage and Handling Requirements:

.1	Keep delivered material dry and free from stains.  Store cementitious material off damp surfaces.

.3	Waste Management and Disposal:

.1	Separate waste materials for [reuse] [and] [recycling] in accordance with Section 01 74 19 – Management and Disposal.

1.6	site conditions

.1	Ambient Conditions:

.1	Maintain minimum 13°C air temperature at tile installation area for 24 hours prior to, during and after installation.

2.	Products

2.1	MATERIALS

.1	Quarry Tile:  to CAN/CGSB-75.1, Type 4, Class MR2, plain face, [square] [cushion] edges except where exposed where edges must be bullnosed, size, [        ], colour will be selected by Province.

.2	Glazed Quarry tile:  to CAN/CGSB-75.1, Type 4, Class MR2, face glazed incorporating non-slip silica granules within the glaze, cushioned edges on all 4 sides, size [      ], colour will be selected by Province.

.3	Quarry Tile Base:  to match tile specified above, [     ] high, [square] [coved] [bullnosed].

.4	Glazed Tile Base:  to match tile specified above, [     ] high with square top edge.

.5	Cement:  [grey] [white] to CAN/CSA-A5.

.6	Sand:  to CSA A23.1.

.7	Water:  potable.

.8	Dry-Set Mortar:  to ANSI A118.1.

SPEC NOTE: Delete the following VOC content limit restriction if project is not to attain LEED certification or if Credit EQ 4.1 is not being sought, or if sustainable building practices are not being followed.

.9	Elastomeric Adhesive:  to CGSB 71-GP-29M,[having VOC content less than the VOC limits of State of California’s South Coast Air Quality Management District Rule #1168, June 2006.]

.10	Portland Cement Grout:  mixture of Portland Cement and fine graded silica sand.

.11	Limited Acid Resistant Grout:  modified Portland Cement compound with additives for corrosion resistance to mild acid and alkali attack; non-rusting, non-dusting non-shrinking, nontoxic and odorless, no epoxy ingredient.  Colour will be selected by Province.

SPEC NOTE:  Specify limited acid resistant grout in places where mild acid and alkali corrosive conditions exist.

.12	Epoxy Grout and Mortar:  100% solids epoxy composed of 2 part thermosetting epoxy and graded silica sand, chemical resistant.  Colour will be selected by Province.

SPEC NOTE:  Specify epoxy grout only in places where extreme acid, chemical and similar corrosive conditions exist.  This material is highly toxic and its use requires special health safety precautions to be taken.  Refer to "Occupational Hygiene Recommended Guidelines for Use of Epoxy Resin Compounds in Tile Setting and Grouting" published by Occupational Health and Safety Division.

2.2	MORTAR MIXES

SPEC NOTE:  2.2.1 to 2.2.5 apply only to cement mortar setting.  Select the "coats" and "beds" to correspond with those used in the appropriate TTMAC details specified in 3.2

.1	Mortar bed:  1 part cement, 1/5 to 1/2 parts lime to suit job conditions, 4 parts sand, 1 part water.  Water volume may be adjusted depending on water content of sand.

.2	Slurry coat:  cement and water mixed to creamy paste.  Latex additive may be included.

.3	Levelling coat:  1 part cement, 4 parts sand, minimum 1/10 part latex additive, 1 part water, including latex additive.

.4	Bond or setting coat:  1 part cement, 1/3 parts lime, 1 part water.

.5	Measure mortar ingredients by volume.

.6	[[Dry set] [Elastomeric] adhesive], [Limited acid resistant grout] [Epoxy grout]:  mix to manufacturer's instructions.

SPEC NOTE:  Delete adhesives if not required by TTMAC details specified in paragraph 3.2.

3.	Execution

3.1	WORKMANSHIP

.1	Apply tile, mortar bed, or bond coat to non-frozen frost free surfaces.

.2	Fit tile units around corners, fitments, fixtures, drains and other built-in objects to maintain uniform joint appearance.  Make cut edges smooth, even and free from chipping.

.3	Make joints between tiles uniform and approximately 6 mm wide, plumb, straight, true, even and with adjacent tile flush.

.4	Align patterns.

.5	Lay out tiles so that perimeter tiles are minimum 1/2 size.

.6	Sound tiles after setting and replace hollow sounding units to obtain full bond.

.7	Make internal angles square, external angles bullnosed.

.8	Clean installed tile surfaces after installation cured.

.9	Maintain building expansion joints.  Keep free of mortar or grout.

3.2	SETTING SYSTEMS

.1	Install tile [and bases] on substrates to TTMAC details No. [200-16] [200-16A] [200-16B] [200-17] [200-17A] [200-18] [200-19] [200-19A] [200-19B] [200-19C].

.2	Install quarry tile treads to TTMAC details Nos. [200-26] [200-26A] [200-26B] [200-26C] [200-26D] [200-26E].

.3	Install quarry tile on mortar bed over insulation in refrigeration rooms to TTMAC details Nos. [200-28] [200-28A].

END OF SECTION