Section Cover Page

Section 09 64 23 2014-11-01 Wood Parquet Flooring

Refer to “LEED Notes and Credits” page for additional guidance for LEED projects. Delete LEED items if project: .1 is excluded by the Department’s policy on LEED, or .2 the Department has determined that the work of this Contract is not to attain a LEED rating.

Use this section to specify requirements for adhesive applied unfinished or prefinished wood parquet flooring including slat type parquet, unit wood blocks and plastic impregnated blocks.

This Master Specification Section contains:

.1	This Cover Sheet

.2	LEED Notes and Credits

.3	Data Sheet - General

.4	Specification Section Text:

1.	General

1.1	Related Sections

1.2	Reference Documents

1.3	Administrative Requirements

1.4	Submittals

1.5	Closeout Submittals

1.6	Maintenance Material Submittals

1.7	Delivery, Storage, and Handling

1.8	Site Conditions

2.	Products

2.1	Wood Subfloor Components

2.2	Wood Parquet

2.3	Accessories

2.4	Finishing Materials

2.5	Fabrication

3.	Execution

3.1	Preparation

3.2	Installation, Wood Subfloor with Sleepers

3.3	Installation, Plywood Subfloor without Sleepers

3.4	Adhesive Application

3.5	Wood Parquet Flooring

3.6	Thresholds

3.7	Sanding and Finishing

LEED Notes:

If the project is not a designated LEED project, but is following sustainable building practices, specify that adhesives meet SCAQMD Rule #1168 and architectural coating products meet SCAQMD Rule #1113.

Pressure treated wood: Copper Chromated Arsenate (CCA) is extremely toxic due to the arsenic which has a wide range of adverse health effects. Alternates to CCA are all around better for the environment and the humans that come in contact with it. There are two alternatives: Copper Azole(CA) and Alkaline Copper Quaternary(ACQ).  They are significantly less toxic than CCA and can be safely disposed of in landfills. This specification calls for CCA free pressure treatment of wood in the subfloor components.

LEED Credits:

Contribution towards LEED credits in this section may apply as follows:

1.	MR Credit 5 Regional Materials: Use building materials or products that have been extracted, harvested, recovered and processed within 800 km (2400 km is shipped by rail or water) of the final manufacturing site.  Demonstrate that the final manufacturing site is within 800 km (2400 km is shipped by rail or water) of the project site for these products. If fabricated regionally, flooring components will count in this credit. The contractor will be required to submit documentation consisting of cost, weight, transportation service and distances as evidence of compliance with credit requirements:

2.	LEED Credit MR 7 Certified Wood: flooring and sub-flooring may apply.

This credit requires a minimum of 50% of wood-based materials and products used on the project be certified in accordance with Forest Stewardship Council’s Principles and Criteria.

3.	LEED Credit EQ 4.1 Low-Emitting Materials: Sealants and Adhesives. Adhesives specified under this section apply.

In order to obtain EQ 4.1, VOC content in adhesives must be less than the VOC content limits of the State of California’s South Coast Air Quality Management District (SCAQMD) Rule #1168, June 2006.

4.	LEED Credit EQ 4.2 Low-Emitting Materials: Paint and Coatings. Finishes to flooring specified under this section apply.

Finishes applied to wood flooring have to comply with the maximum VOC content limits of the State of California’s South Coast Air Quality Management District (SCAQMD) Rule #1113, January 2004.

Parquet flooring may be applied over concrete with or without a wood subfloor.  Wood subfloors may be 19 mm plywood directly fastened to concrete, or plywood on wood sleepers.  Wood subfloors on sleepers provide greater cushioning and are recommended where comfort in use is a primary consideration.  Additional cushioning may also be provided by means of rubber pads applied to the underside of plywood subfloors or the underside of wood sleepers.

Consult with manufacturers prior to designing parquet that is to be applied directly to concrete below grade, or on grade located on hillsides.  Subject to manufacturers' approvals, specify liquid-applied waterproofing material compatible with permanently resilient parquet flooring adhesive recommended by flooring manufacturer.  Coordinate with Section 03 30 00 - Cast-in-Place Concrete.  This method may provide adequate protection against moisture and an integral bond with concrete substrate.

Parquet supplied with metal splines is said to impart a slight curvature to parquet and therefore requires thorough rolling after application to ensure maximum adhesive contact.

Plastic impregnated parquet flooring is recommended to greatly reduce wear in heavy traffic areas and for greater resistance to point loading, e.g. high-heel traffic.  While dimensionally more stable, it is not considered to be more moisture resistant than unimpregnated parquet.

1.	General

SPEC NOTE:  Specify wood base associated with parquet flooring in Finish Carpentry - Section 06 20 00 if standard manufactured item.  Specify wood base in Architectural Woodwork - Section 06 40 00 if custom millwork item.

1.1	RELATED SECTIONS

.1	[LEED Submittal Forms	Section 01 32 16]

.2	[LEED Requirements	Section 01 35 18]

.3	[Environmental Procedures	Section 01 35 20]

.4	Waste Management and Disposal	Section 01 74 19.

.5	Wood base:	Section [06 20 00] [06 40 00].

1.2	refernce documents

SPEC NOTE: Edit this article to include only standards referenced within the edited version of this Section, including LEED documentation and sustainable practices.

.1	Canada Green Building Council (CaGBC):

| .1 | LEED Canada 2009 Rating System | LEED Canada for New Construction and Major Renovations. LEED Canada for Core and Shell Development. Website: www.cagbc.org |
| --- | --- | --- |

.2	Canadian General Standards Board (CGSB):

| .1 | CAN/CGSB-1.36-97 | General Purpose Interior Varnish |
| --- | --- | --- |
| .2 | CAN/CGSB-1.175-97 | Polyurethane Interior Coating |
| .3 | CAN/CGSB-25.2-92 | Paste Floor Wax |
| .4 | CAN/CGSB 51.34 M86 AMEND | Vapour Barrier, Polyethylene Sheet for Use in Building Construction |
| .5 | CAN/CGSB 71.27 M88 | Adhesive for Bonding Parquet Flooring to Wood and Cured Concrete |

.3	Canadian Standards Association (CSA):

| .1 | CAN/CSA-O80, Series | Wood Preservation, Includes Update No. 1 (2008) |
| --- | --- | --- |
| .2 | CAN/CSA-Z808-96 | A Sustainable Forest Management System |
| .3 | CSA-O151-04 | Canadian Softwood Plywood |

.4	South Coast Air Quality Management District (SCAQMD), California State:

| .1 | SCAQMD Rule 1113, January, 2004 | Architectural Coatings |
| --- | --- | --- |
| .2 | SCAQMD Rule 1168, June 2006 | Adhesives and Sealants Applications |

1.3	Administrative Requirements

.1	Sequencing:

.1	Do not deliver material until "wet work" such as concrete and plastering have been completed and allowed to dry as required to provide acceptable substrate moisture content and room relative humidity range.

.2	Refer to 1.7 Delivery, Storage, and Handling and 1.8 Site conditions for requirements.

1.4	Submittals

.1	Product Data:

.1	Submit manufacturer’s printed product literature, specifications and data sheets in accordance with Section 01 33 00 - Submittal Procedures.

.2	Submit product data in duplicate for parquet, adhesives and finishes.

.3	Submit [two] [         ] copies of Workplace Hazardous Materials Information System (WHMIS) Material Safety Data Sheets (MSDS) in accordance with Section [01 33 00 - Submittal Procedures] [         ]. Indicate VOCs during application [and curing] [          ].

.2	Shop Drawings:

.1	Comply with requirements of Division 01.

SPEC NOTE:  Specify when pattern layout in various floor areas is not clearly indicated.  Greater control is achieved by clearly detailing requirements on tender documents.

.2	Clearly indicate area of work, placement and orientation of patterns, borders, cuts at edges, entrances, alcoves, change of levels, and other special conditions affecting layout.

.3	Samples:

.1	Comply with requirements of Division 01.

.2	Provide duplicate [     ] mm x [     ] mm samples of wood parquet, finished as specified.

SPEC NOTE:  Determine size of samples based on type and pattern of flooring.

.4	Sustainable Design Submittals:

SPEC NOTE: Use the following paragraph when LEED Submittals are required.

.1	LEED Submittals: Submit documentation in accordance with Section 01 35 18 – LEED Requirements.  Submit documentation for the following:

.1	Materials & Resources:

SPEC NOTE: Delete LEED submittal item if project is not to attain LEED certification or if Credit MR 5 is not being sought.

.1	MR Credit 5 - Regional Materials: [20%] [30%] Extracted and Manufactured Regionally

SPEC NOTE: Delete LEED submittal item if project is not to attain LEED certification or Credit MR 7 is not being sought.

.2	MR Credit 7 – Certified Wood: Minimum of 50% of wood-based materials and products used on the project be certified in accordance with Forest Stewardship Council’s Principles and Criteria

.2	Indoor Environmental Quality:

SPEC NOTE: Delete LEED submittal item below if project is not to attain LEED certification or if Credit EQ 4.1 Low Emitting Materials: Adhesives and Sealants is not being sought. If project is to follow sustainable building practices but not attaining LEED certification, delete references to LEED and retain SCAQMD Rule 1168 as a sustainable submittal.

.1	EQ Credit 4.1 - Low-Emitting Materials: Adhesives & Sealants

SPEC NOTE: Delete LEED submittal item below if project is not to attain LEED certification or if Credit EQ 4.2 Low Emitting Materials: Paint and Coatings is not being sought. If project is to follow sustainable building practices but not attaining LEED certification, delete references to LEED and retain SCAQMD Rule 1113 as a sustainable submittal.

.2	EQ Credit 4.2 - Low-Emitting Materials: Paint and Coatings

1.5	closeout submittals

.1	Operation and Maintenance Data:

.1	Comply with requirements of Division 01.

.2	Provide maintenance data for materials and floor finishes.

1.6	maintenance MATERIAL submittalS

.1	Extra Stock Materials:

.1	Provide [     ] m2 of each type and pattern used on this project.

SPEC NOTE:  On larger projects 1% of installed material area could be required for maintenance purposes.

.2	Include installation and application instructions.

.3	Store where directed.

.4	Clearly identify each box/carton.

1.7	Delivery, storage, and Handling

.1	Delivery and Acceptance Requirements:

.1	Do not deliver material until "wet work" such as concrete and plastering have been completed and allowed to dry as required to provide acceptable substrate moisture content and room relative humidity range.

.2	Storage and Handling Requirements:

.1	Store wood and parquet flooring, uncovered, in area of installation meeting environmental requirements, for minimum of 5 days prior to commencing work.

.3	Waste Management and Disposal:

.1	Separate waste materials for [reuse] [and] [recycling] in accordance with Section 01 74 19 – Management and Disposal.

1.8	site conditions

.1	Ambient Conditions:

.1	Maintain ambient temperature between 18°C and 21°C and design relative humidity for 72 hours before installation.

SPEC NOTE:  Include following clause for work in new facilities.  Delete if work to be renovation to an existing occupied facility.

.2	Do not proceed with installation until areas are enclosed, permanent mechanical systems are functioning satisfactorily, and interior relative humidity and temperature meet design requirements.

.3	Maintain environmental requirements after installation completed.

2.	Products

2.1	WOOD SUBFLOOR COMPONENTS

SPEC NOTE:  Delete this article when parquet flooring is to be adhered directly to prepared concrete floor.  Edit article to suit type of subfloor.

.1	Moisture Protection Membrane:  polyethylene film to CAN/CGSB-51.34, 150 micrometres thick.

SPEC NOTE: Delete the requirement for FSC product if the project is not to attaining LEED certification or the MR 7 Credit, or the project is not following sustainable building practices.

.2	Sleepers:  38 mm x 64 mm x 1200 mm long kiln dried [spruce] [pine] [fir] [hemlock], preservative pressure treated and CCA free to CAN/CSA-080 [Forest Stewardship Council(FSC) Certified].

.3	Cork Spacers:  as recommended by flooring manufacturer.

SPEC NOTE:  Specify cork spacers when subfloor sleepers are not fastened to structural floor.

.4	Fasteners:  hot-dip galvanized nails suitable for substrates.

SPEC NOTE: Delete the requirement for FSC product if the project is not to attaining LEED certification or the MR 7 Credit, or the project is not following sustainable building practices.

.5	Sheathing plywood:  to CSA O151, 19 mm thick, tongue and groove edges, sheathing grade [Forest Stewardship Council(FSC) Certified].

2.2	WOOD PARQUET

SPEC NOTE:  Ensure drawings indicate selected parquet patterns.

.1	Type:  [slat parquet] [solid unit blocks] [plastic impregnated blocks].

SPEC NOTE: Delete the requirement for FSC product if the project is not to attaining LEED certification or the MR 7 Credit, or the project is not following sustainable building practices.

.2	Species:  kiln dried [oak] [hard maple] [beech] [birch] [     ], [     ] grade to Canadian Lumbermens' Association (CLA) grading rules for Canadian Hardwood Flooring [Forest Stewardship Council(FSC) Certified].

.3	Pattern:  [herringbone] [basketweave] [diamond] [swirl] [finger mosaic] [     ].

.4	Sizes of units:  [     ] mm x [     ] mm x [     ] mm thick.

SPEC NOTE:  Standard size of parquet available in CLA grades is 121 x 121 x 8 mm thick.  Verify availability in CLA grades prior to specifying other sizes.

.5	Finish:  [unfinished] [exposed grain "distressed" finish] [prefinished, plastic-impregnated].

.6	Edges:  [tongue and groove] [square] [bevelled].

.7	Moisture Content:  6-9%.

2.3	ACCESSORIES

SPEC NOTE:  Delete VOC content requirement below if project is not attaining LEED certification or LEED Credit EQ 4.1 is not being sought, or sustainable building practices are not being followed.

.1	Adhesive:  to CAN/CGSB-71.27, resilient elastomeric, compatible with substrate and parquet flooring [VOC content compliant with SCAQMD Rule #1168, June 2006].

SPEC NOTE:  Edit remainder of article to suit project.

.2	Feature [or border] strips:  [     ] mm size, [     ] species.

.3	Threshold:  of same species and grade as wood flooring, [     ] mm wide x full width of opening.

2.4	FINISHING MATERIALS

SPEC NOTE:  Delete if prefinished or plastic impregnated parquet specified.

SPEC NOTE:  For the following item delete VOC content requirement below if project is not attaining LEED certification or LEED Credit EQ 4.2 is not being sought, or sustainable building practices are not being followed.

.1	Finish:  clear [urethane to CAN/CGSB-1.175] [varnish to CAN/CGSB-1.36],  [gloss] [satin] sheen[VOC content compliant with SCAQMD Rule #1113, January 2006].

.2	Wax:  paste wax to CAN/CGSB-25.2-92.

2.5	FABRICATION

.1	Assemble solid unit blocks of specified wood species and patterns.

.2	Secure individual pieces in blocks together in manner which permits ease of handling and secure installation.

.3	Plastic-impregnated Flooring:  impregnated throughout with methyl methacrylate plastic with colour dye to suit.

SPEC NOTE:  When specifying plastic impregnated wood parquet, delete stain and wax finish.

.4	Sand wearing surface of blocks and finish with [deep penetrating oil stain and] urethane finish.

3.	Execution

3.1	PREPARATION

.1	Examine substrate and verify readiness to receive work of this Section.

.2	Verify moisture content of concrete using the Phenolphthalein Test as recommended by National Oak Flooring Manufacturers Association.

3.2	INSTALLATION, WOOD SUBFLOOR WITH SLEEPERS

SPEC NOTE:  Delete this article when parquet is to be glued directly to concrete or structural wood subfloor.

.1	Apply moisture protection membrane over concrete.  Lap joints minimum 600 mm and seal with purpose-made sheathing tape.  Patch punctures and cuts.

.2	Place sleepers on membrane, parallel to short dimension of room and space at 400 mm nominally, to suit sheathing dimensions.  Stagger sleepers and lap ends 150 mm minimum.

.3	Shim sleepers as required to prevent rocking and to provide solid contact with structural substrate.

.4	Maintain minimum 20 mm expansion gap between sleepers and walls and other vertical surfaces.

.5	Glue and nail plywood sheathing with face grain at right angles to sleepers.

.6	Provide 15 mm expansion gap at plywood subfloor perimeter.

3.3	INSTALLATION, PLYWOOD SUBFLOOR WITHOUT SLEEPERS

SPEC NOTE:  Delete this article when parquet is to be glued directly to concrete or structural wood subfloor.

.1	Apply moisture protection membrane over concrete.  Lap joints minimum 300 mm and seal with mastic or sheathing tape.

.2	Lay plywood sheathing over membranes, stagger end joints 1200 mm.

.3	Leave 10 mm gap at vertical surfaces, except provide 3 mm gap at doors and other locations where wall base will not cover gap.  Provide 5 to 10 mm gap between plywood sheets.

.4	Mechanically fasten plywood to concrete, using minimum 9 fasteners per 1200 x 2400 sheet.

3.4	ADHESIVE APPLICATION

.1	Apply adhesive in accordance with manufacturer's instructions.

.2	Apply no more adhesive than can be covered with flooring before working time expires.

.3	Allow no streaks or lumps in adhesive during application.

.4	Remove adhesive that has set or that has formed surface film before flooring is embedded.  Apply fresh coat of adhesive.

3.5	WOOD PARQUET FLOORING

SPEC NOTE:  Use the first three clauses for rectangular floor areas, or modify as applicable.

.1	Locate first working line approximately parallel to wall exactly 4 or 5 parquet units from flooring edge at entry doorway.

.2	Locate perpendicular centre axis so no unit will be less than one-half size.

.3	Install flooring using pyramid or stair-step sequence starting from intersection of perpendicular axes.

.4	Install flooring units to provide parquet pattern indicated on drawings.  Install flooring units with aligned joints 0.4 mm wide between units.

SPEC NOTE:  Ensure drawings indicate pattern required.

.5	Allow 12 mm expansion space at walls or projections in floor area.

.6	Apply flooring units with uniform pressure.  Avoid working adhesive into joints.

.7	Thoroughly roll metal-splined units until adhesive sets, to ensure full bed adhesion.

.8	At start of installation, remove minimum [6] [  ] units before adhesive sets to inspect for complete coverage of adhesive and replace units immediately.  Adjust installation as required to achieve full bed adhesion.

.9	Remove adhesive visible after installation.

3.6	THRESHOLDS

.1	Install thresholds at openings and where indicated.

.2	Attach threshold to adjacent rigid floor surface.

.3	Threshold to act as ramp between floor surfaces over expansion space.

3.7	SANDING AND FINISHING

SPEC NOTE:  Delete this article when prefinished solid unit blocks are specified.

.1	Power sand floor surface smooth with starting with coarse, progressing to medium and finishing with fine grit.

.2	Vacuum clean.

.3	Apply [two] [three] coats of clear floor finish.

.4	Apply wax to manufacturer's recommendations.

END OF SECTION