Section Cover Page

Section 09 67 16 2014-11-01 Epoxy-Marble Chip Flooring

Refer to “LEED Notes and Credits” page for additional guidance for LEED projects. Delete LEED items if project: .1 is excluded by the Department’s policy on LEED, or .2 the Department has determined that the work of this Contract is not to attain a LEED rating.

This Master Specification Section contains:

.1	This Cover Sheet

.2	LEED Notes and Credits

.3	Specification Section Text:

1.	General

1.1	Related Work Specified in Other Sections

1.2	Reference Documents

1.3	Product Options and Substitutions

1.4	Qualifications

1.5	Submittals

1.6	Quality Assurance

1.7	Delivery, Storage, and Handling

1.8	Site Conditions

2.	Products

2.1	Materials

2.2	Colours

3.	Execution

3.1	Examination

3.2	Preparation

3.3	Erection / Installation / Application

3.4	Cleaning

3.5	Application Schedule

LEED Notes:

N/A

LEED Credits:

Contribution towards LEED credits in this section may apply as follows:

LEED Credit EQ 4.2 Low-Emitting Materials: Paint and Coatings.

In order to obtain EQ 4.2 sealers and protective coatings have to comply with the maximum VOC content limits of the State of California’s South Coast Air Quality Management District (SCAQMD) Rule #1113, Architectural Coatings, January 2004.

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	[LEED Submittal Forms	Section 01 32 16.]

.2	[LEED Requirements	Section 01 35 18.]

.3	[Environmental Procedures	Section 01 35 20.]

.4	Waste Management and Disposal		Section 01 74 19.

.5	[Substrate]:	Section [            ].

.6	Sealants:	Section 07 92 00.

.7	Painting:	Section 09 91 05.

.8	Vinyl-acrylic coating:	Section 09 96 53.

.9	Epoxy wall coatings:	Section 09 96 56.

1.2	REFERENCES Documents

SPEC NOTE: Edit this article to include only standards referenced within the edited version of this Section, including LEED documentation and sustainable practices.

.1	American Society for Testing and Materials (ASTM):

| .1 | ASTM C126-09 | Ceramic Glazed Structural Clay Facing Tile, Facing Brick, and Solid Masonry Units |
| --- | --- | --- |
| .2 | ASTM D570-98(2005) | Standard Test Method for Water Absorption of Plastics |
| .3 | ASTM D638-08 | Standard Test Method for Tensile Properties of Plastics |
| .4 | ASTM D696-08 | Standard Test Method for Coefficient of Linear Thermal Expansion of Plastics Between -30&#176C and 30&#176C With a Vitreous Silica Dilatometer |
| .5 | ASTM D905-08e1 | Standard Test Method for Strength Properties of Adhesive Bonds in Shear by Compression Loading |
| .6 | ASTM D1044-08 | Standard Test Method for Resistance of Transparent Plastics to Surface Abrasion |
| .7 | ASTM D1308-02(2007) | Standard Test Method for Effect of Household Chemicals on Clear and Pigmented Organic Finishes |
| .8 | ASTM D2337-01(2005) | Standard Test Method for Freeze-Thaw Stability of Multicolor Lacquers |
| .9 | ASTM E84-09c | Standard Test Method for Surface Burning Characteristics of Building Materials |

.2	Canada Green Building Council (CaGBC):

| .1 | LEED Canada 2009 Rating System | LEED Canada for New Construction and Major Renovations. LEED Canada for Core and Shell Development. Website: www.cagbc.org |
| --- | --- | --- |

.3	Canadian General Standards Board (CGSB):

| .1 | CGSB 1-GP-71 | Set of 3 Standards, January 2003 – Set includes 1-GP-71 No. 5-96, 1-GP-71 No. 38-96 and 1-GP-71 No. 73-96 |
| --- | --- | --- |

.4	South Coast Air Quality Management District (SCAQMD), California State (SCAQMD):

| .1 | SCAQMD Rule 1113, January, 2004 |
| --- | --- |

1.3	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 01 for requirements pertaining to product options and substitutions.

1.4	QUALIFICATIONS

.1	The work of this Section shall be applied only by experienced applicators of the specified products.

1.5	Submittals

.1	Product Data:

.1	Submit manufacturer’s printed product literature, specifications and data sheets in accordance with Section 01 33 00 - Submittal Procedures.

.2	Make available copies of the product data, clearly indicating conditions of acceptance for surfaces and methods of application on site before, and during, period of application of the work of this Section.

.2	Samples:

.1	Submit 300 mm x 300 mm representative sample of flooring in selected colour.  Identify sample by project name including material and colour identification.

.2	Site apply sample installation to minimum 2 m2 area, to surface as directed, for approval by the Province.  Retain approved sample until work is completed and accepted.

SPEC NOTE:  Use below paragraph when LEED submittals are required.

.3	Sustainable Design Submittals:

SPEC NOTE: Delete LEED submittal item below if project is not to attain LEED certification or if Credit IEQ 4.2 Low Emitting Materials: Paint and Coatings is not being sought. If project is to follow sustainable building practices but not attaining LEED certification, delete references to LEED and retain SCAQMD Rule #1113 as a sustainable submittal.

.1	LEED Submittals: Submit documentation in accordance with Section 01 35 18 – LEED Requirements.  Submit documentation for the following:

.1	Indoor Environmental Quality:

.1	IEQ Credit 4.2 - Low-Emitting Materials: Paint and Coatings

1.6	quality assurance:

.1	Qualifications:

.1	Installers / Applicators / Erectors:

.1	The work of this Section shall be applied only by experienced applicators of the specified products.

1.7	DELIVERY, storage, and handling

.1	Delivery and Acceptance Requirements:

.1	Deliver materials undamaged, in original containers, with manufacturer's labels and seals intact.

.2	Waste Management and Disposal:

.1	Separate waste materials for [reuse] [and] [recycling] in accordance with Section 01 74 19 – Management and Disposal.

1.8	site conditions

.1	Ambient Conditions:

.1	For exterior coatings:  Comply with coating manufacturer's recommendations.  Do not apply under adverse weather conditions which could affect coating performance.

.2	For interior coatings:  Ensure minimum surface temperature 10°C 24 hours before, during and 24 hours after application or until cured; adequate controlled ventilation; bright, uniform lighting; broom clean; reasonably dust free.

2.	Products

2.1	MATERIALS

.1	Thermo-setting 100% epoxy coating with matrix, coloured filler and top coat meeting the following requirements:

| Property | Test Method | Requirement |
| --- | --- | --- |
| Abrasion resistance | ASTM D1044 10,000 cycles using CS17 wheels with 1 kg load | 0.04 g loss max |
| Bond strength | After 7 days water immersion ACI Committee 403 Bulletin 5943 | 2275 kPa to concrete |
| Colour fastness | CGSB 1-GP-71, Method 120.1 Fade-ometer | 11.0 NBS units |
| Flammability | ASTM E84 1.3 mm max. Self extinguishing | Extent of burning |
| Impact resistance | CGSB 1-GP-71 Method 147.1 Gardner Impact Test 17 J | No cracking, chipping or delamination |
| Resistance to acid hydroxides, salts & cleaning agents | ASTM D1308 | Unaffected by common household cleaning agents, hydroxides and salts |
| Tensile strength | ASTM D638 | 7 MPa7 MPa |
| Toxicity | Can. Dept. of Agriculture | Approved non-toxic |
| Water absorption | ASTM D570 24 hour immersion | 0.45% max. |

SPEC NOTE:  The above material is for non-bearing industrial use.  The following materials meet the above requirements:  Duochem Epoxy Quartz, Duroquartz by Duron Col Ltd., Decor-Flor by Dex-O-Tex.

.2	Epoxy aggregate flooring, thermo-setting, 100% solids, and meeting following requirements:

| Property | Test Method | Requirement |
| --- | --- | --- |
| Abrasion resistance | ASTM D1044 CS 17 wheels with 2 kg load 5 000 cycles | 0.3 g |
| Coefficient of linear expansion | ASTM D696 | 165.6 x 107/°C |
| Flammability | ASTM E84 | Non-burning |
| Freeze-thaw resistance | ASTM D2337 | Unaffected |
| Hardness | Barcol | 55 |
| Impact resistance | Falling ball method, 50.8 mm in diameter weighing 535 g Gardner Impact Tester (Masonry Backing) | Energy required to cause failure: 12.9 J 9 J: no loss of adhesion |
| Resistance to burning cigarette |  | Very slight discoloration |
| Resistance to cleaning agents, hydroxides and salts | ASTM D1308 | Unaffected by common household cleaning agents, hydroxides and salts |
| Shear bond strength | ASTM D905 | 2 MPa to concrete |
| Surface stain | ASTM C126 | Unaffected |
| Tensile strength (binder only) | ASTM D638 | 23 MPa |
| Toxicity | Can. Dept. of Agriculture | Approved non-toxic |
| Washability | Gardner straight line method 5000 cycles | No visual effect |
| Water absorption | ASTM D570 | 0.2% by mass |

SPEC NOTE:  The above material is for heavy industrial use:  the following materials meet the above requirements:  Duochem 9400,  Morritex by Sika.

2.2	COLOURS

.1	[One] [Two] [          ] colour[s] will be selected by Province from manufacturer's standard range.

OR

.1	Refer to Application Schedule.

3.	Execution

3.1	EXAMINATION

.1	Verification of Conditions:

.1	Examine all surface conditions to which the work of this Section is to be applied.  Report unacceptable surfaces to the Province.

3.2	PREPARATION

.1	Protection of In-Place Conditions:

.1	Protect adjacent surfaces from damage or overspray resulting from work of this Section.  Mask and/or cover adjacent surfaces.  Make good any damage at own expense, to the Province's satisfaction.

.2	Post "Wet Coatings" and "No Smoking" signs, while work is in progress and curing

.2	Surface Preparation:

.1	Prepare surfaces and apply as directed in the manufacturer's literature.

3.3	erection / installation / application

.1	Special Techniques:

.1	Match finished work to approved samples.  Maintain uniform thickness, sheen, colour, texture and free from defects detrimental to appearance of performance.

.2	Cured thickness of applied material:  3 mm.

3.4	CLEANING

.1	Promptly, as the work proceeds and upon completion, clean up excess materials and rubbish.

3.5	APPLICATION SCHEDULE

| Room No./Name | Material | Finish | [Colour] | [Top Coat Thickness] |
| --- | --- | --- | --- | --- |
| [ ] | [Epoxy Matrix] [Epoxy Aggregate] | [Non-slip] [Satin] [Gloss] | [ ] | [300] [600] micrometres |
| [ ] | [ ] | [ ] | [ ] | [ ] |
| All other locations scheduled to receive epoxy flooring | [ ] | [ ] | [ ] | [ ] |

SPEC NOTE:  Top coat thickness only applies to epoxy matrix flooring.  Specify a non-slip finish in Storage Areas and Maintenance Rooms.

SPEC NOTE:  Coordinate above schedule with Room Finish Schedule and with Colour Schedule if a Colour Schedule will be included in Bid Documents.

# END OF SECTION