Section Cover Page

Section 09 96 56 2014-11-01 Epoxy Wall Coatings

Refer to “LEED Notes and Credits” page for additional guidance for LEED projects. Delete LEED items if project: .1 is excluded by the Department’s policy on LEED, or .2 the Department has determined that the work of this Contract is not to attain a LEED rating.

This Master Specification Section contains:

.1	This Cover Sheet

.2	LEED Notes and Credits

.3	Specification Section Text:

1.	General

1.1	Related Work Specified in Other Sections

1.2	Product Options and Substitutions

1.3	Reference Documents

1.4	Qualifications

1.5	Submittals

1.6	Quality Assurance

1.7	Delivery, Storage and Handling

1.8	Site Conditions

1.9	Protection

2.	Products

2.1	Material

2.2	Colours

3.	Execution

3.1	Examination

3.2	Preparation/Application

3.3	Cleanup

3.4	Application Schedule

LEED Notes:

N/A.

LEED Credits:

Contribution towards LEED credits in this section may apply as follows:

LEED Credit EQ 4.2 Low-Emitting Materials: Paint and Coatings.

In order to obtain EQ 4.2 protective coatings have to comply with the maximum VOC content limits of the State of California’s South Coast Air Quality Management District (SCAQMD) Rule #1113, Architectural Coatings, January 2004.

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	[LEED Submittal Forms	Section 01 32 16]

.2	[LEED Requirements	Section 01 35 18]

.3	[Environmental Procedures	Section 01 35 20]

.4	Waste Management and Disposal	Section 01 74 19.

.5	Substrate:	Section [            ].

.6	Sealants:	Section 07 92 00.

.7	Epoxy flooring:	Section 09 67 16.

.8	Painting:	Section 09 91 05.

.9	Vinyl-acrylic coatings:	Section 09 96 53.

1.2	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 01 for requirements pertaining to product options and substitutions.

1.3	REFERENCE Documents

SPEC NOTE: Edit this article to include only standards referenced within the edited version of this Section, including LEED documentation and sustainable practices.

.1	American Society for Testing and Materials (ASTM)

| .1 | ASTM D522-93a(2008) | Standard Test Methods for Mandrel Bend Test of Attached Organic Coatings |
| --- | --- | --- |
| .2 | ASTM D1308-02(2007) | Standard Test Method for Effect of Household Chemicals on Clear and Pigmented Organic Finishes |
| .3 | ASTM D1360-98(2004) | Standard Test Method for Fire Retardancy of Paints (Cabinet Method) |
| .4 | ASTM D2486-06 | Standard Test Methods for Scrub Resistance of Wall Paints |
| .5 | ASTM E96/E96M-05 | Standard Test Methods for Water Vapor Transmission of Materials |

.2	Canada Green Building Council (CaGBC)

| .1 | LEED Canada 2009 Rating System | LEED Canada for New Construction and Major Renovations. LEED Canada for Core and Shell Development. Website: www.cagbc.org |
| --- | --- | --- |

.3	Canadian General Standards Board (CGSB)

| .1 | CGSB 1-GP-71 Set of 3 Standards 2003 | Methods of Testing Paints and Pigments - Set includes 1-GP-71 No. 5-96, 1-GP-71 No. 38-96 and 1-GP-71 No. 73-96 |
| --- | --- | --- |

.4	Green Seal (GS)

| .1 | Green Seal Standards GS-11 | Paints, First Edition, May 20, 1993 |
| --- | --- | --- |

1.4	QUALIFICATIONS

.1	The work of this Section shall be applied only by experienced applicators of the specified products.

1.5	Submittals

.1	Product Data:

.1	Submit manufacturer’s printed product literature, specifications and data sheets in accordance with Section 01 33 00 - Submittal Procedures.

.2	Submit [two] [          ] copies of Workplace Hazardous Materials Information System (WHMIS) Material Safety Data Sheets (MSDS) in accordance with Section [01 33 00 - Submittal Procedures] [         ]. Indicate VOCs during application [and curing] [         ].

.2	Samples:

.1	Submit 300 mm x 300 mm representative sample of wall coating in selected colour.  Identify sample by project name including material and colour identification.

.2	Site apply sample installation to minimum 2 m2 area, to surface as directed, for approval by the Province.  Retain approved sample until work is completed and accepted.

.3	Sustainable Design Submittals:

SPEC NOTE: Use the following paragraph when LEED Submittals are required.

.1	LEED Submittals: Submit documentation in accordance with Section 01 35 18 – LEED Requirements.  Submit documentation for the following:

.1	Indoor Environmental Quality:

SPEC NOTE: Delete LEED submittal item below if project is not to attain LEED certification or if Credit EQ 4.2 Low Emitting Materials: Paint and Coatings is not being sought. If project is to follow sustainable building practices but not attaining LEED certification, delete references to LEED and retain SCAQMD Rule 1113 and GS-11 as a sustainable submittals.

.1	EQ Credit 4.2 - Low-Emitting Materials: Paint and Coatings

1.6	Quality Assurance

.1	Qualifications:

.1	Installers / Applicators / Erectors:

.1	The work of this Section shall be applied only by experienced applicators of the specified products.

1.7	DELIVERY, Storage, and Handling

.1	Delivery and Acceptance Requirements:

.1	Deliver materials undamaged, in original containers, with manufacturer's labels and seals intact.

.2	Storage and Handling Requirements:

.1	Store materials in protected conditions with a minimum temperature of 12°C.

.3	Waste Management and Disposal:

.1	Separate waste materials for [reuse] [and] [recycling] in accordance with Section 01 74 19 – Management and Disposal.

1.8	site CONDITIONS

.1	Ambient Conditions:

.1	For exterior coatings:  Comply with coating manufacturer's recommendations.  Do not apply under adverse weather conditions which could affect coating performance.

.2	For interior coatings:  Minimum surface temperature 10°C 24 hours before, during and 24 hours after application or until cured; adequate controlled ventilation; bright, uniform lighting; broom clean; reasonably dust free.

1.9	PROTECTION

.1	Protect adjacent surfaces from damage and overspray resulting from work of this Section.  Mask or cover adjacent surfaces.  Make good any damage at own expense, to the Province's satisfaction.

.2	Post "Wet Coatings" and "No Smoking" signs while work is in progress and curing.

2.	Products

2.1	MATERIAL

.1	Solvent based, two component thermo-setting, 100% epoxy coating meeting the following requirements:

| Property | Test Method | Requirement |
| --- | --- | --- |
| Water vapour transmission | ASTM E96 | 0.3 metric perms. max. |
| Colour fastness | CGSB 1-GP-71 Fade-ometer | No colour change, chalking or film defects, after 48 hours |
| Fire resistance | ASTM D1360 Cabinet method | Less than 17 g lost over masonry backing |
| Scrubbability | ASTM D2486 Gardner Scrubbability Machine | No effect on film after 5000 cycles |
| Radiation resistance | Exposure to Gamma rays of 35 roentgen intensity per hour at distance of 1625 mm from Cobalt 60 cell | Unaffected as measured by difference in reflectance |
| Toxicity | Evaluated by Canadian Department of Agriculture | Approved non-toxic |

Continued next page

2.1	MATERIALS (Cont'd)

| Property | Test Method | Requirement |
| --- | --- | --- |
| Heat & cold cycling | 50 cycles on masonry backing. Each cycle 8 hours at 70°C 16 hours at 23°C | No cracking, loss of adhesion, or other film defects |
| Flexibility | ASTM D522 Mandrel Test | Passing 3 mm bend without cracking or peeling |
| Impact resistance | CGSB 1-GP-71, Method 147.1 Gardner Impact Test | Passing 11 J without cracking |
| Stain resistance | ASTM D1308 | Not affected by common acids, hydroxides, salts and household cleaning agents |

SPEC NOTE:  The above material is used internally where optimum chemical and solvent resistance is required; recommended for meat and food processing plants.  The following materials meet the above requirements:   Epo-Kote 2000 manufactured by Monteith, Duroplast 100 manufactured by Duochem or approved alternative.

2.2	COLOURS

.1	[One] [Two] [     ] colours will be selected by the Province from manufacturer's standard range.

OR

.1	Refer to Application Schedule.

SPEC NOTE:  Coordinate above with schedule at end of this Section.

3.	Execution

3.1	EXAMINATION

.1	Examine all surface conditions to which the work of this Section is to be applied.  Report any deficient surfaces to the Province.

3.2	PREPARATION/APPLICATION

.1	Prepare surfaces and apply in accordance with manufacturer's instruction.

.2	Match finished work to approved samples, maintain uniform thickness, sheen, colour, texture and free from defects detrimental to appearance or performance.

.3	Minimum cured thickness of applied material shall be 200 to 250 micrometres.

3.3	CLEANUP

.1	Promptly, as the work proceeds and upon completion, clean up excess materials and rubbish.

3.4	APPLICATION SCHEDULE

| Room No./Name | Finish | [Colour] |
| --- | --- | --- |
| [ ] | [Satin] [Semi-gloss] [Gloss] | [ ] |
| [ ] | [ ] | [ ] |
| All other locations scheduled to receive epoxy coating | [ ] | [ ] |

END OF SECTION