Section Cover Page

Section 32 17 10 2018-08-15 Road and Parking Appurtenances

Use this Section to specify supply and installation of products listed.  Specify supply and installation of premanufactured car plug-in posts in Division 26.  Specify electrical requirements in Division 26.

This Master Specification Section contains:

.1	This Cover Sheet

.2	Specification Section Text:

1.	General

1.1	Related Requirements

1.2	Reference Documents

1.3	Product Options and Substitutions

1.4	Detail Drawings

1.5	Coordination

2.	Products

2.1	Concrete Bases

2.2	Metal Car Plug-In Rails and Posts

2.3	Wooden Car Plug-In Rails

2.4	Guard Posts

2.5	Premanufactured Curbs

2.6	Site Painting and Finishing Materials

2.7	Fabrication of Metal Components

3.	Execution

3.1	Installation, General

3.2	Installation of Concrete Bases

3.3	Installation of Wooden Car Plug-In Rails

3.4	Painting and Finishing

3.5	Site Painting and Finishing Schedule

.3	Detail Drawings:

32 17 10.01	Street Light Base

32 17 10.02	Metal Car Plug-In Rail

32 17 10.03	Metal Car Plug-In Rail (Hollow Structural Steel Beam)

32 17 10.04	Wooden Car Plug-In Rail

32 17 10.05	Metal Pedestal Plug-In Post

32 17 10.06	Guard Post Detail

1.	General

1.1	RELATED Requirements

.1	[Custom Steel Fabrications:	Section 05 50 00].

.2	[Site Painting and Finishing General Requirements:	Section 09 91 05].

.3	[Exterior Site Painting and Finishing Schedules:	Section 09 91 13].

.4	Electrical components and installation:	Division 26.

.5	[Premanufactured Car Heater Posts:	Section [           ].

.6	[Poles and Standards:	Section 26 56 13].

.7	Site Excavating, Filling and Grading: 	Section 31 23 10.

1.2	REFERENCE DOCUMENTS

.1	Canadian Standards Association (CSA):

| .1 | CSA A23.4-16 | Precast Concrete - Materials and Construction |
| --- | --- | --- |
| .2 | CSA G30.18-09 (R2014) | Carbon Steel Bars for Concrete Reinforcement |
| .3 | CAN/CSA-G40.20-13/G40.21-13 | General Requirements for Rolled or Welded Structural Quality Steel / Structural quality steel |
| .4 | CAN/CSA G164-M92 (R2003) | Hot Dip Galvanizing of Irregularly Shaped Articles |
| .5 | CAN/CSA-O141-05 (R2014) | Softwood Lumber |

1.2	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 01 for requirements pertaining to product options and substitutions.

1.3	DETAIL DRAWINGS

.1	The following detail drawings are appended hereto and form part of this Section:

Number	Title

32 17 10.01	Street Light Base

32 17 10.02	Metal Car Plug-In Rail

32 17 10.03	Metal Car Plug-In Rail 1	(Hollow Structural Steel Beam1

32 17 10.04	Wooden Car Plug-In Rail

32 17 10.05	Metal Pedestal Plug-In Post

32 17 10.06	Guard Post Detail

SPEC NOTE:  Include only those Detail Drawings applicable to the Project.  Coordinate project working drawings with Detail Drawings.  Delete detail for precast concrete curbs if only plastic curbs are specified.

SPEC NOTE:  If soils report indicates unusual conditions, design of concrete bases may have to be revised from standard detail drawings.

1.4	COORDINATION

.1	Coordinate anchor bolt locations for street lights with Section 26 56 13.

.2	Coordinate anchor bolt locations for premanufactured plug-in posts with Section [                    ].

.3	Coordinate requirements for electrical components to be embedded in concrete or concealed in steel components with work specified in Division 26.

2.	Products

2.1	CONCRETE BASES

.1	Reinforcing Steel:  deformed steel bars to CSA G30.18.

.2	Concrete:  20 MPa compressive strength @ 28 days, [Type 10-normal] [Type 50-sulphate resistant].

.3	Anchor Bolts and Nuts:  steel, hot dip galvanized to CAN/CSA G164, as detailed.

2.2	METAL CAR PLUG-IN RAILS AND POSTS

SPEC NOTE:  Specify premanufactured plug-in posts in Division 26.

.1	[Steel Sections and Plates:  to CAN/CSA-G40.20 and CAN/CSA-G40.21, Grade [260W][   ]].

.2	Concrete:  20 MPa compressive strength @ 28 days, [Type 10-normal][Type 50-sulphate resistant].

.3	Reinforcing Steel:  deformed steel bars to CSA G30.18, as detailed.

.4	Shop Primer:  shop standard compatible with site painting and finishing materials.

2.3	WOODEN CAR PLUG-IN RAILS

.1	Wood:  douglas fir, pine or hemlock, kiln-dried, S4S dimension lumber to CAN/CSA-O141, preservative pressure-treated.

.2	Nails, Spikes & Straps:  steel, hot-dip galvanized.

2.4	GUARD POSTS

SPEC NOTE:  Detail drawing 32 17 10.6 at end of this Section describes guard posts for protection to site elements not generally exposed to vehicle traffic, e.g. electrical transformers.  Amend drawing as required where greater exposure to vehicle traffic is anticipated, e.g. at vehicle entrance doors.

.1	Steel Post:  to CAN/CSA-G40.20 and CAN/CSA-G40, Grade [260W][   ].

.2	Concrete:  20 MPa compressive strength @ 28 days, [Type 10-normal] [Type 50-sulphate resistant].

.3	Shop Primer:  shop standard compatible with site painting and finishing materials.

2.5	SITE PAINTING AND FINISHING MATERIALS

SPEC NOTE:  This Section assumes site painting and finishing materials applies to new work only.  For exterior site repainting and refinishing requirements refer to Section 09 91 15.

.1	As specified in Sections 09 91 05 and 09 9 13.

OR

SPEC NOTE:  Delete previous paragraph and specify following paragraph if roadway and parking appurtenances is part of a separate site development contract and Sections 09 91 05 and 09 91 13 are not used.

.1	Use products listed in Chapter 5, Products List, of the Canadian Painting Contractors Association (CPCA) Manual, and as specified in Site Painting and Finishing Schedule.

2.6	FABRICATION OF METAL COMPONENTS

.1	As specified in Section 05 50 00.

OR

SPEC NOTE:  Delete previous clause and specify the following if roadway and parking appurtenances is part of a separate site development contract and Section 05 50 00 is not used.

.1	Fabricate components square, straight, true, free from warpage and other defects.  Accurately cut, machine, file and fit joints, corners, copes and mitres.

.2	Remove loose mill scale, rust, oil, grease, dirt and other foreign matter using one or more of the following methods:

.1	solvent cleaning

.2	wire brushing

.3	power wire brushing

.4	sandblasting

.3	Apply primer to bare steel within six hours after blast cleaning, in accordance with manufacturer's recommendations.

.4	Apply thick layer of asphaltic paint to concealed surface of base plates to be set into concrete.  Allow to dry before installation.

3.	Execution

3.1	INSTALLATION, GENERAL

.1	Install components square, straight and true to line.  Securely anchor components and accessories in place.

3.2	INSTALLATION OF CONCRETE BASES

.1	Do not pour concrete against frozen surfaces.

.2	Correctly relocate items displaced during concrete placement.

3.3	INSTALLATION OF WOODEN CAR PLUG-IN RAILS

.1	Compact bottom of wood post holes to provide firm foundation.  Backfill in 150 mm layers.  Compact each layer before placing succeeding layer.

.2	Leave a depression 150 mm deep around wood posts until painting is completed, then fill to finished grade level.

3.4	PAINTING AND FINISHING

.1	As specified in Sections 09 91 05 and 09 91 13.

OR

SPEC NOTE:  Delete previous paragraph and specify following paragraph if roadway and parking appurtenances is part of a separate site development contract and Sections 09 91 05 and 09 91 13 are not used.

.1	Comply with Canadian Painting Contractors' Architectural Specification (CPCA) Manual.

.2	Treat cut tops of wood posts and cut ends of wood rails with two coats of wood preservative prior to application of primer.

3.5	SITE PAINTING AND FINISHING SCHEDULE

SPEC NOTE:  Delete this article if Section 09 91 13 is used.  Edit to suit project requirements.

| Substrate | Finish System | Product No. |
| --- | --- | --- |
| Wood | EXT 1-A Alkyd Finish |  |
|  | 1st Coat: Alkyd or Oil Primer | 5 or 7 |
|  | 2nd Coat: Alkyd | 8, 9 |
|  | 3rd Coat: Alkyd | 8, 9 |
|  | EXT 1-B Latex Finish |  |
|  | 1st Coat: Alkyd or Oil Primer | 5 or 7 |
|  | 2nd Coat: Latex | 10, 11, 119 |
|  | 3rd Coat: Latex | 10, 11, 119 |
|  | EXT 1-C Semi-Transparent Stain Finish |  |
|  | 1st Coat: Semi-Transparent Oil Stain | 13 |
|  | 2nd Coat: Semi-Transparent Oil Stain | 13 |
|  | EXT 1-D Solid Colour Stain Finish |  |
|  | 1st Coat: Solid Colour Oil Stain | 14 |
|  | 2nd Coat: Solid Colour Oil Stain | 14 |
|  | EXT 1-E Latex Solid Colour Stain Finish |  |
|  | 1st Coat: Solid Colour Oil Stain | 16 |
|  | 2nd Coat: Solid Colour Oil Stain | 16 |
| Steel | EXT 11-A Alkyd Finish |  |
|  | 1st Coat: Alkyd Metal Primer | 23,24 or 25 |
|  | 2nd Coat: Alkyd | 8, 9 |
|  | 3rd Coat: Alkyd | 8, 9 |
|  | EXT 11-B Quick Dry Spray Finish |  |
|  | 1st Coat: Quick Dry Primer | 95 |
|  | 2nd Coat: Quick Dry Enamel | 96 |
|  | 3rd Coat: Quick Dry Enamel | 96 |

3.5	SITE PAINTING AND FINISHING SCHEDULE (CONTINUED)

| Substrate | Finish System | Product No. |
| --- | --- | --- |
| Steel (cont'd) | EXT 11-C Aluminum Paint Finish |  |
|  | 1st Coat: Alkyd Metal Primer | 23,24 or 25 |
|  | 2nd Coat: Aluminum Paint | 1 |
|  | 3rd Coat: Aluminum Paint | 1 |
|  | EXT 11-D Two Component Epoxy Finish |  |
|  | 1st Coat: Primer | 101 Type I |
|  | 2nd Coat: Two Component Epoxy | 98 or 77 |
|  | 3rd Coat: Two Component Epoxy | 98 or 77 |
|  | EXT 11-E Water Based Epoxy Finish |  |
|  | 1st Coat: Rust Inhibitive Primer | 128 |
|  | 2nd Coat: Water Based Coating | 115 |
|  | 3rd Coat: Water Based Coating | 115 |
| Galvanized | EXT 12-A Alkyd Finish |  |
| Metal |  |  |
|  | 1st Coat: Cementitious Primer | 26 |
|  | 2nd Coat: Alkyd | 8, 9 |
|  | 3rd Coat: Alkyd | 8, 9 |
|  | EXT 12-B Aluminum Finish |  |
|  | 1st Coat: Cementitious Primer | 26 |
|  | 2nd Coat: Aluminum Paint | 1 |
|  | 3rd Coat: Aluminum Paint | 1 |
|  | EXT 12-D Latex Finish |  |
|  | 1st Coat: Cementitious Primer | 26 |
|  | 2nd Coat: Acrylic Latex | 10, 11, 119 |
|  | 3rd Coat: Acrylic Latex | 10, 11, 119 |
|  | EXT 12-E Latex Dry Fall Finish |  |
|  | 1st Coat: Cementitious Primer | 26 |
|  | 2nd Coat: Latex Dry Fall | 118 |

END OF SECTION