Section Cover Page

Section 03354 2002-07-04 Concrete Floor Finishes

Use this Section to specify concrete floor finishes such as hardened concrete floor finish, coloured concrete, sealed concrete and waxed concrete.

This Master Specification Section contains:

.1	This Cover Sheet

.2	Specification Section Text:

1.	General

1.1	Related Work Specified in Other Sections

  - Reference Standards

  - Product Data

  - Delivery, Storage and Handling

  - Environmental Requirements

  - Coordination

2.	Products

2.1	Materials

3.	Execution

3.1	Verification of Conditions

3.2	Hardened Floor Finish

  - Coloured Concrete

  - Concrete Sealer

  - Wax Finish

  - Concrete Floor Finish Schedule

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	Cast-in-place concrete:	Section [03300] [03302].

1.2	REFERENCE documents

.1	CAN/CSA-A23.1-00, Concrete Materials and Methods of Concrete Construction.

.2	CAN/CGSB-25.20-95, Surface Sealer for Floors.

  - Product Data

.1	Submit product data for each product in accordance with Division 01.

.2	Include application instructions for [hardeners] [colouring agents] [and] [sealers]

.3	Submit WHMIS MSDS – Material Safety Data Sheets for each product. Indicate VOC levels.

  - DeLivery, Storage and handling

.1	Deliver materials to site in containers sealed and labeled by manufacturers.

.2	Comply with requirements of Workplace Hazardous Materials Information System (WHMIS) regarding storage, handling and disposal of hazardous materials.

  - environmental requirements

.1	Provide temporary lighting, as required, to provide a minimum of 1200 watt light source, placed 2.5 meters above floor surface, for each 40 m2 of floor being finished.

.2	Maintain ambient temperature of 10°C minimum from [7] [  ] days before installation to at least 48 hours after completion of work and maintain relative humidity not higher than 40% during same period.

.3	Ensure substrate is within moisture limits prescribed by product manufacturers.

.4	Ventilate enclosed spaces as required during product application and for 48 hours after application.

  - coordination

.1	Coordinate the work of this section with the work of Section 03300 as required for [hardeners] [and] [colouring agents] to ensure proper application.

2.	Products

  - MATERIALS

SPEC NOTE: It is sometimes advisable to specify coloured products to ensure visible uniform application of product where use of colour will not be detrimental to aesthetics or project requirements.

.1	Non-Metallic Floor Hardener:  premixed, dry shake surface hardener, cement to hardener ratio of [2 to 1], [clear] [[     ] coloured] cement, [light reflective].

SPEC NOTE: Volcanic basaltic aggregate (traprock) should be used for low spark capability. Quartz aggregate do not have good impact resistance but are adequate for light to medium duty floors. Quartz aggregate is lighter in colour than traprock and therefore is a better aggregate for coloured floors.

.1	Volcanic basaltic aggregate (Traprock).

.2	Quartz aggregate.

SPEC NOTE: Use metallic floor hardeners in dry areas only.

.2	Metallic Floor Hardener:  premixed, cement to hardener ratio [2 to 1], [light reflective], [static disseminating] oxidizable metallic hardener.

.3	Slip Resistant Abrasive Aggregate: [crushed emery with minimum [50]% aluminum oxide] [homogeneous aluminum oxide, minimum 95%] [ferric oxide, minimum 25%] [silicon carbide].

.4	Colouring Agent:  non-metallic type concrete colouring pigments.

.5	Surface Sealer: to CAN/CGSB-25.20, [Type 1 – Solvent Based] [Type 2 – Water Based], [clear] [coloured].

.1	Surface sealers manufactured or formulated with aromatic solvents, formaldehyde, halogenated solvents, mercury, lead, hexavelant chromium and their compounds are not acceptable.

.2	Surface sealer shall be compatible with the hardener and shall be manufactured by  the hardener manufacturer.

.6	Wax:  [coloured] [clear] acrylic carnuba wax.

.7	Colour:  Minister will select colour for each product from manufacturer’s full colour range, unless a colour has been specified.

3.	Execution

3.1	verification of conditions

.1	Verify that [slabs] [substrate] [site conditions] and surfaces are ready to receive work.

  - HARDENED FLOOR FINISH

SPEC NOTE:  Floor hardener applications are considered as light 3.66 to 4.88 kg/m2, medium 4.88 to 6.1 kg/m2, and heavy 6.1 to 9.76 kg/m2.  Anything greater than 9.76 kg/m2 is a topping application and should be specified in Section 03300 – Cast-In-Place Concrete.

.1	Apply [non-metallic] [metallic] floor hardener at rate of [   ] kg/m² of surface area, to manufacturer's instructions and as follows.

.2	Use measured areas to ensure accurate quantity is applied.

.3	Apply hardener in two shakes; first shake – 2/3 of rate specified, second shake – 1/3 of rate specified.

.4	Use slip resistant aggregate in strict accordance with manufacturer’s written application and finishing instructions.

.5	Immediately after first mechanical floating, apply first hardener shake uniformly by broadcast method.

.6	Float first shake when hardener is saturated by the concrete mix and has started to blend with the concrete mortar.

.7	Immediately after floating first shake, apply second shake perpendicular to direction of first shake.

.8	Float second shake, when saturated by moisture absorbed from concrete, [once to produce coarse textured non-slip finish] [twice to produce medium textured non-slip finish].

.9	[Flat steel trowel to produce fine textured non-slip finish.]

  - Coloured Concrete

.1	Apply colouring agent in accordance with manufacturer’s written instructions and as follows:

.1	Apply colouring agent at rate recommended by manufacturer to produce uniform colouring over the entire slab surface, using measured areas to ensure accurate quantity is applied.

.2	Apply colouring agent in two shakes; first shake – 2/3 of rate specified, second shake – 1/3 of rate specified.

.3	Apply second shake perpendicular to direction of the first shake.

  - Concrete sealer

.1	Apply surface sealer in accordance with manufacturer’s written instructions.

3.5	WAX FINISH

.1	Apply wax finish in accordance with manufacturer's instructions [to all concrete floors, except those which are scheduled to receive finishes specified herein or in other Sections.]

3.6	concrete floor finish schedule

SPEC NOTE: Specify product, location and colour to suit project. Use format below, shown with examples.

| # Product | # Location | # Colour |
| --- | --- | --- |
| [Non-metallic floor hardener] | [Chemical storage room] | [ ] [N/A] |
| [Metallic floor hardener] | [Storage rooms] | [ ] [N/A] |
| [with non-slip aggregate] | [Kitchen] [Shower rooms] | [ ] [N/A] |
| [Chemical hardener] | [Mechanical rooms] | [ ] [N/A] |
| [Colouring Agent] | [Rooms 101, 103, 115] | [Red] |
|  | [Rooms 215, 225, 230] | [Green] |
|  | [Room 303, 310] | [Grey] |
| [Surface sealer] | [Gymnasium floor slab] | [ ] [N/A] |
| [Wax] | [Rooms 125, 126, 127] | [ ] [N/A] |
|  | [Room 128] | [Red] |

END OF SECTION