Section Cover Page

Section 06400 2007-08-24 Architectural Woodwork

Use this Section to specify supply and installation of all interior and exterior shop-fabricated woodwork items, except items noted as exceptions on Data Sheet - Section Scope.

This Master Specification Section contains:

.1	This Cover Page.

.2	Data Sheets for the following: Section Scope, Specification Preparation, Technical Data, Coordination and  Sample Schedule

.3	Specification Section Text:

1.	General

1.1	Related Sections

  - Reference Documents

  - Product Options and Substitutions

1.4	Shop Drawings

1.5	Product Data

1.6	Samples

  - Project Record Documents

  - Quality Assurance

1.9	Mock-up

1.10	Delivery, Storage and Handling

  - Coordination

  - Extended Warranty

  - Security for Extended Warranty

  - Inspection

2.	Products

2.1	Lumber, General

2.2	Panel Products, General

2.3	Accessories

  - Casework Hardware

  - Casework, General

2.6	Casework, [Stain with] Clear Finish [, Type [ ]]

2.7	Casework, Opaque Finish [, Type [ ]]

2.8	Casework, High Pressure Decorative Laminate (HPDL) Finish [, Type []]

2.9	High Pressure Decorative Laminate (HPDL) Countertops [and Splashbacks,] Self-Edge Type

2.10	High Pressure Decorative Laminate (HPDL) Countertops and Splashbacks, Post-Formed Type

2.11	Flush Panelling, Veneer

2.12	Stile and Rail Panelling, [Stain with] Clear Finish

2.13	[Trim] [and] [Handrails], [Stain with] Clear Finish

  - [Trim] [and] [Handrails], Opaque Finish

2.15	Fabrication

2.16	Factory Finishing Materials

2.17	Factory Finishing

3.	Execution

3.1	Verification of Conditions

3.2	Installation

3.3	Architectural Woodwork Schedule

This Master Specification Section includes shop-fabricated items listed on Section Cover Page, under Part 2 - Products.

Refer to construction trade definitions for a more complete listing of items that may need to be included in this Section.

Specify in this Section all items included in construction trade definitions, except the following:

.1	Flush Wood Doors, specified in Section 08211.

.2	Plastic Faced Doors and Panels, specified in Section 08221.

Also specify the following items in this Section, even though similar products may be specified in other Sections:

.1	Casework hardware.

.2	Factory Finishing Materials.

.3	Sealants for casework.

.4	Glass and plastic glazing completely surrounded by architectural woodwork.

.5	Mirrors installed in wood frames.

.6	Custom-fabricated wood furniture.

USE OF REFERENCE DOCUMENTS

This Specification is based primarily on “Architectural Woodwork Quality Standards Illustrated” 2003 edition, published by the Architectural Woodwork Manufacturers Association of Canada and the Architectural Woodwork Institute, in the U.S., hereinafter referred to as the AWMAC Manual.  Specifier should have a copy on hand, be familiar with, and frequently refer to this edition of the AWMAC Manual in order to properly specify requirements of this Section.

# QUALITY

AWMAC quality grades allow the architectural woodwork manufacturer a number of options in the choice of materials and construction.  This specification selects some of these options and establishes some requirements for materials and workmanship that differ from the referenced standard. For example, this specification does not permit the use of melamine and limits the use of medium density fibreboard (MDF) to drawer bottoms only.

SPECIFICATION SECTION STRUCTURE

Specification Section text is highly structured.  Review entire Section prior to editing.  Section structure in Part 2 is based primarily on general categories of components, as identified in Article headings 2.5 to 2.14.  These articles include detailed specification requirements applicable to a given component category (except for accessories and requirements related to factory finishing, which are specified separately).

If there are required items that do not fit into any of the standard Articles (component categories), add additional Articles as required.  If all items within a given component category have identical specification requirements, it is unnecessary to assign any type designations and the structure remains relatively simple.  However, for some projects not all items within a component category will have identical requirements, e.g. some "Casework for Clear Finish" components may need to be red oak, others birch.  In such cases, assign different type designations to differentiate the component categories.  Specify the variables by inserting one or more additional articles to address the exceptions to the first component category.  For example:

2.6	CASEWORK, CLEAR FINISH, TYPE B

.1	Same as Casework, Clear Finish, Type A, except as follows:

Use the "Architectural Woodwork Schedule" at end of Section to provide a summary listing of all components required for project, including their locations, factory finish requirements where applicable, and other variables as necessary.  Refer to Data Sheet - Sample Schedule.

HIGH PRESSURE DECORATIVE LAMINATE (HPDL)

High Pressure Decorative Laminate (HPDL) is also known as Plastic Laminate. The types for vertical applications are thinner than the types for horizontal applications. HPDL, in accordance with 2000 NEMA usage, is available in the following types.

- Horizontal  and Vertical General Purpose:

  - (HGS) and (VGS): thickest laminates available.

  - (HGL) and (VGL): slightly thinner than HGS and VGS respectively.

- Horizontal and Vertical Post Forming, (HGP) and (VGP): post forming use only.

- Fire Rated, (HGF)

- Cabinet Liner (CLS): Liner grade.

- Backer (BKL): Laminate backer grade.

HIGH PRESSURE DECORATIVE LAMINATE FINISHES AND SURFACE TEXTURES

“Cashmere”, “textured”, “suede” and “matte” are terms different manufacturers use to describe the most common type of finish available. As these finishes relate mostly to the way they reflect light, or sheen, the manufacturer’s finish terms listed above will be referred to as “matte”.  Another common type of finish is “gloss”. Other finishes are available at increased cost.  Consult with manufacturers prior to specifying a finish other than matte or gloss.

High pressure decorative laminates are also available with different surface textures. These surface textures may be smooth or textured. Textured surfaces may be lightly textured with a slightly pebbled surface, or they may have a pronounced texture such as simulated slate or some other texture determined by the manufacturer. If a surface texture other than smooth is specified, provide a generic description.

Alternatively, an acceptable range of finish and surface texture may be specified by naming a minimum of three products, each of which has an acceptable finish and surface texture.

# COORDINATION WITH DRAWINGS

Ensure that drawings show the following:

- Location of items, including hardware types.

- Extent of woodwork, configuration, operation of doors.

- Barrier-free accessibility requirements, as applicable.

- Architectural woodwork as distinct from stock design manufactured casework.

- Architectural woodwork as distinct from site fabricated finish  carpentry.

- Special veneer matching not specified as a recognized industry system.

- Details showing profiles, elevations, mouldings, edge treatment, and transitions from veneer to lumber for Stile and Rail Panelling for Clear Finish.

- Details required but not included in AWMAC Manual.

- Same terminology as specifications, without repeating or adding specification requirements.

- Dimensions.

- Wood grain direction and plastic laminate pattern direction, when applicable.

- Items specified in other Sections but requiring cut-outs for incorporation into architectural woodwork.

- Arrangement of sliding door hardware, locks, light fixtures, panel hangers and anchorage, and similar hardware and accessories.

- Glass doors and shelves and other non-wood components.

Do not include information on drawings that describes quality of materials, components or assemblies.  Specify such requirements in this Section.

Do not provide on drawings detailing already included by reference to the AWMAC Manual.

3.3	ARCHITECTURAL WOODWORK SCHEDULE

| Location/Components | Finish and Surface Texture |  | Gloss Level | Colour/ Pattern | Finished at |
| --- | --- | --- | --- | --- | --- |
| Rms: 137, 143, 267, 279 |  |  |  |  |  |
| Casework, Clear Finish, Type 1 Exposed Surfaces Semi-exposed Surfaces |  | Polyurethane Varnish Polyurethane Varnish | Satin | Clear | Factory |
| Countertops and Splashbacks HPDL Finish, Self Edge Type |  | Self-Edge Type, Matte & Smooth |  | Blue/speckled | Factory |
| Flush Panelling, Veneer |  | Polyurethane Varnish | Satin | Clear | Site |
| Trim |  | Polyurethane Varnish | Semi Gloss | Clear | Site |
| Rms: 107, 256 |  |  |  |  |  |
| Casework, Opaque Finish, Type 2 Exposed Surfaces Semi-exposed Surfaces |  | Alkyd Alkyd | Velvet Velvet | Almond Almond | Factory |
| Countertops and Splashbacks HPDL Finish, Post Formed |  | Matte & Smooth | Matte | Blue | Factory |
| Trim |  | Alkyd | Semi Gloss | Almond | Site |
| Rm: 102, |  |  |  |  |  |
| Casework, HDPL Finish Exposed Surfaces Semi-exposed Surfaces |  | Matte & Textured Matte & Smooth |  | Off White | Factory |
| Countertops and Splashbacks, HPDL Finish, Self Edge Type |  | Matte & Textured |  | Blue/speckled | Factory |
| Trim |  | Alkyd | Semi Gloss | Off White | Site |

END OF DATA SHEETS

1.	General

1.1	RELATED SECTIONS

.1	Finish Carpentry:	Section 06200.

.2	Flush Wood Doors:	Section 08211.

.3	Plastic Faced Doors and Panels:	Section 08221.

.4	Site Painting and Finishing - General Requirements:	Section 09901.

1.2	REFERENCE DOCUMENTS

.1	“Architectural Woodwork Quality Standards Illustrated”, Eighth edition, 2003, published by the Architectural Woodwork Institute of the U.S. and jointly copyrighted with the Architectural Woodwork Manufacturer's Association of Canada (AWMAC). This document is herein referred to as the “AWMAC Manual”.

.2	ANSI/BMHA A156.9-1994, American National Standard for Cabinet Hardware.

  - Product options and substitutions

.1	Refer to Section 01621 for requirements pertaining to product options and substitutions.

1.4	SHOP DRAWINGS

.1	Comply with requirements of Division 1.

.2	Indicate materials, factory finishes, thicknesses, and hardware. Include plans, elevations, sections and details at the following drawing scales:

.1	Plans and elevations – 1:20

.2	Sections – 1:10

.3	Details – 1:2

.3	Indicate construction details, locations of built-in items, connections, attachments, anchorage and location of exposed fastenings, as applicable.

1.5	PRODUCT DATA

.1	Comply with requirements of Division 1.

.2	Submit manufacturer's product literature for items not manufactured by architectural woodwork manufacturer, when requested.

1.6	SAMPLES

.1	Comply with requirements of Division 1.

.2	Submit 215 mm x 280 mm samples of panel products for each factory applied finish system.

.3	Submit 32 mm x 350 mm samples of lumber of each species.

.4	Finish one side and edge of samples representing items to receive factory finishes.

.5	Submit samples of veneer flitches when requested.

SPEC NOTE:  Specify samples of veneer flitches only if applicable, e.g. premium grade veneer paneling or custom laid up panels.

.6	Submit samples of plastic laminate for selection of colour.

1.7	PROJECT RECORD DOCUMENTS

SPEC NOTE:  Include this article for architectural woodwork valued at over $25,000.00, or woodwork involving unusual materials, fabrication methods or finishes.

.1	Comply with requirements of Division 1.

.2	Provide project record sheet identifying project title and address, Contractor and architectural woodwork manufacturer.

.3	Provide one set of reviewed shop drawings, indicating modifications to materials and shop finishes, and type and source of hardware and any specialty items used.

  - quality assurance

.1	Materials and workmanship shall meet or exceed recommendations and requirements of "AWMAC Manual".

.2	Requirements of this Section shall govern in case of conflict between this Section and the AWMAC Manual.

.3	Reference to custom or premium grade in this Section shall be as defined in the AWMAC Manual.

.4	Items without a grade specified shall be custom grade.

.5	Maintain a copy of the specified AWMAC Manual at the factory, readily available for duration of work.

.6	Installer shall be responsible for supplying field dimensions that will affect the work of this Section.

  - MOCK-UP

SPEC NOTE:  Include this Article when a large or complex quantity of Architectural Woodwork is involved.

.1	Provide mock-up of the following components [to site] [in factory]:

.1	[       ].

.2	[       ].

.2	Keep approved mock-up [on site] [in factory].

.3	Approved mock-up shall establish minimum standard and may [not] be incorporated into finished work of this Section.

1.10	DELIVERY, STORAGE AND HANDLING

.1	Deliver to site after receiving and storage areas have stable humidity and temperature conditions as recommended in AWMAC Manual.

.2	Protect architectural woodwork items against dampness during and after delivery.

.3	Store architectural woodwork items on level surfaces in ventilated areas, protected from direct sunlight and extreme changes in temperature or humidity.

1.11	COORDINATION

SPEC NOTE:  Delete following clause if all architectural woodwork is to be factory finished.

.1	For architectural woodwork items to be site finished, coordinate with work of Section 09901 to ensure that back-priming of surfaces concealed after installation is performed prior to installation.

SPEC NOTE:  Delete following clause if inapplicable.  Identify woodwork items and locations.  If extent of coordination required warrants, consider as column heading in Architectural Woodwork Schedule at end of this Section.

.2	Coordinate installation of the following items during fabrication of [         ], located in [         ]:

.1	[Electrical conduit.]

.2	[Electrical junction boxes.]

.3	[Electrical fixtures.]

.4	[         .]

1.12	extended warranty

.1	Provide a two year extended warranty on the work of the architectural woodwork trade, commencing on the date of Interim Acceptance of the Work. The terms of this extended warranty shall be the same as those provided under the terms of the AWMAC Certificate of Guarantee.

.2	The foregoing shall not be construed to mean that the architectural woodwork subcontractor or supplier must be a member of AWMAC or that an AWMAC Certificate of Guarantee must be provided.

  - SECURITY FOR Extended warranty

SPEC NOTE:  Consider specifying this Article only if the additional cost can be justified and the estimated cost of architectural woodwork is at least $25,000.00.

Cost of AWMAC Certificate of Guarantee ranges, on a sliding scale, from a minimum of $750.00 to less than 0.5% of the value of the architectural woodwork.  Contact AWMAC for current fee schedule.  Cost of a maintenance bond in 2003 varies from $4.50 to $6.00 per $1,000.00 of amount bonded.

.1	Provide security for the performance of Contractor's obligations under the extended warranty in the form of:

.1	an AWMAC Certificate of Guarantee, or

.2	a maintenance bond in the amount of 100% of the value of the architectural woodwork subcontract and in a form acceptable to the Minister.

.2	Submit AWMAC Certificate of Guarantee or maintenance bond prior to Interim Acceptance of the Work.

  - INSPECTION

SPEC NOTE:  Consider including this Article, together with Security for Extended Warranty, only if the estimated cost of architectural woodwork $50,000.00 or more.

Specifying inspection, in addition to security for the extended warranty, provides additional quality assurance (at additional cost) for non-members of AWMAC.  If inspection is specified, non-members must pay an inspection fee to AWMAC that is equivalent to the cost of obtaining the AWMAC Certificate of Guarantee in addition to the cost of a maintenance bond.

.1	Arrange and pay for inspection by an AWMAC appointed inspector at the plant and at the site, regardless of whether or not the architectural woodwork subcontractor or supplier is a member of AWMAC.

.2	Submit a copy of the AWMAC inspection report with the AWMAC Certificate of Guarantee or the maintenance bond.

2.	Products

2.1	LUMBER, GENERAL

.1	Materials:  to AWMAC Manual, except where otherwise specified.

.1	Framing lumber: specified species, no. 1 grade, S4S.

.2	Hardwood lumber:  meeting AWMAC [custom] [premium] grade, [edge grain] for species specified.

.2	 Moisture Content:  between 4-9%.

2.2	PANEL PRODUCTS, GENERAL

.1	Provide panel products manufactured with phenol-formaldehyde or, if available, formaldehyde-free adhesive.

.2	Materials and Moisture Content:  to AWMAC Manual, except where otherwise specified.

.3	Particleboard:  to ANSI A208.1-1999, grade M-2, sanded faces, minimum density 720 kg/m3.

.4	Medium Density Fibreboard (MDF): to ANSI A208.2-1994, minimum density 769 kg/m3.

.5	Tempered Hardboard:  to CAN/CGSB-11.3-M87, Type 2, minimum density of 476 kg/m3.

.6	Softwood Plywood: to applicable CSA standards referenced in AWMAC Manual, G2S.

.7	Hardwood Plywood: to CSA-O115-M1982 (R2001). Graded in accordance with the Official Grading Rules for Canadian Hardwood Plywood.

.8	Veneers:

.1	Open-grain species:  minimum 0.71 mm thick.

.2	Close-grain species:  minimum 0.61 mm thick.

SPEC NOTE:  Verify suitability and availability of veneer characteristics for intended use.

.9	High Pressure Decorative Laminate (HPDL):  to AWMAC Manual.

2.3	ACCESSORIES

.1	Glass:  [               ]

.2	Glazing Accessories:  [               ].

SPEC NOTE:  If glass is completely surrounded by architectural woodwork, select applicable glass and glazing accessories from Basic Master Specification Section 08801 - Glass and Glazing General Requirements, and include here.

.3	Silicone Sealant:  to CAN/CGSB-19.13-M87, Shore A hardness 15-25, [            ] colour.

.4	[            ].

.5	Other Accessories:  to AWMAC Manual.

2.4	CASEWORK HARDWARE

SPEC NOTE: Hardware specified herein meets the Department’s minimum requirements for flush overlay casework.

.1	Where products are specified by proprietary names, other unnamed products may be substituted in accordance with the requirements of Section 01621 – Product Options and

Substitutions.

.2	Hinges: to ANSI-A156.9, B01612 – concealed hinge, self closing, 120 to 125 degree of opening, full overlay type for screw attachment complete with mounting plates. 	Acceptable

products:

.1	Model “71T558” by Blum.

.2	Model “HD1311-552” by Mepla.

.3	Model “A00P94” by Salice.

.4	Model “9956” by Hettich.

.3	Door and Drawer Pulls: back mount, 96 mm wire ‘D’ pulls, [brushed] [chrome] [brass]  [       ] finish.

.4	Drawer Slides For Drawers Up To 150 mm Deep: to ANSI-A156.9, B85051, side mount, steel construction, ¾ extension, ball bearing operation, rail disconnect system, bright zinc finish, length as required. Acceptable Products:

.1	Model “2132” by Accuride.

.2	Model “8300” by Knape & Vogt.

.3	Model “4500” by Waterloo.

.4	Model “5632” by Hettich.

.5	Drawer Slides For Drawers Deeper Than 150 mm: to ANSI-A156.9, B85051, side mount, steel construction, full extension, ball bearing operation, bright zinc finish, length as required. Acceptable Products:

.1	Model “3832” by Accuride.

.2	Model “8400” by Knape and Vogt.

.3	Model “3690” by Waterloo.

.4	Model “5632” by Hettich.

.6	Adjustable Shelving  Standards: to ANSI-A156.9, B84071, steel construction, adjustable in 13 mm increments, [almond]  [white] [brass] [zinc] finish. Acceptable Product:

.1	“KV-255” by Knape & Vogt.

.7	Shelf Rests: to ANSI-A156.9, B84091, steel construction, [almond] [white] [brass] [zinc] finish. Acceptable Product:

.1	“KV-256” by Knape & Vogt.

.8 	Locks: Inlay or rim style deadbolt or cam lock system, nickel finished.  Confirm keying required (master keyed, keyed alike in groups or keyed differently – supply keying schedule).

SPEC NOTE:  Add additional hardware beyond the typical casework hardware specified as required for specific projects.

SPEC NOTE: For casework requiring varying types of hardware or hardware finishes, compose the typical casework hardware, and any additional hardware required, into hardware sets and name the appropriate sets in Architectural Woodwork Schedule.

  - casework, general

.1	Fabricate casework to AWMAC grade specified in the individual casework articles in this Section.

.2	Furring, Blocking, Nailing Strips and Grounds: standard grade, to NLGA grading rules, for boards and dimension lumber.

.3	Framing:  pine species.

.4	Case Bodies, Ends, Dividers, Bottoms and Doors and Exposed Backs: 19 mm unfinished thickness.

.5	Non-exposed Backs: 6 mm unfinished thickness for all base, tall and wall cabinets with hanging strips and minimum of 12 mm for wall cabinets without hanging strips.

.6	Maximum Unsupported Shelf Length: 1219 mm.

.6	Thickness of Shelves Prior to Finishing:

.1	Unsupported lengths up to 813 mm: 19 mm particle board. or 19 mm veneer core plywood.

.2	Unsupported lengths between 814 mm and 914 mm: 19 mm veneer core plywood.

.3	Unsupported lengths between 915 mm and 1066 mm: 25 mm particle board or 27 mm veneer core plywood.

.4	Unsupported lengths between 1067 mm and 1219 mm: 27 mm veneer core plywood.

.7	Fabricate drawers of box construction as follows:

.1	Perimeters:  12 mm thickness prior to finishing, solid birch or maple for clear and opaque finishes and plywood or particleboard for plastic laminate finish.

.2	Bottoms:  6 mm thickness prior to finishing, MDF or tempered hardboard, dadoed or grooved into perimeter, captured on 3 sides, screwed to back of drawer with a minimum of 4 screws.

.3	Faces:  19 mm thickness prior to finishing.

.8	Edge banding:  hardwood, or plastic laminate. PVC edge banding is not acceptable.

.9	Apply panel face HPDL to overlap edges of edge banding HDPL.

.10	Mortise shelf standards fully into casework.

.11 	Maximum gap between adjacent doors or drawers shall be 3 mm.

.12	When screw fastening, fasten into MDF or particle board by pre-drilling holes as required and inserting plastic or metal screw dowels to receive screw fasteners.

2.6	CASEWORK, [stain with] CLEAR FINISH [, TYPE [ ]]

SPEC NOTE: Specify Custom grade for most conventional architectural woodwork. Specify Premium grade when the highest degree of workmanship is required, e.g., for special projects and for feature areas within an otherwise conventional architectural woodwork project or when required for casework with a clear finish.

.1	AWMAC Quality Grade:  [Custom][Premium].

.2	Construction:  to AWMAC Manual for flush overlay, except as otherwise detailed on drawings.

SPEC NOTE:  Ensure drawing details are coordinated with AWMAC Manual.

.3	Edge Banding:  wood, mitred, [as detailed on drawings] [no. 1 grade material to match face veneer, 8 mm thickness].

.4	Exposed and Semi-exposed Parts:

.1	Panel Products:

.1	Plywood Species: [[Red] [White] [Oak]] [[Red] [White] [Natural] [Ash] [Birch] [Maple]] [Walnut] [Cherry].

.2	Core:  [veneer] [multi-core] [or] [particle board]. Use only particle board core for doors and drawer fronts.

.3	Veneer Grade:  [AA] [A].

.4	Veneer Cut:  [rotary-cut] [plain or flat sliced] [quarter sliced] [half-round sliced] [rift-cut].

.5	Veneer Match:  [book] [slip] [and sequence matched].

SPEC NOTE: Only veneer grade AA is sequence matched, refer to grading rules for specific properties. Veneer grade AA is mandatory for Premium grade casework but optional for Custom grade. Verify availability before specifying veneer cut in veneer species specified.

.2	Hardwood Lumber:

.1	Species:  [material matching panel product veneer] [         ].

.2	Grade: no. 1.

.3	Grain:  [mixed] [edge].

SPEC NOTE: Specify stain colour required or that will best represent the anticipated colour to enable Contractors to bid on equivalent finishes.

.6	Finish: [Semi-]Transparent stain, [[        ] colour] [three] colours] followed by] clear finish. [Refer to Architectural Woodwork Schedule for colours and locations.]

2.7	CASEWORK, OPAQUE FINISH [, TYPE [ ]]

.1	AWMAC Quality Grade:  Custom.

.2	Construction:  to AWMAC Manual for flush overlay, except as otherwise detailed on drawings.

SPEC NOTE:  Ensure drawing details are coordinated with AWMAC Manual.

.3	Edge Banding:  wood, [as detailed on drawings,] [no. 1 grade material to match face veneer, [3] [6] mm thickness].

.4	Exposed and Semi-exposed Parts:

.1	Panel Products:  [Birch] [Maple] plywood with [multicore] [veneer core] [particle board core], G2S . Use only particle board core for doors and drawer fronts.

.2	Lumber:  [Birch] [Maple], no. 1 grade.

2.8	CASEWORK, HIGH PRESSURE DECORATIVE LAMINATE (HDPL) FINISH [, TYPE [ ]]

SPEC NOTE:  Specify high pressure decorative laminate finish for exposed surfaces required to be resistant to moderate impact, hygienic, subject to intermittent exposure to moisture, or located in buildings with high interior humidity, e.g., computer centres, museums, hospitals, and buildings containing swimming pools.

SPEC NOTE: Specify Custom grade for most conventional architectural woodwork. Specify Premium grade when the highest degree of workmanship is required for special projects or feature areas within an otherwise conventional architectural woodwork project.

.1	AWMAC Quality Grade:  [Custom] [Premium].

.2	Construction:  to AWMAC Manual for flush overlay, except as otherwise detailed on drawings.

SPEC NOTE:  Ensure drawing details are coordinated with AWMAC Manual.

.3	Exposed and Semi-exposed Parts:

.1	Panel Products:

.1	Core: hardwood species, shop sanded exterior grade veneer core plywood, G2S, or industrial grade particleboard. Use only particle board core for doors and drawer fronts.

.2	High Pressure Decorative Laminate (HPDL):

.1	Horizontal General Purpose Grade (HGS): thickness of 1.2 mm ±0.12 mm, used on the following:

.1	Horizontal surfaces, unless specified otherwise.

.2	Edges of core materials.

.2	Vertical General Purpose Grade (VGS): thickness of 0.7 mm ±0.10 mm, used on the following:

.1	Vertical surfaces, unless specified otherwise.

.2	Exposed portions of case bodies, including ends, divisions and bottoms.

.3	Exposed shelves.

.4	Casework Doors: exposed and semi-exposed surfaces.

.5	Drawer Faces: exposed and semi-exposed surfaces.

.3	Liner Grade (CLS): thickness of 0.5 mm ±0.10 mm, used on the following:

.1	Semi-exposed shelves.

.2	Interior portions of case bodies.

.3	All surfaces of drawer boxes.

.4	Laminate backer grade (BKL): thickness of 0.5 mm ±0.10 mm, used on the following:

.1	Concealed surface of casework backs.

.2	Concealed surfaces, unless specified otherwise.

.5	Laminate Finish and Surface: [matte] [gloss] finish, [smooth] [textured] surface. [Describe textured surface.]

SPEC NOTE:  Consult with woodwork manufacturers for availability and suitability of laminate finishes.  Some laminates are not available in general purpose grade, standard duty.

.6	Laminate Colour [and Pattern]:  similar to [                                   ] [as scheduled], [[ ] [colours] [and] [patterns] to be selected by Minister from manufacturer's standard range].

OR

[.6	Acceptable Products: [List a minimum of 3 acceptable products that meet the above specification.]

SPEC NOTE:  If more than one product or colour is required, specify location in Architectural Woodwork Schedule at end of Section. In the absence of a specified laminate product or colour, woodwork manufacturers will furnish base-priced (excluding upcharged) decorative laminates from decorative laminate manufacturer’s standard selections, maximum of four different colors and patterns per project, limited to one per casework elevation.

.2	Lumber:

.1	Species:  [            ].

.2	Grade: no. 1 .

.3	Grain:  [mixed] [edge].

2.9	HIGH PRESSURE DECORATIVE LAMINATE (HDPL) COUNTERTOPS [AND SPLASHBACKS], SELF-EDGE TYPE

.1	Laminate (HDPL):  [horizontal general purpose grade (HGS), thickness of 1.2 mm ±0.12 mm] [vertical general purpose grade (VGS), thickness of 0.7 mm ±0.10 mm] [laboratory grade, general purpose grade] and laminate backer grade (BKL), thickness of 0.5 mm ±0.10 mm.

SPEC NOTE:  Normally specify general purpose grade, standard duty.  Laboratory grade has limited solid colours.

.1	Laminate Finish and Surface: [matte] [gloss] finish, [smooth] [textured] surface. [Describe textured surface.]

SPEC NOTE:  Consult with manufacturers for availability and suitability of laminate finishes.

.2	Laminate Colour [and Pattern]:  [ similar to [       ]] [as scheduled]. [[Number] [colours] [and] [patterns] selected by Minister from manufacturer's standard range].

SPEC NOTE:  If more than one product or colour is required, specify location in Architectural Woodwork Schedule at end of Section. In the absence of a specified laminate product or colour, woodwork manufacturers will furnish base-priced (excluding upcharged) decorative laminates from decorative laminate manufacturer’s standard selections, maximum of four different colors and patterns per project, limited to one per casework elevation.

OR

[.2	Acceptable Products: [List a minimum of 3 acceptable products that meet the above specification.]

.2	Core:  poplar, spruce or birch shop sanded exterior grade veneer core plywood, G2S, minimum 19 mm thickness or industrial grade particleboard, minimum 29 mm thickness.

.3	Backing: HDPL backer applied to underside of countertops and back of splashbacks.

.4	Edge Type:   [HGS high pressure decorative laminate] [lumber, no. 1 grade][, as detailed on drawings].

.5	Splashback:  profile as detailed on drawings.

2.10	HIGH PRESSURE DECORATIVE LAMINATE (HDPL) COUNTERTOPS AND SPLASHBACKS, POST-FORMED TYPE

.1	General:  to AWMAC standard, with integral splashback [100][   ] mm high.

.2	Laminate:  [postforming grade (HGP), thickness of 1.2 mm ±0.12 mm] [postforming and laboratory grade] and laminate backer grade.

SPEC NOTE:  Laboratory grade has typically limited solid colours.

.1	Laminate Finish:   [matte] finish, [smooth] [textured] surface. [Describe textured surface.]

.2	Laminate Colour [and Pattern]:  [       ] [as scheduled] [[  ] [colours] [and] [patterns] selected by Minister from manufacturer's standard range].

SPEC NOTE:  If more than one product or colour is required, specify location in Architectural Woodwork Schedule at end of Section. In the absence of a specified laminate product or colour, woodwork manufacturers will furnish base-priced (excluding upcharged) decorative laminates from decorative laminate manufacturer’s standard selections, maximum of four different colors and patterns per project, limited to one per casework elevation.

OR

[.2	Acceptable Products: [List a minimum of 3 acceptable products that meet the above specification.]

.3	Core:  particleboard, minimum 29 mm thick.

.4	Backing: laminate backer applied to underside of countertops and backs of splashbacks.

.5	Edges: [full wrap] [non-drip] type.

2.11	FLUSH PANELLING, [stain with] clear finish

.1	AWMAC Quality Grade:  [Custom] [Premium].

SPEC NOTE: Specify Custom grade for most conventional flush panelling. Specify Premium grade when the highest degree of workmanship is required for special projects and feature areas within an otherwise conventional architectural woodwork project.

.2	Plywood:  [  ] mm thick, to AWMAC Manual, [multicore] [particle board core].

.3	Veneer Species:  [             ].

.4	Veneer Grade:  [AA] [A].

SPEC NOTE: Only veneer grade AA is sequence matched, refer to grading rules for specific properties. Veneer grade AA is mandatory for Premium grade casework but optional for Custom grade. Verify availability before specifying veneer cut in veneer species specified.

.5	Veneer Cut:  [rotary] [plain or flat sliced] [quarter sliced] [rift cut].

SPEC NOTE:  Include remainder of this article only if premium grade is specified.  Consult with AWMAC members on availability.

.6	Matching of Adjacent Pieces of Veneer:  [bookmatch] [slipmatch] [random match].

.7	Panel Face Assembly: [book match] [slip centre book] [box match] [diamond match] [  ].

.8	Matching of Adjacent Panels:  [full width sets] [selectively reduced in width sets] [sequence matched uniform size sets] [blueprint matched panels and components].

.9	Veneer Selection:  Minister will select Veneer from flitch samples.

2.12	STILE AND RAIL PANELLING, [stain with] CLEAR FINISH

.1	AWMAC Quality Grade:  Premium.

.2	Panel Products:

.1	Veneer Species:  [              ].

.2	Veneer Grade:  AA.

.3	Veneer Cut:  [rotary] [plain or flat sliced] [quarter sliced] [rift cut].

.4	Veneer Match:   running matched.

.5	Panel Type: [beveled] [raised] [flat].

.6	Panel Match:  maintain grain continuity by horizontal and vertical sequence matching.

SPEC NOTE:  If stile and rail panelled doors, specified in another Section, are located in stile and rail panelled walls, coordinate the specifying of veneer appearance requirements in both Sections to match door appearance with panelling.

SPEC NOTE:  Verify availability and matching of veneers.  It is difficult to achieve colour and grain match of veneer with lumber.

.3	Lumber:

.1	Species:  to match panel products.

.2	Grade:  no.1, compatible in grain and colour with veneer panel products.

.3	Grain direction shall be the long direction of components.

.4	Mouldings:  [solid] [applied] [,as detailed].

.5	Fabrication:

.1	Top, cross and bottom rails shall run between stiles.

.2	Mitre mouldings.

.3	Join stiles, rails and mullions using mortise and tenon, or dowels, and glue under pressure to produce hairline joints.

.4	Raised Veneered Panel Rim:  mitred, splined or doweled, and glued.

.5	Conceal panel product cores as detailed on drawings.

SPEC NOTE:  Ensure core concealment is detailed on drawings.

2.13	[TRIM] [AND] [HANDRAILS], [stain with] CLEAR FINISH

SPEC NOTE:  If both solid and veneered material is specified, ensure locations are indicated on the Architectural Woodwork Schedule or on drawings.

.1	AWMAC Quality Grade:  Premium.

.2	Lumber:

.1	Species:  [               ], no.1 grade.

.2	Grain:  [mixed] [edge].

SPEC NOTE:  Edge grain may be substantially greater in cost or unavailable in species specified.

.3	Panel Products:

.1	Species:  [               ] plywood, G1S.

.2	Veneer Grade:   AA.

.3	Veneer Cut:  [rotary] [plain or flat sliced] [quarter sliced] [half-round sliced] [rift-cut].

.4	Core: [multi-core] [particle board core].

.4	Edge Banding:  [as detailed on drawings] [no.1 grade material to match face veneer,[3] [6] mm thickness].

.5	Provide continuity and compatibility of grain and colour.

2.14	[TRIM] [AND] [HANDRAILS], OPAQUE FINISH

.1	AWMAC Quality Grade:  Custom.

.2	Lumber:  [Birch] [Maple], no.1 grade.

.3	Panel Products:

.1	Species:  [Birch] [Maple] plywood, G1S.

.2	Veneer Grade:   [B].

.3	Core: [multicore] [particle board] core.

.4	Edge Banding:  [as detailed on drawings] [no.1 grade material to match face veneer, [3] [6] mm thickness].

2.15		fabrication

.1	Details for casework shall conform to flush overlay design.

.2	Set nails and countersink screw, apply plain wood filler to indentations, sand smooth and leave ready to receive finish.

.3	Shop install cabinet hardware.

.4	Use draw bolts in countertops and casework joints.

.5	Provide hairline joints in architectural woodwork.

.6	Fabricate work for delivery to site in sizes easily handled and to ensure passage through building openings.

SPEC NOTE:  Delete following two articles in their entirety if all architectural woodwork is to be site finished.  Clearly identify which portion of the project will be factory finished (e.g.: casework and countertops) and site finished (e.g.: handrails, trim, casing, windowsills) after they are fitted on site.

2.16	FACTORY FINISHING MATERIALS

SPEC NOTE:  Verify compatibility of finishes with fire retardant and preservative treated materials.

.1	Factory finishing materials:  Use only products included in Manufacturers' Product List of the Master Painter Institute Architectural Specification Manual, latest edition.

.2	Backprimers:  white alkyd enamel primer or gloss varnish thinned 25%, compatible with exposed finish, as applicable.

.3	Do not use combination filler/stain.

2.17	FACTORY FINISHING

SPEC NOTE:  Clarify what items are to be factory finished by including the finishing location in the Architectural Woodwork Schedule.

.1	Comply with applicable requirements and recommendations for factory finishing in AWMAC Manual.

.2	Refer to Architectural Woodwork Schedule at end of this Section for factory finishing requirements.

.3	Applied and cured coatings shall be uniform in thickness, sheen, colour and texture, and free of defects detrimental to appearance or performance.

.4	Backprime the following surfaces that will be concealed after installation:

.1	Surfaces in contact with concrete, masonry, floors or floor finishes.

.2	Underside of front edges of countertops and toe-spaces.

.3	Other surfaces that may be subjected to moisture during normal use or cleaning operations.

.5	Use two coats white alkyd wood primer to back prime components receiving opaque finishes.

.6	Use gloss varnish, clear urethane or clear lacquer to back prime components receiving clear finishes.

3.	Execution

3.1	VERIFICATION OF CONDITIONS

.1	Verify job site conditions in accordance with AWMAC Manual.

.2	Verify humidity and temperature conditions are stable and as recommended in AWMAC Manual.

.3	Do not deliver to site until job site conditions comply with the requirements outlined in the AWMAC Manual.

3.2	INSTALLATION

.1	Install items in accordance with AWMAC Manual.

.2	Position items accurately, secure and rigid.

.3	Scribe and cut as required to fit neatly to abutting walls and recesses and to projecting, intersecting or penetrating objects.

.4	Apply smallest practicable bead of silicone sealant at junction of splashbacks and adjacent wall finish.

.5 	Provide cutouts for plumbing fixtures, inserts, appliances, outlet boxes and other fixtures.

.6	Back prime surfaces of cut-outs for sinks, drains and other mechanical services that will be concealed after installation.

3.3	ARCHITECTURAL WOODWORK SCHEDULE

SPEC NOTE:  The intent of this schedule is to provide a summary listing of all components included within the scope of this Section, by location.  Refer to Sample Schedule on Data Sheets for an example of a properly edited schedule; follow its format.

SPEC NOTE:  Use this schedule also to specify variables within components in Part 2, e.g. factory finishing, sheen, colour, plastic laminate finishes, hardware packages, etc.  Paint finishes are normally specified in Section 09901.  Clearly identify which portion of the project will be factory finished (e.g.: casework and countertops) and site finished (e.g.: handrails, trim, casings, windowsills) after they are fitted on site.

SPEC NOTE:  Additional variables may occur among subcomponents.  For example, wall cabinets and base cabinets may be of different plastic laminate colours within the same Casework Type. For such situations, consider introducing cabinet types as first level indent headings below Casework Types.

| Location/Components | Finish and Surface Texture | [Gloss Level] | [Colour and Pattern] | Finished at |
| --- | --- | --- | --- | --- |
| [ ] |  |  |  |  |
| [ ] | [ ] | [ ] | [ ] | [Factory] [Site] |

END OF SECTION