Section Cover Page

Section 09331 2000-04-14 Quarry Tile Flooring

This Master Specification Section contains:

.1	This Cover Sheet

.2	Specification Section Text:

1.	General

1.1	Related Work in Other sections

1.2	Quality Standard

1.3	Samples

1.4	Shop Drawings

1.5	Handling and Storage of Materials

1.6	Job Environment

2.	Products

2.1	Materials

2.2	Mortar Mixes

3.	Execution

3.1	Workmanship

3.2	Setting Systems

Applicable Standards:

.1	ANSI A118.1-1992	Specifications for Dry-Set Portland Cement Mortar (Included in ANSI A108.1)

.2	CGSB 71-GP-29M	Adhesive, Elastomeric, for Installation of Quarry Tiles

.3	CAN/CGSB-75.1-M88	Tile, Ceramic

.4	CAN/CSA-A5-93 	Portland Cement

.5	CSA A23.1-94	Concrete Materials and Methods of Concrete Construction

These reference documents may be available for reference purposes in the Technical Resources and Standards Branch Library, Alberta Infrastructure, 3rd Floor, 6950 - 113 Street, Edmonton; Telephone: (780) 427-7924.

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	Application of sealants:	Section 07920.

.2	Ceramic tile:	Section 09310.

1.2	QUALITY STANDARD

.1	Do tile work in accordance with Installation Manual 200, "Ceramic Tile", produced by Terrazzo Tile and Marble Association of Canada (TTMAC), except where specified otherwise.

1.3	SAMPLES

.1	Submit duplicate 600 x 600 mm sample panels of each colour, texture, size and pattern of tile required for this project.

.2	Adhere tile samples to 12 mm thick plywood and grout joints to represent project installation.

.3	Obtain approval of each tile sample prior to supplying material to project.

1.4	SHOP DRAWINGS

SPEC NOTE:  Normally the following clause is only required for projects involving special features.

.1	Submit shop drawings of quarry tile work in accordance with Division 1.

.2	Clearly show layout, [pattern] and relationship of tile joints to fixed accessories and project-formed details.

1.5	HANDLING AND STORAGE OF MATERIALS

.1	Deliver packaged materials in original unopened containers.

.2	Keep delivered material dry and free from stains.  Store cementitious material off damp surfaces.

1.6	JOB ENVIRONMENT

.1	Maintain minimum 13°C air temperature at tile installation area for 24 hours prior to, during and after installation.

2.	Products

2.1	MATERIALS

.1	Quarry Tile:  to CAN/CGSB-75.1-M88, Type 4, Class MR2, plain face, [square] [cushion] edges except where exposed where edges must be bullnosed, size, [        ], colour will be selected by Minister.

.2	Glazed Quarry tile:  to CAN/CGSB-75.1-M88, Type 4, Class MR2, face glazed incorporating non-slip silica granules within the glaze, cushioned edges on all 4 sides, size [      ], colour will be selected by Minister.

.3	Quarry Tile Base:  to match tile specified above, [     ] high, [square] [coved] [bullnosed].

.4	Glazed Tile Base:  to match tile specified above, [     ] high with square top edge.

.5	Cement:  [grey] [white] to CAN/CSA-A5-93.

.6	Sand:  to CSA A23.1-94.

.7	Water:  potable.

.8	Dry-Set Mortar:  to ANSI A118.1-92.

.9	Elastomeric Adhesive:  to CGSB 71-GP-29M.

.10	Portland Cement Grout:  mixture of Portland Cement and fine graded silica sand.

.11	Limited Acid Resistant Grout:  modified Portland Cement compound with additives for corrosion resistance to mild acid and alkali attack; non-rusting, non-dusting non-shrinking, nontoxic and odorless, no epoxy ingredient.  Colour will be selected by Minister.

SPEC NOTE:  Specify limited acid resistant grout in places where mild acid and alkali corrosive conditions exist.

.12	Epoxy Grout and Mortar:  100% solids epoxy composed of 2 part thermosetting epoxy and graded silica sand, chemical resistant.  Colour will be selected by Minister.

SPEC NOTE:  Specify epoxy grout only in places where extreme acid, chemical and similar corrosive conditions exist.  This material is highly toxic and its use requires special health safety precautions to be taken.  Refer to "Occupational Hygiene Recommended Guidelines for Use of Epoxy Resin Compounds in Tile Setting and Grouting" published by Occupational Health and Safety Division.

2.2	MORTAR MIXES

SPEC NOTE:  2.2.1 to 2.2.5 apply only to cement mortar setting.  Select the "coats" and "beds" to correspond with those used in the appropriate TTMAC details specified in 3.2

.1	Mortar bed:  1 part cement, 1/5 to 1/2 parts lime to suit job conditions, 4 parts sand, 1 part water.  Water volume may be adjusted depending on water content of sand.

.2	Slurry coat:  cement and water mixed to creamy paste.  Latex additive may be included.

.3	Levelling coat:  1 part cement, 4 parts sand, minimum 1/10 part latex additive, 1 part water, including latex additive.

.4	Bond or setting coat:  1 part cement, 1/3 parts lime, 1 part water.

.5	Measure mortar ingredients by volume.

.6	[[Dry set] [Elastomeric] adhesive], [Limited acid resistant grout] [Epoxy grout]:  mix to manufacturer's instructions.

SPEC NOTE:  Delete adhesives if not required by TTMAC details specified in paragraph 3.2.

3.	Execution

3.1	WORKMANSHIP

.1	Apply tile, mortar bed, or bond coat to non-frozen frost free surfaces.

.2	Fit tile units around corners, fitments, fixtures, drains and other built-in objects to maintain uniform joint appearance.  Make cut edges smooth, even and free from chipping.

.3	Make joints between tiles uniform and approximately 6 mm wide, plumb, straight, true, even and with adjacent tile flush.

.4	Align patterns.

.5	Lay out tiles so that perimeter tiles are minimum 1/2 size.

.6	Sound tiles after setting and replace hollow sounding units to obtain full bond.

.7	Make internal angles square, external angles bullnosed.

.8	Clean installed tile surfaces after installation cured.

.9	Maintain building expansion joints.  Keep free of mortar or grout.

3.2	SETTING SYSTEMS

.1	Install tile [and bases] on substrates to TTMAC details No. [200-16] [200-16A] [200-16B] [200-17] [200-17A] [200-18] [200-19] [200-19A] [200-19B] [200-19C].

.2	Install quarry tile treads to TTMAC details Nos. [200-26] [200-26A] [200-26B] [200-26C] [200-26D] [200-26E].

.3	Install quarry tile on mortar bed over insulation in refrigeration rooms to TTMAC details Nos. [200-28] [200-28A].

END OF SECTION