Section Cover Page

Section 09671 2000-04-14 Epoxy Flooring

This Master Specification Section contains:

.1	This Cover Sheet

.2	Specification Section Text:

1.	General

1.1	Related Work Specified in Other Sections

1.2	Product Options and Substitutions

1.3	Qualifications

1.4	Samples

1.5	Manufacturer's Literature

1.6	Delivery

1.7	Environmental Conditions

1.8	Protection

2.	Products

2.1	Materials

2.2	Colours

3.	Execution

3.1	Examination

3.2	Preparation/Application

3.3	Cleaning

3.4	Application Schedule

Applicable Standards

.1	ASTM C126-96	Ceramic Glazed Structural Clay Facing Tile, Facing Brick, and Solid Masonry Units

.2	ASTM D570-95	Water Absorption of Plastics

.3	ASTM D638-M96	Tensile Properties of Plastics

.4	ASTM D696-91	Coefficient of Linear Thermal Expansion of Plastics Between -30oC and 30oC

.5	ASTM D905-94	Strength Properties of Adhesive Bonds in Shear by Compression Loading

.6	ASTM D1044-94	Resistance of Transparent Plastic to Surface Abrasion

.7	ASTM D1308-87(1993)el	Effect of Household Chemicals on Clear and Pigmented Organic Finishes

.8	ASTM D2337-84(R1996)el	Freeze-Thaw Stability of Multicolor Lacquers

.9	ASTM E84a-96a	Surface Burning Characteristics of Building Materials

.10	CGSB 1-GP-71	Methods of Testing Paints and Pigments

These reference documents may be available for reference purposes in the Technical Resources and Standards Branch Library, Alberta Infrastructure, 3rd Floor, 6950 - 113 Street, Edmonton; Telephone: (780) 427-7924.

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	[Substrate]:	Section [   ].

.2	Sealants:	Section 07920.

.3	Painting:	Section 09901.

.4	Epoxy wall coatings:	Section 09961.

.5	Vinyl-acrylic coating:	Section 09962.

1.2	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 1 for requirements pertaining to product options and substitutions.

1.3	QUALIFICATIONS

.1	The work of this Section shall be applied only by experienced applicators of the specified products.

1.4	SAMPLES

.1	Submit 300 mm x 300 mm representative sample of flooring in selected colour.  Identify sample by project name including material and colour identification.

.2	Site apply sample installation to minimum 2 m2 area, to surface as directed, for approval by the Minister.  Retain approved sample until work is completed and accepted.

1.5	MANUFACTURER'S LITERATURE

.1	Make available copies of the material literature, clearly indicating conditions of acceptance for surfaces and methods of application on site before, and during, period of application of the work of this Section.

1.6	DELIVERY

.1	Deliver materials undamaged, in original containers, with manufacturer's labels and seals intact.

1.7	ENVIRONMENTAL CONDITIONS

.1	For exterior coatings:  Comply with coating manufacturer's recommendations.  Do not apply under adverse weather conditions which could affect coating performance.

.2	For interior coatings:  Ensure minimum surface temperature 10°C 24 hours before, during and 24 hours after application or until cured; adequate controlled ventilation; bright, uniform lighting; broom clean; reasonably dust free.

1.8	PROTECTION

.1	Protect adjacent surfaces from damage or overspray resulting from work of this Section.  Mask and/or cover adjacent surfaces.  Make good any damage at own expense, to the Minister's satisfaction.

.2	Post "Wet Coatings" and "No Smoking" signs, while work is in progress and curing.

2.	Products

2.1	MATERIALS

.1	Thermo-setting 100% epoxy coating with matrix, coloured filler and top coat meeting the following requirements:

| Property | Test Method | Requirement |
| --- | --- | --- |
| Abrasion resistance | ASTM D1044-94 10 000 cycles using CS17 wheels with 1 kg load | 0.04 g loss max |
| Bond strength | After 7 days water immersion ACI Committee 403 Bulletin 5943 | 2275 kPa to concrete |
| Colour fastness | CGSB 1-GP-71, Method 120.1 Fade-ometer | 11.0 NBS units |
| Flammability | ASTM E84-96a 1.3 mm max. Self extinguishing | Extent of burning |
| Impact resistance | CGSB 1-GP-71 Method 147.1 Gardner Impact Test 17 J | No cracking, chipping or delamination |
| Resistance to acid hydroxides, salts & cleaning agents | ASTM D1308-87(1993) | Unaffected by common household cleaning agents, hydroxides and salts |
| Tensile strength | ASTM D638-M96 | 7 MPa7 MPa |
| Toxicity | Can. Dept. of Agriculture | Approved non-toxic |
| Water absorption | ASTM D570-95 24 hour immersion | 0.45% max. |

SPEC NOTE:  The above material is for non-bearing industrial use.  The following materials meet the above requirements:  Quartzite 2000 by Macnaughton-Brooks Products Ltd., Duroquartz by Duron Col Ltd., Chemford 800 by H.L. Blachford Ltd., Ceramite by Everguard-Hallmark, Decor-Flor distributed by Heffernan Floor and Wall Products Ltd.

.2	Epoxy aggregate flooring, thermo-setting, 100% solids, and meeting following requirements:

| Property | Test Method | Requirement |
| --- | --- | --- |
| Abrasion resistance | ASTM D1044-94 CS 17 wheels with 2 kg load 5 000 cycles | 0.3 g |
| Coefficient of linear expansion | ASTM D696-91 | 165.6 x 107/°C |
| Flammability | ASTM E84-96a | Non-burning |
| Freeze-thaw resistance | ASTM D2337-84 (R1996) | Unaffected |
| Hardness | Barcol | 55 |
| Impact resistance | Falling ball method, 50.8 mm in diameter weighing 535 g Gardner Impact Tester (Masonry Backing) | Energy required to cause failure: 12.9 J 9 J: no loss of adhesion |
| Resistance to burning cigarette |  | Very slight discoloration |
| Resistance to cleaning agents, hydroxides and salts | ASTM D1308-87(1993) | Unaffected by common household cleaning agents, hydroxides and salts |
| Shear bond strength | ASTM D905-94 | 2 MPa to concrete |
| Surface stain | ASTM C126-96 | Unaffected |
| Tensile strength (binder only) | ASTM D638-M96 | 23 MPa |
| Toxicity | Can. Dept. of Agriculture | Approved non-toxic |
| Washability | Gardner straight line method 5000 cycles | No visual effect |
| Water absorption | ASTM D570-95 | 0.2% by mass |

SPEC NOTE:  The above material is for heavy industrial use:  the following materials meet the above requirements:  Resolast by Duron Co. Ltd., Chemiford 200 by H.L. Blachford Ltd., Romalast by Everguard-Hallmark, Morritex by Macnaughton-Brooks Products Ltd.

2.2	COLOURS

.1	[One] [Two] [          ] colour[s] will be selected by Minister from manufacturer's standard range.

OR

.1	Refer to Application Schedule.

3.	Execution

3.1	EXAMINATION

.1	Examine all surface conditions to which the work of this Section is to be applied.  Report unacceptable surfaces to the Minister.

3.2	PREPARATION/APPLICATION

.1	Prepare surfaces and apply as directed in the manufacturer's literature.

.2	Match finished work to approved samples.  Maintain uniform thickness, sheen, colour, texture and free from defects detrimental to appearance of performance.

.3	Cured thickness of applied material:  3 mm.

3.3	CLEANING

.1	Promptly, as the work proceeds and upon completion, clean up excess materials and rubbish.

3.4	APPLICATION SCHEDULE

| Room No./Name | Material | Finish | [Colour] | [Top Coat Thickness] |
| --- | --- | --- | --- | --- |
| [ ] | [Epoxy Matrix] [Epoxy Aggregate] | [Non-slip] [Satin] [Gloss] | [ ] | [300] [600] micrometres |
| [ ] | [ ] | [ ] | [ ] | [ ] |
| All other locations scheduled to receive epoxy flooring | [ ] | [ ] | [ ] | [ ] |

SPEC NOTE:  Top coat thickness only applies to epoxy matrix flooring.  Specify a non-slip finish in Storage Areas and Maintenance Rooms.

SPEC NOTE:  Coordinate above schedule with Room Finish Schedule and with Colour Schedule if a Colour Schedule will be included in Bid Documents.

# END OF SECTION