Section Cover Page

Section 09902 Exterior Painting and 2001-08-28 Finishing Schedule

Use this Section to schedule finishing systems for all new, exterior substrates requiring site painting and finishing, except mechanical and electrical work.

The Alberta Infrastructure Basic Master Specification contains the following series of Sections that specify site painting and finishing:

.1	Section 09901 - Painting and Finishing General Requirements

.2	Section 09902 - Exterior Painting and Finishing Schedule (this Section)

.3	Section 09903 - Exterior Repainting and Refinishing Schedule

.4	Section 09904 - Interior Painting and Finishing Schedule

.5	Section 09905 - Interior Repainting and Refinishing Schedule

.6	Section 09906 - Painting of Mechanical and Electrical Work

These sections are interrelated.  Section 09901 specifies general requirements while the remaining Sections in the series specify finish systems, i.e. specific products and number of coats, required for various types of substrates.  Always include Section 09901.  Include one or more of the remaining Sections only to the extent they are applicable to the project.

This Master Specification Section contains:

.1	This Cover Sheet

.2	Data Sheet - General

.3	Specification Section Text:

- 1.	General

1.1	Intent

- 2.	Products

(Not used)

- 3.	Execution

3.1	Exterior Painting and Finishing Schedule

This Section includes a comprehensive listing of various new, exterior, substrates complete with MPI code numbers, finishing system descriptions and product descriptions.

Individual finishing systems listed in this master schedule must be edited to suit the project. Note that the schedule generally calls for 3 coats (premium grade), which is the normal standard for Alberta Infrastructure projects.  If 2 coats (custom grade) are deemed to be adequate for a particular project, the schedule needs to be edited accordingly.

Specifier has the option of scheduling site painting and finishing by one of two methods:

.1	Method #1:  Indicate on drawings, on exterior finish schedule, or elsewhere as appropriate, the proper code designation and where applicable, gloss level, of the required finish system for each item or substrate that requires site finishing.  In this Section, specify the finish system corresponding to each required finish.  Coordinate with drawings, exterior finish schedule, etc.

.2	Method #2:  Incorporate a comprehensive listing of each item or substrate that requires site finishing into this Section.  Do not indicate code designations elsewhere.  Since this Section describes substrate elements in general terms only, mainly for reference purposes, it may require modification and expansion to include more specific and detailed substrate descriptions.

Carefully consider all surfaces to be painted or finished and ensure that appropriate finishing systems are specified for each surface type. Review the system evaluation and surface preparation sections of the MPI Manual when selecting finishing systems.

Specify only those finishing systems that are applicable to the project. Delete all other finishing systems.

- END OF DATA SHEET

- 1.	General

- 1.1	INTENT

.1	Read this Section in conjunction with Section 09901 - Painting and Finishing General Requirements.

- 2.	Products

.1	(Not used).

- 3.	Execution

- 3.1	EXTERIOR PAINTING AND FINISHING SCHEDULE

.1	The following code numbers, finishing system descriptions, gloss levels, coats and product descriptions are derived from the MPI Architectural Painting Specification Manual and the MPI Approved Products List.

SPEC NOTE: Delete finishing systems as required to include only systems required for the project. Edit all option fields.  Where more than one Gloss Level is required for a particular substrate, include all applicable gloss levels and ensure location of various gloss levels are clearly defined in Section 09901, Article 2.4, Paragraph 2.4.2

- EXT 2.1 – ASPHALT SURFACES

| EXT 2.1A | Latex Zone / Traffic Marking | Latex Zone/Traffic Marking Paint, Apply in strict accordance with manufacturer’s instructions. |
| --- | --- | --- |
| EXT 2.1B | Alkyd Zone / Traffic Marking | Alkyd Zone/Traffic Marking Paint, Apply in strict accordance with manufacturer’s instructions. |

EXT 3.1 – CONCRETE VERTICAL SURFACES

| EXT 3.1A | Latex | 1st | Latex |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 3.1B | Latex Aggregate / Latex | 1st | Latex Aggregate |
|  | [Coarse] [Medium] texture, | 2nd | Latex |
|  | Gloss level [G1] [G5] [G6] | 3rd | Latex |
| EXT 3.1C | Waterborne Light Industrial Coating | 1st | W. B. Light Industrial Coating |
|  | Gloss level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |
| EXT 3.1D | Epoxy | 1st | Epoxy |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| EXT 3.1E | Epoxy, Water Based | 1st | W. B. Epoxy |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| EXT 3.1F | Elastomeric |  | Elastomeric Coating, Apply in strict accordance with manufacturer’s instructions. |
| EXT 3.1G | Water Repellent |  | Water Repellent, Apply in strict accordance with manufacturer’s instructions. |
|  | (not paintable) |  |  |
| EXT 3.1H | Water Repellent |  | Water Repellent, Apply in strict accordance with manufacturer’s instructions. |
|  | (paintable) |  |  |
| EXT 3.1J | Concrete Stain |  | Concrete Stain, Apply in strict accordance with manufacturer’s instructions. |
| EXT 3.1K | Latex | 1st | Alkali Resistant Primer |
|  | (over alkali resistant primer) | 2nd | Latex |
|  | Gloss level [G1] [G5] [G6] | 3rd | Latex |
| EXT 3.1L | High Build Latex |  | High Build Latex, Apply in strict accordance with manufacturer’s instructions. |
| EXT 3.1M | Polyurethane, Pigmented | 1st | Epoxy |
|  | (over epoxy) | 2nd | Epoxy |
|  |  | 3rd | Polyurethane |
| EXT 3.1N | Latex Aggregate |  | Latex Aggregate, Apply in strict accordance with manufacturer’s instructions. |
|  | [Coarse] [Medium] texture, |  |  |
|  | Gloss level [G1] [G5] [G6] |  |  |

EXT 3.2 – CONCRETE HORIZONTAL SURFACES

| EXT 3.2A | Latex Floor Paint | 1st | Floor Paint |
| --- | --- | --- | --- |
|  | Gloss level [G3] [G6] | 2nd | Floor Paint |
|  |  | 3rd | Floor Paint |
| EXT 3.2B | Latex Deck Coating |  | Latex, Apply in strict accordance with manufacturer’s instructions. |
| EXT 3.2C | Epoxy Non-slip Deck Coating |  | Epoxy, Apply in strict accordance with manufacturer’s instructions. |
| EXT 3.2D | Alkyd Floor Enamel | 1st | Alkyd |
|  | Gloss level [G4] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 3.2E | Latex Zone / Traffic Marking |  | Latex, Apply in strict accordance with manufacturer’s instructions. |
| EXT 3.2F | Alkyd Zone / Traffic Marking |  | Alkyd, Apply in strict accordance with manufacturer’s instructions. |
| EXT 3.2G | Sealer, Clear | 1st | Clear Sealer |
|  |  | 2nd | Clear Sealer |
|  |  | 3rd | Clear Sealer |
| EXT 3.2H | Sealer, Clear, Water Based | 1st | Clear Sealer |
|  |  | 2nd | Clear Sealer |
|  |  | 3rd | Clear Sealer |
| EXT 3.2J | Concrete Stain |  | Concrete Stain, Apply in strict accordance with manufacturer’s instructions. |

EXT 3.3 – CEMENTITIOUS COMPOSITION BOARD

| EXT 3.3A | Latex | 1st | Latex |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 3.3B | Alkyd | 1st | Exterior Latex Primer |
|  | Gloss level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 3.3C | Waterborne Light Industrial Coating | 1st | W. B. Light Industrial Coating |
|  | Gloss level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |
| EXT 3.3D | Epoxy, Water Based | 1st | W. B. Epoxy |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| EXT 3.3E | Epoxy | 1st | Epoxy |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| EXT 3.3F | Polyurethane, Pigmented | 1st | Epoxy |
|  | (over epoxy) | 2nd | Epoxy |
|  |  | 3rd | Polyurethane |
| EXT 3.3G | Latex Aggregate |  | Latex Aggregate, Apply in strict accordance with manufacturer’s instructions. |
|  | [Coarse] [Medium] texture |  |  |
|  | Gloss level [G1] [G5] [G6] |  |  |
| EXT 3.3H | High Build Latex |  | High Build Latex, Apply in strict accordance with manufacturer’s instructions. |
| EXT 3.3J | Latex | 1st | Alkali Resistant Primer |
|  | (over alkali resistant primer) | 2nd | Latex |
|  | Gloss level [G1] [G5] [G6] | 3rd | Latex |

EXT 4.1 – CLAY MASONRY UNITS

| EXT 4.1A | Latex | 1st | Latex |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 4.1B | Latex Aggregate [Coarse] [Medium] texture, Gloss level [G1] [G5] [G6] |  | Latex Aggregate, Apply in strict accordance with manufacturer’s instructions. |
| EXT 4.1C | Waterborne Light Industrial Coating | 1st | W. B. Light Industrial Coating |
|  | Gloss level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |
| EXT 4.1D | Epoxy | 1st | Epoxy |
|  | (for smooth brick) | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| EXT 4.1E | Epoxy, Water Based | 1st | W. B. Epoxy |
|  | (for smooth brick) | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| EXT 4.1F | Water Repellent |  | Water Repellent, Apply in strict accordance with manufacturer’s instructions |
|  | (not paintable) |  |  |
| EXT 4.1G | Water Repellent |  | Water Repellent, Apply in strict accordance with manufacturer’s instructions |
|  | (paintable) |  |  |
| EXT 4.1H | High Build Latex |  | High Build Latex, Apply in strict accordance with manufacturer’s instructions. |
| EXT 4.1J | Polyurethane, Pigmented | 1st | Epoxy |
|  | (over epoxy) | 2nd | Epoxy |
|  |  | 3rd | Polyurethane |

EXT 4.2 – CONCRETE MASONRY UNITS

| EXT 4.2A | Latex | 1st | Block Filler |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 4.2B | Latex Aggregate |  | Latex Aggregate, Apply in strict accordance with manufacturer’s instructions. |
|  | [Coarse] [Medium] texture |  |  |
|  | Gloss level [G1] [G5] [G6] |  |  |
| EXT 4.2C | Waterborne Light Industrial Coating | 1st | Block Filler |
|  | Gloss level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  |  | 3rd | W.B. Light Industrial Coating |
| EXT 4.2D | Elastomeric |  | Elastomeric Coating, Apply in strict accordance with manufacturer’s instructions. |
| EXT 4.2E | Epoxy | 1st | Epoxy Block Filler |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| EXT 4.2F | Epoxy, Water Based | 1st | Epoxy Block Filler |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| EXT 4.2G | Polyurethane, Pigmented | 1st | Epoxy Block Filler |
|  | (over high build epoxy) | 2nd | High Build Epoxy |
|  |  | 3rd | Polyurethane |
| EXT 4.2H | Water Repellent |  | Water Repellent, Apply in strict accordance with manufacturer’s instructions. |
|  | (not paintable) |  |  |
|  | (not for light weight concrete block) |  |  |
| EXT 4.2J | Water Repellent |  | Water Repellent, Apply in strict accordance with manufacturer’s instructions. |
|  | (paintable) |  |  |
|  | (not for light weight concrete block) |  |  |
| EXT 4.2K | High Build Latex |  | High Build Latex, Apply in strict accordance with manufacturer’s instructions. |
| EXT 4.2L | Latex | 1st | Alkali Resistant Primer |
|  | (over alkali resistant primer) | 2nd | Latex |
|  | Gloss level [G1] [G5] [G6] | 3rd | Latex |

EXT 5.1 – STRUCTURAL STEEL & METAL FABRICATIONS

| EXT 5.1A | Quick Dry Enamel | 1st | Quick Dry Primer |
| --- | --- | --- | --- |
|  | Gloss level [G5] [G6] | 2nd | Quick Dry Enamel |
|  |  | 3rd | Quick Dry Enamel |
| EXT 5.1B | Waterborne Light Industrial Coating | 1st | Inorganic Zinc |
|  | (over inorganic zinc) | 2nd | W.B. Light Industrial Coating |
|  | Gloss Level [G3] [G5] [G6] | 3rd | W.B. Light Industrial Coating |
| EXT 5.1C | Waterborne Light Industrial Coating (over alkyd primer) | 1st | Alkyd Metal Primer |
|  |  | 2nd | W.B. Light Industrial Coating |
|  | Gloss Level [G3] [G5] [G6] | 3rd | W.B. Light Industrial Coating |
| EXT 5.1D | Alkyd | 1st | Alkyd Metal Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 5.1E | Epoxy, Water Based | 1st | Rust Inhibitive Primer |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| EXT 5.1F | Epoxy | 1st | Epoxy Primer |
|  |  | 2nd | High Build Epoxy |
|  |  | 3rd | Epoxy |
| EXT 5.1G | Polyurethane, Pigmented | 1st | Epoxy Zinc Rich Primer |
|  | (over epoxy zinc rich primer and high build epoxy) | 2nd | High Build Epoxy |
|  |  | 3rd | Polyurethane |
|  |  | 4th | Polyurethane |
| EXT 5.1H | Polyurethane, Pigmented | 1st | Epoxy Primer |
|  | (over epoxy) | 2nd | Epoxy |
|  |  | 3rd | Polyurethane |
|  |  | 4th | Polyurethane |
| EXT 5.1J | Polyurethane, Pigmented | 1st | Epoxy Primer |
|  | (over high build epoxy) | 2nd | High Build Epoxy |
|  |  | 3rd | Polyurethane |
| EXT 5.1K | Aluminum Paint | 1st | Alkyd Metal Primer |
|  |  | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |
| EXT 5.1L | Polyurethane, Pigmented | 1st | Inorganic Zinc Rich Primer |
|  | (over inorganic zinc rich primer and high build epoxy) | 2nd | High Build Epoxy |
|  |  | 3rd | Polyurethane |
| EXT 5.1M | Waterborne Light Industrial Coating | 1st | Rust Inhibitive Primer |
|  | (over w.b. primer) | 2nd | W.B. Light Industrial Coating |
|  | Gloss Level [G3] [G5] [G6] | 3rd | W.B. Light Industrial Coating |
| EXT 5.1N | Waterborne Light Industrial Coating | 1st | Epoxy Primer |
|  | (over epoxy primer) | 2nd | W.B. Light Industrial Coating |
|  | Gloss Level [G3] [G5] [G6] | 3rd | W.B. Light Industrial Coating |
| EXT 5.1P | Polyurethane, Pigmented | 1st | Epoxy Zinc Rich Primer |
|  | (over epoxy zinc rich primer epoxy) | 2nd | Epoxy |
|  |  | 3rd | Polyurethane |

EXT 5.2 – STEEL – HIGH HEAT

| EXT 5.2A | Heat Resistant Enamel | Heat Resistant Enamel, Apply in strict accordance with Manufacturer’s Instructions |
| --- | --- | --- |
|  | Maximum 205°C (400°F) |  |
| EXT 5.2B | Heat Resistant Enamel, Aluminum | Aluminum Heat Resistant Enamel, Apply in strict accordance with Manufacturer’s Instructions |
|  | Maximum 427°C (800°F) |  |
| EXT 5.2C | Inorganic Zinc Rich Coating | Inorganic Zinc Rich Coating, Apply in strict accordance with Manufacturer’s Instructions |
|  | Maximum 400°C (750°F) |  |
| EXT 5.2D | High Heat Resistant Coating | High Heat Resistant Coating, Apply in strict accordance with Manufacturer’s Instructions |
|  | Maximum 593°C (1100°F) |  |

EXT 5.3 – GALVANIZED METAL

| EXT 5.3A | Latex | 1st | Cementitious Primer |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 5.3B | Alkyd | 1st | Cementitious Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 5.3C | Epoxy | 1st | Epoxy Primer |
|  | (high contact / traffic) | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| EXT 5.3D | Polyurethane, Pigmented | 1st | Vinyl Wash Primer |
|  | (high contact / traffic) | 2nd | Epoxy |
|  |  | 3rd | Polyurethane |
|  |  | 4th | Polyurethane |
| EXT 5.3E | Bituminous | 1st | Bituminous |
|  | (low contact / traffic) | 2nd | Bituminous |
| EXT 5.3F | Aluminum Paint | 1st | Cementitious Primer |
|  | (low contact / traffic) | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |
| EXT 5.3G | Waterborne Light Industrial Coating | 1st | Cementitious Primer |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  |  | 3rd | W.B. Light Industrial Coating |
| EXT 5.3H | Latex | 1st | W. B. Primer |
|  | (over w.b. primer) | 2nd | Latex |
|  | (low contact / traffic) | 3rd | Latex |
|  | Gloss Level [G1] [G5] [G6] |  |  |
| EXT 5.3J | Waterborne Light Industrial Coating | 1st | W. B. Primer |
|  | (over w.b. primer) | 2nd | W.B. Light Industrial Coating |
|  | Gloss Level [G3] [G5] [G6] | 3rd | W.B. Light Industrial Coating |

EXT 5.4 – ALUMINUM (non-anodized)

| EXT 5.4A | Alkyd | 1st | Vinyl Wash Primer |
| --- | --- | --- | --- |
|  | (over vinyl wash primer and q.d. primer) | 2nd | Quick Dry Metal Primer |
|  |  | 3rd | Alkyd |
|  | Gloss Level [G1] [G5] [G6] | 4th | Alkyd |
| EXT 5.4B | Polyurethane, Pigmented | 1st | Vinyl Wash Primer |
|  | (over epoxy) | 2nd | Epoxy |
|  |  | 3rd | Polyurethane |
|  |  | 4th | Polyurethane |
| EXT 5.4C | Aluminum Paint | 1st | Vinyl Wash Primer |
|  |  | 2nd | Quick Dry Metal Primer |
|  |  | 3rd | Aluminum Paint |
|  |  | 4th | Aluminum Paint |
| EXT 5.4D | Bituminous | 1st | Bituminous |
|  |  | 2nd | Bituminous |
|  |  | 3rd | Bituminous |
| EXT 5.4E | Epoxy | 1st | Vinyl Wash Primer |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| EXT 5.4F | Alkyd | 1st | Quick Dry Metal Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 5.4G | Waterborne Light Industrial Coating | 1st | Quick Dry Metal Primer |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  |  | 3rd | W.B. Light Industrial Coating |
| EXT 5.4H | Latex | 1st | Quick Dry Metal Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |

EXT 5.5 – COPPER (excluding roofs)

| EXT 5.5A | Alkyd | 1st | Vinyl Wash Primer |
| --- | --- | --- | --- |
|  | (over vinyl wash primer) | 2nd | Alkyd |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Alkyd |
| EXT 5.5B | Polyurethane, Pigmented | 1st | Vinyl Wash Primer |
|  | (over epoxy) | 2nd | Epoxy |
|  |  | 3rd | Polyurethane |
|  |  | 4th | Polyurethane |
| EXT 5.5C | Aluminum Paint | 1st | Vinyl Wash Primer |
|  |  | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |
| EXT 5.5D | Bituminous | 1st | Bituminous |
|  |  | 2nd | Bituminous |
|  |  | 3rd | Bituminous |
| EXT 5.5E | Epoxy | 1st | Vinyl Wash Primer |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| EXT 5.5F | Alkyd | 1st | Quick Dry Metal Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 5.5G | Waterborne Light Industrial Coating | 1st | Quick Dry Metal Primer |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  |  | 3rd | W.B. Light Industrial Coating |
| EXT 5.5H | Latex | 1st | Quick Dry Metal Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |

EXT 5.6 – STAINLESS STEEL (not polished)

| EXT 5.6A | Alkyd | 1st | Vinyl Wash Primer |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 5.6B | Polyurethane, Pigmented | 1st | Vinyl Wash Primer |
|  | (over epoxy) | 2nd | Epoxy |
|  |  | 3rd | Polyurethane |
|  |  | 4th | Polyurethane |
| EXT 5.6C | Aluminum Paint | 1st | Vinyl Wash Primer |
|  |  | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |
| EXT 5.6D | Epoxy | 1st | Epoxy Primer |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| EXT 5.6E | Epoxy, Water Based | 1st | Epoxy Primer |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| EXT 5.6F | Latex | 1st | Bonding Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 5.6G | Waterborne Light Industrial Coating | 1st | Quick Dry Metal Primer |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  |  | 3rd | W.B. Light Industrial Coating |

EXT 6.1 – GLUE LAMINATED BEAMS AND COLUMNS

| EXT 6.1A | Latex | 1st | Oil/Alkyd Primer |
| --- | --- | --- | --- |
|  | (over alkyd primer) | 2nd | Latex |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Latex |
| EXT 6.1B | Alkyd | 1st | Oil/Alkyd Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 6.1C | Solid Colour Stain | 1st | Oil/Alkyd Primer |
|  |  | 2nd | Solid Colour Stain |
|  |  | 3rd | Solid Colour Stain |
| EXT 6.1D | Varnish | 1st | Semi-transparent Stain |
|  | (over stain) | 2nd | Varnish |
|  | Gloss Level [G5] [G6] | 3rd | Varnish |
|  |  | 4th | Varnish |
| EXT 6.1E | Polyurethane, Clear, 2 Component | 1st | Semi-transparent Stain |
|  | (over stain) | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
|  |  | 4th | Polyurethane |
| EXT 6.1F | Fire Retardant, Pigmented |  | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| EXT 6.1G | Fire Retardant, Penetrating Wood Preservative, Clear |  | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| EXT 6.1H | Polyurethane, Clear, 2 Component | 1st | Polyurethane |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| EXT 6.1J | Polyurethane, Pigmented | 1st | Polyurethane |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| EXT 6.1K | Varnish | 1st | Varnish |
|  | Gloss Level [G5] [G6] | 2nd | Varnish |
|  |  | 3rd | Varnish |
|  |  | 4th | Varnish |
| EXT 6.1L | Latex | 1st | Latex Primer |
|  | (over latex primer) | 2nd | Latex |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Latex |

EXT 6.2 – DIMENSION LUMBER

| EXT 6.2A | Latex | 1st | Oil/Alkyd Primer |
| --- | --- | --- | --- |
|  | (over alkyd primer) | 2nd | Latex |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Latex |
| EXT 6.2B | Solid Colour Stain, Waterborne. | 1st | Oil/Alkyd Primer |
|  |  | 2nd | Latex Stain |
|  |  | 3rd | Latex Stain |
| EXT 6.2C | Alkyd | 1st | Oil/Alkyd Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 6.2D | Solid Colour Stain | 1st | Oil/Alkyd Primer |
|  |  | 2nd | Solid Colour Stain |
|  |  | 3rd | Solid Colour Stain |
| EXT 6.2E | Varnish | 1st | Wood Stain |
|  | (over stain) | 2nd | Varnish |
|  | Gloss Level [G5] [G6] | 3rd | Varnish |
|  |  | 4th | Varnish |
| EXT 6.2F | Fire Retardant, Pigmented |  | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| EXT 6.2G | Fire Retardant, Penetrating Wood Preservative, Clear |  | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| EXT 6.2H | Polyurethane, Clear, 2 Component | 1st | Polyurethane |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| EXT 6.2J | Polyurethane, Pigmented | 1st | Polyurethane |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| EXT 6.2K | Varnish | 1st | Varnish |
|  | Gloss Level [G5] [G6] | 2nd | Varnish |
|  |  | 3rd | Varnish |
|  |  | 4th | Varnish |
| EXT 6.2L | Semi-transparent Stain | 1st | Semi-transparent Stain |
|  |  | 2nd | Semi-transparent Stain |
| EXT 6.2M | Latex | 1st | Latex Primer |
|  | (over latex primer) | 2nd | Latex |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Latex |

EXT 6.3 – DRESSED LUMBER

| EXT 6.3A | Latex | 1st | Oil/Alkyd Primer |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Latex |
|  | (do not use G1 on doors) | 3rd | Latex |
| EXT 6.3B | Alkyd | 1st | Oil/Alkyd Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  | (do not use G1 on doors) | 3rd | Alkyd |
| EXT 6.3C | Solid Colour Stain | 1st | Oil/Alkyd Primer |
|  | (not for high contact or doors) | 2nd | Solid Colour Stain |
|  |  | 3rd | Solid Colour Stain |
| EXT 6.3D | Semi-transparent Stain | 1st | Wood Stain |
|  | (not for use on doors) | 2nd | Wood Stain |
| EXT 6.3E | Varnish | 1st | Wood Stain |
|  | (over stain) | 2nd | Varnish |
|  | Gloss Level [G5] [G6] | 3rd | Varnish |
|  |  | 4th | Varnish |
| EXT 6.3F | Varnish | 1st | Varnish |
|  | Gloss Level [G5] [G6] | 2nd | Varnish |
|  |  | 3rd | Varnish |
|  |  | 4th | Varnish |
| EXT 6.3G | Polyurethane, Clear, 2 Component | 1st | Polyurethane |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| EXT 6.3H | Polyurethane, Pigmented | 1st | Polyurethane |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| EXT 6.3J | Waterborne Light Industrial Coating | 1st | Oil/Alkyd Primer |
|  | Gloss Level [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  | (doors and frames only) | 3rd | W. B. Light Industrial Coating |
| EXT 6.3K | Solid Colour Stain, Waterborne | 1st | Oil/Alkyd Primer |
|  | (do not use on doors) | 2nd | Latex Stain |
|  |  | 3rd | Latex Stain |
| EXT 6.3L | Latex | 1st | Latex Primer |
|  | (over latex primer) | 2nd | Latex |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Latex |
|  | (do not use G1 on doors) |  |  |

EXT 6.4 – WOOD PANELING

| EXT 6.4A | Solid Colour Stain, Waterborne | 1st | Primer |
| --- | --- | --- | --- |
|  |  | 2nd | Latex Stain |
|  |  | 3rd | Latex Stain |
| EXT 6.4B | Alkyd | 1st | Oil/Alkyd Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 6.4C | Solid Colour Stain | 1st | Oil/Alkyd Primer |
|  |  | 2nd | Solid Colour Stain |
|  |  | 3rd | Solid Colour Stain |
| EXT 6.4D | Semi-transparent Stain | 1st | Wood Stain |
|  |  | 2nd | Wood Stain |
| EXT 6.4E | Fire Retardant, Pigmented |  | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| EXT 6.4F | Fire Retardant, Penetrating Wood Preservative, Clear |  | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| EXT 6.4G | Latex | 1st | Oil/Alkyd Primer |
|  | (over alkyd primer) | 2nd | Latex |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Latex |
| EXT 6.4H | Varnish | 1st | Varnish |
|  | Gloss Level [G5] [G6] | 2nd | Varnish |
|  |  | 3rd | Varnish |
|  |  | 4th | Varnish |
| EXT 6.4J | Varnish | 1st | Wood Stain |
|  | (over stain) | 2nd | Varnish |
|  | Gloss Level [G5] [G6] | 3rd | Varnish |
|  |  | 4th | Varnish |
| EXT 6.4K | Latex | 1st | Latex Primer |
|  | (over latex primer) | 2nd | Latex |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Latex |

EXT 6.5 – WOOD DECKS AND STAIRS/STEPS

| EXT 6.5A | Latex Porch & Floor | 1st | Alkyd Primer |
| --- | --- | --- | --- |
|  | (over alkyd primer) | 2nd | Latex Porch & Floor |
|  | Gloss level [G3] [G6] | 3rd | Latex Porch & Floor |
| EXT 6.5B | Alkyd Floor Enamel | 1st | Alkyd Floor Enamel |
|  | Gloss level [G4] [G6] | 2nd | Alkyd Floor Enamel |
|  | [Anti-skid Additive] | 3rd | Alkyd Floor Enamel |
| EXT 6.5C | Alkyd Floor Enamel | 1st | Wood Preservative |
|  | (over wood preservative) | 2nd | Alkyd Floor Enamel |
|  | Gloss level [G4] [G6] | 3rd | Alkyd Floor Enamel |
|  | [Anti-skid Additive] | 4th | Alkyd Floor Enamel |
| EXT 6.5D | Deck Stain | 1st | Wood Preservative |
|  | (over wood preservative) | 2nd | Deck Stain |
|  |  | 3rd | Deck Stain |
| EXT 6.5E | Latex Porch & Floor | 1st | Latex Wood Primer |
|  | (over latex primer) | 2nd | Latex Porch & Floor |
|  | Gloss level [G3] [G6] | 3rd | Latex Porch & Floor |
| EXT 6.5F | Deck Stain | 1st | Deck Stain |
|  |  | 2nd | Deck Stain |
| EXT 6.5F | Latex Deck Coating |  | Latex Deck Coating, Apply in strict accordance with Manufacturer’s Instructions |
|  | (for plywood decks) |  |  |

EXT 6.6 – WOOD SHINGLE AND SHAKE SIDING (excluding roofs)

| EXT 6.6A | Latex | 1st | Oil/Alkyd Primer |
| --- | --- | --- | --- |
|  | (over alkyd primer) | 2nd | Latex |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Latex |
| EXT 6.6B | Alkyd | 1st | Oil/Alkyd Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 6.6C | Solid Colour Stain | 1st | Oil/Alkyd Primer |
|  |  | 2nd | Solid Colour Stain |
|  |  | 3rd | Solid Colour Stain |
| EXT 6.6D | Solid Colour Stain, Waterborne | 1st | Oil/Alkyd Primer |
|  |  | 2nd | Latex Stain |
|  |  | 3rd | Latex Stain |
| EXT 6.6E | Latex | 1st | Latex Wood Primer |
|  | (over latex primer) | 2nd | Latex |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Latex |
| EXT 6.6F | Semi-transparent Stain | 1st | Semi-transparent Stain |
|  |  | 2nd | Semi-transparent Stain |

EXT 6.7 – FIBERGLASS

| EXT 6.7A | Latex | 1st | Bonding Primer |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 6.7B | Alkyd | 1st | Bonding Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 6.7C | Waterborne Light Industrial Coating | 1st | Bonding Primer |
|  | Gloss Level [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |
| EXT 6.7D | Polyurethane, Pigmented | 1st | Epoxy |
|  | (over epoxy) | 2nd | Epoxy |
|  |  | 3rd | Polyurethane |
| EXT 6.7E | Epoxy, Water Based | 1st | W. B. Epoxy |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| EXT 6.7F | Epoxy | 1st | Epoxy |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |

EXT 6.8 – PLASTIC

| EXT 6.8A | Latex | 1st | Bonding Primer |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 6.8B | Alkyd | 1st | Bonding Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 6.8C | Waterborne Light Industrial Coating | 1st | Bonding Primer |
|  | Gloss Level [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |

EXT 9.1 - STUCCO

| EXT 9.1A | Latex | 1st | Latex |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 9.1B | Waterborne Light Industrial Coating | 1st | W. B. Light Industrial Coating |
|  | Gloss Level [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |
| EXT 9.1C | Elastomeric |  | Elastomeric Coating, Apply in strict accordance with manufacturer’s instructions. |
| EXT 9.1D | Epoxy | 1st | Epoxy |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| EXT 9.1E | Epoxy, Water Based | 1st | W. B. Epoxy |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| EXT 9.1F | Water Repellent (not paintable) |  | Water Repellent, Apply in strict accordance with manufacturer’s instructions. |
| EXT 9.1G | Water Repellent (paintable) |  | Water Repellent, Apply in strict accordance with manufacturer’s instructions. |
| EXT 9.1H | High Build Latex |  | High Build Latex, Apply in strict accordance with manufacturer’s instructions. |
| EXT 9.1J | Latex (over alkali resistant primer) | 1st | Alkali Resistant Primer |
|  | Gloss level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |

EXT 10.1 – CANVAS AND COTTON COVERINGS

| EXT 10.1A | Latex | 1st | Latex |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 10.1B | Waterborne Light Industrial Coating | 1st | W. B. Light Industrial Coating |
|  | Gloss Level [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |
| EXT 10.1C | Alkyd | 1st | Latex |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 10.1D | Aluminum Paint | 1st | Latex |
|  |  | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |

EXT 10.2 – BITUMINOUS COATED SURFACES

| EXT 10.2A | Latex | 1st | Rust Inhibitive Primer |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
| EXT 10.2B | Latex Aggregate, [Coarse] [Medium] texture, Gloss level [G1] [G5] [G6] |  | Latex Aggregate, Apply in strict accordance with manufacturer’s instructions. |
| EXT 10.2C | Alkyd | 1st | Rust Inhibitive Primer |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| EXT 10.2D | Aluminum Paint | 1st | Rust Inhibitive Primer |
|  |  | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |

- END OF SECTION