Section Cover Page

Section 09961 2000-04-14 Epoxy Wall Coatings

This Master Specification Section contains:

.1	This Cover Sheet

.2	Specification Section Text:

1.	General

1.1	Related Work Specified in Other Sections

1.2	Product Options and Substitutions

1.3	Qualifications

1.4	Samples

1.5	Manufacturer's Literature

1.6	Delivery

1.7	Storage

1.8	Environmental Conditions

1.9	Protection

2.	Products

2.1	Material

2.2	Colours

3.	Execution

3.1	Examination

3.2	Preparation/Application

3.3	Cleanup

3.4	Application Schedule

Applicable Standards

.1	ASTM D522-93a	Mandrel Bend Test of Attached Organic Coatings

.2	ASTM D1308-87(1993)el	Effect of Household Chemicals on Clear and Pigmented Organic Finishes

.3	ASTM D1360-90a(1995)a	Fire Retardancy of Paints (Cabinet Method)

.4	ASTM D2486-96	Scrub Resistance of Wall Paints

.5	ASTM E96-95	Water Vapour Transmission of Materials

.6	CGSB 1-GP-71	Methods of Testing Paints and Pigmets

These reference documents may be available for reference purposes in the Technical Resources and Standards Branch Library, Alberta Infrastructure, 3rd Floor, 6950 - 113 Street, Edmonton; Telephone: (780) 427-7924.

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	Substrate:	Section [   ].

.2	Sealants:	Section 07920.

.3	Epoxy flooring:	Section 09671.

.4	Painting:	Section 09901.

.5	Vinyl-acrylic coatings:	Section 09962.

1.2	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 1 for requirements pertaining to product options and substitutions.

1.3	QUALIFICATIONS

.1	The work of this Section shall be applied only by experienced applicators of the specified products.

1.4	SAMPLES

.1	Submit 300 mm x 300 mm representative sample of wall coating in selected colour.  Identify sample by project name including material and colour identification.

.2	Site apply sample installation to minimum 2 m2 area, to surface as directed, for approval by the Minister.  Retain approved sample until work is completed and accepted.

1.5	MANUFACTURER'S LITERATURE

.1	Make available copies of the material literature, clearly indicating conditions of acceptance for surfaces and methods of application on site before, and during, period of application of the work of this Section.

1.6	DELIVERY

.1	Deliver materials undamaged, in original containers, with manufacturer's labels and seals intact.

1.7	STORAGE

.1	Store materials in protected conditions with a minimum temperature of 12°C.

1.8	ENVIRONMENTAL CONDITIONS

.1	For exterior coatings:  Comply with coating manufacturer's recommendations.  Do not apply under adverse weather conditions which could affect coating performance.

.2	For interior coatings:  Minimum surface temperature 10°C 24 hours before, during and 24 hours after application or until cured; adequate controlled ventilation; bright, uniform lighting; broom clean; reasonably dust free.

1.9	PROTECTION

.1	Protect adjacent surfaces from damage and overspray resulting from work of this Section.  Mask or cover adjacent surfaces.  Make good any damage at own expense, to the Minister's satisfaction.

.2	Post "Wet Coatings" and "No Smoking" signs while work is in progress and curing.

2.	Products

2.1	MATERIAL

.1	Solvent based, two component thermo-setting, 100% epoxy coating meeting the following requirements:

| Property | Test Method | Requirement |
| --- | --- | --- |
| Water vapour transmission | ASTM E96-95 | 0.3 metric perms. max. |
| Colour fastness | CGSB 1-GP-71 Fade-ometer | No colour change, chalking or film defects, after 48 hours |
| Fire resistance | ASTM D1360-90a Cabinet method | Less than 17 g lost over masonry backing |
| Scrubbability | ASTM D2486-96 Gardner Scrubbability Machine | No effect on film after 5000 cycles |
| Radiation resistance | Exposure to Gamma rays of 35 roentgen intensity per hour at distance of 1625 mm from Cobalt 60 cell | Unaffected as measured by difference in reflectance |
| Toxicity | Evaluated by Canadian Department of Agriculture | Approved non-toxic |

Continued next page

2.1	MATERIALS (Cont'd)

| Property | Test Method | Requirement |
| --- | --- | --- |
| Heat & cold cycling | 50 cycles on masonry backing. Each cycle 8 hours at 70°C 16 hours at 23°C | No cracking, loss of adhesion, or other film defects |
| Flexibility | ASTM D522-93a Mandrel Test | Passing 3 mm bend without cracking or peeling |
| Impact resistance | CGSB 1-GP-71, Method 147.1 Gardner Impact Test | Passing 11 J without cracking |
| Stain resistance | ASTM D1308-87 | Not affected by common acids, hydroxides, salts and household cleaning agents |

SPEC NOTE:  The above material is used internally where optimum chemical and solvent resistance is required; recommended for meat and food processing plants.  The following materials meet the above requirements:  Armite manufactured by Macnaughton-Brooks Ltd., Epo-Kote manufactured by Everguard-Hallmark, Duroplast 100 manufactured by Duron Ltd., or approved alternative.

2.2	COLOURS

.1	[One] [Two] [     ] colours will be selected by the Minister from manufacturer's standard range.

OR

.1	Refer to Application Schedule.

SPEC NOTE:  Coordinate above with schedule at end of this Section.

3.	Execution

3.1	EXAMINATION

.1	Examine all surface conditions to which the work of this Section is to be applied.  Report any deficient surfaces to the Minister.

3.2	PREPARATION/APPLICATION

.1	Prepare surfaces and apply in accordance with manufacturer's instruction.

.2	Match finished work to approved samples, maintain uniform thickness, sheen, colour, texture and free from defects detrimental to appearance or performance.

.3	Minimum cured thickness of applied material shall be 200 to 250 micrometres.

3.3	CLEANUP

.1	Promptly, as the work proceeds and upon completion, clean up excess materials and rubbish.

3.4	APPLICATION SCHEDULE

| Room No./Name | Finish | [Colour] |
| --- | --- | --- |
| [ ] | [Satin] [Semi-gloss] [Gloss] | [ ] |
| [ ] | [ ] | [ ] |
| All other locations scheduled to receive epoxy coating | [ ] | [ ] |

END OF SECTION