Section Cover Page

Section 09962 2000-04-14 Vinyl Acrylic Coatings

This Master Specification Section contains:

.1	This Cover Sheet

.2	Specification Section Text:

1.	General

1.1	Related Work Specified in Other Sections

1.2	Product Options and Substitutions

1.3	Qualifications

1.4	Samples

1.5	Manufacturer's Literature

1.6	Delivery

1.7	Storage

1.8	Environmental Conditions

1.9	Protection

2.	Products

2.1	Materials

2.2	Colours

3.	Execution

3.1	Examination

3.2	Preparation/Application

3.3	Clean Up

3.4	Application Schedule

Applicable Standards

.1	ASTM D1308-87(1993)el	Effects of Household Chemicals on Clear and Pigmented Organic Finishes

.2	ASTM E84-96a	Surface Burning Characteristics of Building Materials

.3	ASTM E96-95	Water Vapour Transmission of Materials

.4	CGSB 1-GP-71	Methods of Testing Paints and Pigments

.5	CAN/CGSB-1.186-M89	High Performance Glazed Coating System, Interior

These reference documents may be available for reference purposes in the Technical Resources and Standards Branch Library, Alberta Infrastructure, 3rd Floor, 6950 - 113 Street, Edmonton; Telephone: (780) 427-7924.

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	Substrate:	Section [     ].

.2	Sealants:	Section 07920.

.3	Epoxy flooring:	Section 09671.

.4	Painting:	Section 09901.

.5	Epoxy (wall) coating:	Section 09961.

.6	Polyurethane coating:	Section [     ].

.7	Aggregate wall coating:	Section [     ].

1.2	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 1 for requirements pertaining to product options and substitutions.

1.3	QUALIFICATIONS

.1	The work of this Section shall be applied only by experienced applicators of the specified products.

1.4	SAMPLES

.1	Submit 300 x 300 mm representative sample coating in selected colour.  Identify sample by project name including material and colour identification.

.2	Site apply sample installation to minimum 2.0 m2 area, to surface as directed, for approval by the Minister.  Retain approved sample until work is completed and accepted.

1.5	MANUFACTURER'S LITERATURE

.1	Make available copies of the material literature, clearly indicating conditions of acceptance for surfaces and methods of application on site before, and during, period of application of the work of this Section.

1.6	DELIVERY

.1	Deliver materials undamaged, in original containers, with manufacturer's labels and seals intact.

1.7	STORAGE

.1	Store material in protected conditions with a minimum temperature of 13°C.

1.8	ENVIRONMENTAL CONDITIONS

.1	For exterior coatings:  Comply with coating manufacturer's recommendations.  Do not apply under adverse weather conditions which could effect coating performance.

.2	For interior coatings:  Minimum surface temperature 10°C 24 hours before, during and 24 hours after application; bright, uniform lighting; broom clean; reasonably dust free.

1.9	PROTECTION

.1	Protect adjacent surfaces from damage or overspray resulting from work of this Section.  Mask and/or cover adjacent surfaces.  Make good any damage at own expense, to the Minister's satisfaction.

.2	Post "Wet Coatings" and "No Smoking" signs, while work is in progress and curing.

2.	Products

2.1	MATERIALS

.1	Emulsion based, vinyl acrylic, mastic coating meeting the following minimum property requirements and complying with CAN/CGSB-1.186-M89:

| Property | Test Method | Requirement |
| --- | --- | --- |
| Fire resistance | ASTM E84-96a | Flame spread 0 Fuel contributed 5 Max. smoke developed 10 |
| Scrubbability | CGSB 1-GP-71 Method 125.1 | No loss of gloss or other deleterious defects for 10,000 cycles |
| Colour fastness | CGSB 1-GP-71 Fademeter | No colour change after 48 hours |
| Impact resistance | CGSB 1-GP-71 Method 147.1 Gardner | Unaffected at 1.1 J 9.0 J min. |
| Water vapour | ASTM E96-95 | 0.3 metric perms max |
| Toxicity | Canadian Dept. of Agriculture | Approved nontoxic |
| Stain resistance | ASTM D1308-87 (R1993) | Not affected by common acids, hydroxides, salts and household cleaning agents |

SPEC NOTE:  The above material is used in wet or high humidity conditions or where coating is steam cleaned.  The following materials meet the above requirements:  Glazetite Type II, by Macnaughton-Brooks Ltd., Evrok, by Everguard-Hallmark, Duroplast 300, by Duron Co. Ltd.

2.2	COLOURS

.1	[One] [Two] [     ] colours will be selected by Minister from manufacturer's standard range.

OR

.1	Refer to Application Schedule.

3.	Execution

3.1	EXAMINATION

.1	Examine all surfaces conditions to which the work of this Section is to be applied.  Report any deficient surfaces to the Minister.

3.2	PREPARATION/APPLICATION

.1	Prepare surfaces and apply as directed in the manufacturer's literature.

.2	Match finished work to approved samples, maintain uniform in thickness, sheen, colour, texture and free from defects detrimental to appearance or performance.

.3	Minimum cured thickness of applied material to be 380 micrometres.

3.3	CLEANUP

.1	Promptly, as the work proceeds and upon completion, clean up excess materials and rubbish.

3.4	APPLICATION SCHEDULE

| Room No./Name | Finish | [Colour] |
| --- | --- | --- |
| [ ] | [satin] [semi-gloss] [tile-like] | [ ] |
| [ ] | [ ] | [ ] |
| All other locations scheduled to receive vinyl acrylic coating | [ ] | [ ] |

END OF SECTION